SUPPLEMENTARY MATERIAL

Data mining in photocatalytic water splitting over perovskites literature for higher hydrogen production

Elif Cana, Ramazan Yildirim*a

aDepartment of Chemical Engineering, Bogazici University, Istanbul, 34342, Turkey.

E-mail: yildirra@boun.edu.tr

| Contents | Page |
| --- | --- |
| S1. Additional Information for Computational Section | 2 |
| S2. Additional Results for Review and Pre-Analysis of Database | 8 |
| S3. Additional Results for Machine Learning Analysis | 13 |
| References | 21 |
| Appendix A. Database | 22 |

S1. Additional Information for Computational Section

S.1.1 Constructing the database

Database for hydrogen production rate and stability are given in Appendix A.

S.1.2. Computational Details

The input variables used in analysis and their ranges are given in Table S1. In most of the articles, the hydrogen production (μmol g-cat-1) was reported as a function time to show the performance. However, the hydrogen production in all these papers increased almost linearly with time; consequently, the hydrogen production rate  (μmol g-cat-1h-1) used as the input variable to eliminate time from the input list.

For association rule mining and decision tree classification, each datasets were categorized in three classes as low, medium and high hydrogen production rates. The data between 0.08-30, 30-350, and 350-21318 (μmol gcat-1 h-1) were respectively labelled as low, medium and high for visible light while 0.001-130, 130-550, and 550-36750 (μmol gcat-1 h-1) intervals were used for UV data. This way, the number of data points in classes become approximately equal to prevent class imbalance problem.

The band gap data were also divided into three classes: 143 instances for visible (1.27-3.1125 eV) (visible), 120 instances for UV_A (3.1125-3.89 eV) and 109 instances for high UV_BC (3.89-6.3 eV), which refers to UV-B + UV-C together.

The 4-fold cross validation procedure was applied in decision tree and random forest analysis; the dataset was divided into four smaller sets, and the model was built with three subsets (training) and tested with the remaining subset. This procedure rotated four times and the average testing error was used to evaluate the fitness of the model (successful in classifying or predicting the unseen data, and valid for the entire range). For each method, the root mean square error for testing (RMSE) was calculated for various models with varying complexity and the model giving the minimum average RMSE for testing was selected as the best model.

The multicollinearity, which may be exist among the catalyst preparation variables and measured characteristic, were checked, and no significant correlation were detected.

Table S1. Input variables included into the dataset and their ranges

| Input Variable | Ranges for continuous or identities for discrete variables |
| --- | --- |
| Elements Used in A site of Perovskite (including both host and doped elements) (ABX3) | Ag, Ba, Bi, Ca, Ce, Co, Cr, Cu, Ga, H, In, K, La, Li, Mn, Na, Ni, Sb, Sm, Sn, Sr, Ta, Y, Yb, Zn |
| Elements Used in B site of Perovskite (including both host and doped elements) (ABX3) | Bi, Cd, Co, Cr, Cu, Fe, Ga, In, K, Nb, Ni, Rh, Sb, Sn, Ta, Ti, Zr |
| Elements Used in X site of Perovskite (including both host and doped elements) (ABX3) | N, O, S |
| Weight Percent of A site | 0.070 - 0.770 |
| Weight Percent of B site | 0.050 - 0.770 |
| Weight Percent of X site | 0.053 - 0.540 |
| Perovskite Preparation Methods | Co-precipitation (co-pre), electrospinning (ES), flux-type, hydrothermal (HT), ion-exchange (IE), novel, polymerized complex (PC), Pechini-type process (PTP), sol-gel, (SG), solid state reaction (SSR) |
| Calcination Temperature (K) | maximum 1773 |
| Calcination Time (hour) | maximum 72 |
| Promoter Loading Methods | Impregnation, photo-deposition (PD) |
| Elements Used as Promoters | Ag, Au, Cu, IrO2, Ni, NiO, Pt, Rh, Ru, RuO2 |
| Weight Percent of Promoter | maximum 8 |
| Crystal Structure | amorphous, cubic, hexagonal, monoclinic, octahedral, orthorhombic,polyhedron, rhombohedral, tetragonal |
| Band Gap (eV) | 1.27 -5.85 |
| Surface Area (m2/g) | 0.3 -206.5 |
| Catalyst Weight (g/L) | 0.2 -12.5 |
| Percent of Alcohol in Reaction Solution | 0 -100 |
| Sacrificial Agents Used in Reaction Solution | AgNO3, CH2O, CH3COOH, C3H8O CH4, FeCl3, H2SO4,NaI KNO3, HCOOH, KOH, Na2S, Na2SO3, Na2SO4, NaNO2, NaOH |
| Light Types | halogen, Hg lamp, UV, visible, Xe lamp |
| Power of Light (W) | 8 - 1000 |
| Minimum Wavelength of Light (nm) | 200 - 440 |

S.1.2.1. Association rule mining

The apriori algortihm in the package of arules was used for modelling and arulesViz was preferred for visualization of the rules obtained.[S1,S2]

S.1.2.2. Classification tree

The package of rpart, which can handle both categorical and continuous variables, was used to construct classification trees.[S3] The complexity of the decision tree models were adjusted by changing minsplit, which is the allowable minimum number of instances in a node before splitting. As it was expected, when minsplit number decreased the trees became bigger and model became more complex. The testing and training errors were evaluated with the increasing model complexity or decreasing minsplit number to prevent over-prediction. For all datasets (visible, UV and band gap datasets) the minsplit numbers were changed between 5 and 50 and, the over-prediction was not observed even with the minsplit of five. Then, the complexity parameter (cp), hence the depth of tree, was changed at the minsplit value of 5 to see the changes in cross validation error. Figure S7 shows the cross validation error (X_val Relative Error) versus complexity parameter (cp) plots, which were constructed using printcp or plotcp functions of rpart, for hydrogen production models and the band gap are presented in. In these figures, y-axis represents X_val Relative Error, while lower x-axis is for cp and the upper x-axis stands for the depth of decision tree (last two are directly corelated). In the plot on the left (visible light hydrogen production) and the middle (UV light hydrogen production) the error continue to decrease with increasing cp in entire range while there is an optimum value of cp (0.03) for band gap. Hence, the optimum tree was constructed by adjsuting the minsiplit values for hydrogen production data whereas the cp value of 0.03 was used for band gap dataset. For the hydrogen production models, the minsplit values resulting the highest accuracy for high and low classes and with the simplest structure (for easy to follow heuristics for future works) were selected; the accuracy of high class is important to learn what to do while that of low class serves to determine what to avoid for high hydrogen production rates. These values for  minsplit were found to be 15 and 10 visible and UV dataset respectively.

Fig. S1. The cross validation error vs. complexity parameter and depth of tree for visible dataset (left), UV dataset (middle), and band gap dataset (right)

Class imbalance is a problem in machine learning classification algorithms where number of instances in one class is much higher than that of in another class. If the problem exists between the classes generated, the training algorithm will be biased towards the class with higher number of instances, so the model will fail to predict the output class correctly in testing step. In our work the number of instances in low, medium, and high classes, as can be seen Table S2 below, were adjusted to prevent class imbalance problem.

Table S2. Number of instances in each classes of visible and UV dataset

| Dataset | Low | Medium | High |
| --- | --- | --- | --- |
| UV | 109 | 106 | 109 |
| Visible | 73 | 71 | 72 |

In the case of band gap prediction the upper and lower limits of visible, UV_A, and UV_BC classes were defined according to the wavelength regions of visible, UV-A, and UV-B & UV-C lights. [S4] For example; the lower limit of visible bang gap class (1.27 eV) is the minimum band gap of instances recorded into the dataset, and the upper limit of visible class is defined as 3.1125 eV. That number (3.1125) was found by calculating the corresponding band gap value to the lower limit of wavelength of visible light (400 nm). At the end of those calculations, the number of instances in visible, UV_A, and UV_BC classes were 143, 120, and 109, respectively. This may create a class inbalance problem favoring the visible class; however the limits of classes have physical meanings, therofe they could not be changed. Altough random sampling (i.e. the duplicating some data points in the small classes randomly) could be used to adjust the class sizes, it was not needed in this work because the difference in class sizes were not too big, and the testing prediction accuracies for all classes were sufficiently high.

S.1.2.3 Random Forest

The prediction of outputs (band gap or hydrogen production rate) was carried out by random forest algorithm and randomForest package of R was used for this purpose.[S5] The number of trees, ntree and, allowable minimum number of instances in a node before splitting nodesize was tuned to reach best predictivity.

Since random forest creates decision trees using variables and instances randomly selected, it is not possible to produce exactly same model in even consecutive runs. Therefore set.seed function in R was used for pseudo-random number generation and reproduce same models.[S6]

The complexity of the random fores models were adjusted by changing ntree and nodesize. As ntree increases and/or nodesize decreases, model become more complex. The testing and training errors were evaluated with the increasing algorithm complexity (decreasing nodesize and/or increasing ntree number) to prevent over-prediction, but over-prediction was not observed when ntree changes from 1 to 100 and nodesize was changed from 1 to 5 for all datasets. Therefore the ntree and nodesize values which gave the highest R2 and lowest rmse were recorder for each dataset and then the ultimate models were developed by using those ntree and nodesize values. The ultimaye model for visible data set was constructed using ntree value of 16 and the nodesize of 2 while those values were 16 and 4 respectively for the UV dataset.  For band gap dataset, the ntree was selected as 13, and the nodesize was taken as 5.

S.1.2.4 Complementary R-Packages Used

Also some other packages of R were used as complementary to data mining algorithms used. RMSE and MAE (mean absolute error) of models were evaluated using rmse and mae functions of hydroGOF package in R [S7] or rmse and mae functions of Metrics package in R.[S8]  The xlsx package of R was used to import the matrices from R to Excel. To check whether multicollinearity was a problem or not among the input variables, corrplot package of R was used both finding correlation and displaying them.[S9] For better visualization of decision trees fancyRpartplot function of the package rattle was preferred.[S10]

S2. Additional Results for Review and Pre-Analysis of Database

Table S3. Frequency of A and B doping for the most commonly used perovskites

(i.e. complete list of dopants for most common perovskites)

|  | Total | A-Single Doped | A-Double Doped | B-Single Doped | B-Double Doped | A and B Co-doped | X-Single Doped |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Tantalates | 200 | 43 | 23 | 32 | 0 | 17 | 7 |
| BaTaO | 6 | Ni (1) | 0 | Zr (1) | 0 | 0 | 0 |
| BiTaO | 33 | Ca (6), Ba (6), Sr (1) | K-La (5) | Cu (4) | 0 | 0 | 0 |
| CaTaO | 8 | 0 | 0 | Zr (7) | 0 | 0 | N (6) |
| InTaO | 3 | Ni (1) | 0 | 0 | 0 | 0 | N (1) |
| KTaO | 25 | 0 | Ca-Sr (18) | Zr (1) | 0 | La-Bi (1) | 0 |
| LaTaO | 12 | K (1), H(1) | 0 | Al (7) | 0 | 0 | 0 |
| NaTaO | 92 | Ba (1), Bi (1), Ca (1), Ce (2), K (6), La (9), Sr (2), Y (2), Yb (2) | 0 | Bi (6), Nb (6) | 0 | La-Co (1), La-Cr (1) | 0 |
| SrTaO | 21 | Bi (1), H (1) | 0 | 0 | 0 | H-Nb (10), Bi-Ce (4) | 0 |
| Titanates | 109 | 13 | 0 | 17 | 7 | 22 | 2 |
| BaTiO | 3 | 0 | 0 | 0 | 0 | La-Cr (2) | 0 |
| BiTiO | 7 | Na (6) | 0 | 0 | 0 | 0 | N (1) |
| CaTiO | 11 | 0 | 0 | 0 | 0 | La-Cr (8) | 0 |
| CrTiO | 1 | 0 | 0 | Ta (1) | 0 | 0 | 0 |
| KTiO | 7 | Sn (1) | 0 | 0 | 0 | 0 | 0 |
| NaTiO | 8 | La (1) | 0 | Zr (2) | 0 | 0 | 0 |
| SmTiO | 1 | 0 | 0 | 0 | 0 | 0 | S (1) |
| SrTiO | 71 | Ag (1), Cr (2), La (1), Na (1) | 0 | Al (13), Fe (1) | Rh-Sb (7) | La-Cr (8), Cr-Sb (1), Bi-Fe (1), Cr-Ta (1), Ni-Ta (1) | 0 |
| Niobates | 89 | 20 | 0 | 25 |  | 11 | 0 |
| BaNbO | 6 | Ni (1), Zn (2) | 0 | Co (1), Ta (1) | 0 | 0 | 0 |
| BiNbO | 9 | Ba (1), Ca (1), Sr (1) | 0 | 0 | 0 | La-Al (6) | 0 |
| CoNbO | 3 | Ba (1), Ca (1), Sr (1) | 0 | 0 | 0 | 0 | 0 |
| InNbO | 3 | Ba (1), Ca (1), Sr (1) | 0 | 0 | 0 | 0 | 0 |
| KNbO | 18 | 0 | 0 | Zr (6) | 0 | 0 | 0 |
| LaNbO | 13 | H (1) | 0 | Ta (5) | 0 | H-In (5) | 0 |
| NaNbO | 33 | Ca (4) | 0 | In (11) | 0 | 0 | 0 |
| SrNbO | 4 | H (3) | 0 | Al (1) | 0 | 0 | 0 |
| Indium- based | 22 | 5 | 0 | 6 | 0 | 0 | 0 |
| BaInO | 1 | 0 | 0 | Ta (1) | 0 | 0 | 0 |
| CuInS | 7 | 0 | 0 | Ga (5) | 0 | 0 | 0 |
| ZnInS | 14 | Ag (5) | 0 | 0 | 0 | 0 | 0 |
| Others |  |  |  |  |  |  |  |
| ZnCdS | 15 | Cu (5) | 0 | 0 | 0 | 0 | 0 |
| SrSnO | 9 | Ba (1) | 0 | 0 | 0 | 0 | 0 |

Table S4. The average calcination temperature of the samples prepared using different methods

|  | Average Calcination Temperature |  |  | Number of Instances |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Visible | UV_A | UV_BC | Visible | UV_A | UV_BC |
|  | 1.27-3.11 eV | 3.11-3.89 eV | 3.89-6.3 eV | 1.27-3.11 eV | 3.11-3.89 eV | 3.89-6.3 eV |
| SSR | 1284.6 | 1166.2 | 1297.3 | 43 | 61 | 84 |
| HT | 273.28 | 401.29 | 534.6 | 88 | 38 | 20 |
| PC | 993.83 | 1123 | 1225.3 | 12 | 17 | 22 |
| SG | 984.82 | 1008 | 1075.9 | 11 | 10 | 17 |

- Calcination temperature was taken as 273 K if no calcination was employed.

Fig. S2. Effects of inorganic sacrificial agents on average hydrogen production rates for visible and UV light conditions

Fig. S3. Stability of some titanates. For each perovskite, bottom bar is the first run, the others are repeats in increasing order;* duration of test;**rate in first run.

Fig. S4. Stability of some niobates. For each perovskite, bottom bar is the first run, the others are repeats in increasing order;* duration of test;**rate in first run.

Fig. S5. Stability of some indium-based perovskites. For each perovskite, bottom bar is the first run, the others are repeats in increasing order;* duration of test;**rate in first run.

S3. Additional Results for Machine Learning Analysis

Table S5. Results of association rule mining for visible light data for production rate class high

| LHS We are interested in this production rate level |  | RHS This feature was used in production rate levels in LHS | Support This is fraction of all data belonging to class in LHS and has feature in RHS | Confidence This is fraction of data belonging to class in LHS and has feature in RHS | Lift This fraction of data in LHS has feature in RHS / this fraction of data in all data has feature in RHS |
| --- | --- | --- | --- | --- | --- |
| HIGH | 350 (μmol/gcat.h) and above | {Undoped_Perovskite=ZnCdS} | 0.07 | 0.21 | 3.00 |
|  |  | {Prep_Meth=novel} | 0.13 | 0.39 | 2.33 |
|  |  | {SacAgent1=Na2S} | 0.13 | 0.39 | 2.27 |
|  |  | {SacAgent2=Na2SO3} | 0.13 | 0.39 | 2.27 |
|  |  | {SurfaceArea=9} | 0.07 | 0.22 | 2.09 |
|  |  | {Calctime=2} | 0.05 | 0.15 | 1.94 |
|  |  | {Undoped_Perovskite=NaTaO} | 0.08 | 0.24 | 1.89 |
|  |  | {Promoter=NAN} | 0.17 | 0.51 | 1.73 |
|  |  | {Calctime=NAN} | 0.19 | 0.57 | 1.60 |
|  |  | {Crystal=hexagonal} | 0.06 | 0.18 | 1.56 |
|  |  | {CalcT=NAN} | 0.14 | 0.43 | 1.48 |
|  |  | {Crystal=orthorombic} | 0.10 | 0.31 | 1.43 |
|  |  | {Prom_Meth=NAN} | 0.19 | 0.58 | 1.38 |
|  |  | {CalcT=5} | 0.07 | 0.22 | 1.33 |
|  |  | {Alcohol%=NAN} | 0.18 | 0.54 | 1.26 |
|  |  | {SurfaceArea=4} | 0.16 | 0.49 | 1.15 |
|  |  | {B_1stdoped=NAN} | 0.21 | 0.63 | 1.05 |
|  |  | {B_2nddoped=NAN} | 0.33 | 1.00 | 1.03 |
|  |  | {Prep_Meth=HT} | 0.12 | 0.36 | 1.03 |
|  |  | {Alcohol%=2} | 0.08 | 0.25 | 1.00 |
|  |  | {A_2nddoped=NAN} | 0.33 | 1.00 | 1.00 |

Table S6. Results of Association rule mining for UV light data for production rate class high

| LHS We are interested in this production rate level |  | RHS This feature was used in production rate levels in LHS | Support This is fraction of all data belonging to class in LHS and has feature in RHS | Confidence This is fraction of data belonging to class in LHS and has feature in RHS | Lift This fraction of data in LHS has feature in RHS / this fraction of data in all data has feature in RHS |
| --- | --- | --- | --- | --- | --- |
| HIGH | 350 (μmol/gcat.h) and above | {SacAgent1=NaNO2} | 0.06 | 0.19 | 2.33 |
|  |  | {Alcohol%=2} | 0.14 | 0.43 | 1.83 |
|  |  | {SurfaceArea=6} | 0.05 | 0.16 | 1.46 |
|  |  | {Undoped_Perovskite=NaTaO} | 0.10 | 0.29 | 1.45 |
|  |  | {CalcT=8} | 0.08 | 0.25 | 1.42 |
|  |  | {Calctime=NAN} | 0.07 | 0.22 | 1.36 |
|  |  | {CalcT=NAN} | 0.07 | 0.22 | 1.36 |
|  |  | {Crystal=octahedral} | 0.07 | 0.20 | 1.22 |
|  |  | {Calctime=7} | 0.06 | 0.17 | 1.21 |
|  |  | {Calctime=2} | 0.07 | 0.20 | 1.20 |
|  |  | {Prom_Meth=PD} | 0.09 | 0.28 | 1.16 |
|  |  | {Promoter=NAN} | 0.15 | 0.46 | 1.06 |
|  |  | {Prom_Meth=NAN} | 0.15 | 0.46 | 1.06 |
|  |  | {A_2nddoped=NAN} | 0.32 | 0.96 | 1.04 |
|  |  | {SacAgent2=NAN} | 0.33 | 1.00 | 1.00 |
|  |  | {Promoter=NiO} | 0.06 | 0.18 | 1.00 |
|  |  | {B_2nddoped=NAN} | 0.33 | 1.00 | 1.00 |

Table S7. Distribution of data points among the performance classes for significant variables (visible light dataset)

| LHS | RHS | Support | Confidence | Lift |
| --- | --- | --- | --- | --- |
| {Undoped_Perovskite=NaTaO} | {ProdRate=HIGH} | 0.079 | 0.630 | 1.889 |
| {Undoped_Perovskite=NaTaO} | {ProdRate=MEDIUM} | 0.009 | 0.074 | 0.225 |
| {Undoped_Perovskite=NaTaO} | {ProdRate=LOW} | 0.037 | 0.296 | 0.877 |
| LHS | RHS | Support | Confidence | Lift |
| {Undoped_Perovskite=SrTiO} | {ProdRate=HIGH} | 0.04 | 0.16 | 0.47 |
| {Undoped_Perovskite=SrTiO} | {ProdRate=MEDIUM} | 0.13 | 0.55 | 1.67 |
| {Undoped_Perovskite=SrTiO} | {ProdRate=LOW} | 0.07 | 0.29 | 0.87 |
| LHS | RHS | Support | Confidence | Lift |
| {Prep_Meth=SSR} | {ProdRate=HIGH} | 0.03 | 0.15 | 0.44 |
| {Prep_Meth=SSR} | {ProdRate=MEDIUM} | 0.07 | 0.33 | 1.01 |
| {Prep_Meth=SSR} | {ProdRate=LOW} | 0.12 | 0.52 | 1.54 |
| LHS | RHS | Support | Confidence | Lift |
| {Prep_Meth=HT} | {ProdRate=HIGH} | 0.12 | 0.34 | 1.03 |
| {Prep_Meth=HT} | {ProdRate=MEDIUM} | 0.15 | 0.42 | 1.28 |
| {Prep_Meth=HT} | {ProdRate=LOW} | 0.08 | 0.24 | 0.70 |
| LHS | RHS | Support | Confidence | Lift |
| {Prep_Meth=PC} | {ProdRate=HIGH} | 0.00 | 0.00 | 0.00 |
| {Prep_Meth=PC} | {ProdRate=MEDIUM} | 0.01 | 0.20 | 0.61 |
| {Prep_Meth=PC} | {ProdRate=LOW} | 0.03 | 0.70 | 2.07 |
| LHS | RHS | Support | Confidence | Lift |
| {Prep_Meth=SG} | {ProdRate=HIGH} | 0.01 | 0.30 | 0.90 |
| {Prep_Meth=SG} | {ProdRate=MEDIUM} | 0.00 | 0.00 | 0.00 |
| {Prep_Meth=SG} | {ProdRate=LOW} | 0.03 | 0.60 | 1.78 |
| LHS | RHS | Support | Confidence | Lift |
| {Promoter=Pt} | {ProdRate=HIGH} | 0.09 | 0.21 | 0.63 |
| {Promoter=Pt} | {ProdRate=MEDIUM} | 0.18 | 0.41 | 1.25 |
| {Promoter=Pt} | {ProdRate=LOW} | 0.17 | 0.38 | 1.12 |
| LHS | RHS | Support | Confidence | Lift |
| {Promoter=NAN} | {ProdRate=HIGH} | 0.17 | 0.58 | 1.73 |
| {Promoter=NAN} | {ProdRate=MEDIUM} | 0.06 | 0.22 | 0.67 |
| {Promoter=NAN} | {ProdRate=LOW} | 0.06 | 0.20 | 0.60 |
| LHS | RHS | Support | Confidence | Lift |
| {Crystal=cubic} | {ProdRate=HIGH} | 0.12 | 0.30 | 0.91 |
| {Crystal=cubic} | {ProdRate=MEDIUM} | 0.12 | 0.30 | 0.92 |
| {Crystal=cubic} | {ProdRate=LOW} | 0.16 | 0.40 | 1.17 |
| LHS | RHS | Support | Confidence | Lift |
| {Crystal=orthorombic} | {ProdRate=HIGH} | 0.10 | 0.48 | 1.43 |
| {Crystal=orthorombic} | {ProdRate=MEDIUM} | 0.09 | 0.43 | 1.32 |
| {Crystal=orthorombic} | {ProdRate=LOW} | 0.02 | 0.09 | 0.26 |

| Table S7.Continued |  |  |  |  |
| --- | --- | --- | --- | --- |
| LHS | RHS | Support | Confidence | Lift |
| {Alcohol%=NAN} | {ProdRate=HIGH} | 0.18 | 0.42 | 1.26 |
| {Alcohol%=NAN} | {ProdRate=MEDIUM} | 0.11 | 0.25 | 0.75 |
| {Alcohol%=NAN} | {ProdRate=LOW} | 0.14 | 0.33 | 0.99 |
| LHS | RHS | Support | Confidence | Lift |
| {Alcohol%=20} | {ProdRate=HIGH} | 0.08 | 0.33 | 1.00 |
| {Alcohol%=20} | {ProdRate=MEDIUM} | 0.06 | 0.24 | 0.73 |
| {Alcohol%=20} | {ProdRate=LOW} | 0.11 | 0.43 | 1.26 |
| LHS | RHS | Support | Confidence | Lift |
| {SacAgent1=Na2S} | {ProdRate=HIGH} | 0.13 | 0.76 | 2.27 |
| {SacAgent1=Na2S} | {ProdRate=MEDIUM} | 0.04 | 0.22 | 0.66 |
| {SacAgent1=Na2S} | {ProdRate=LOW} | 0.00 | 0.00 | 0.00 |

Table S8. Distribution of data points among the performance classes for significant variables

(UV dataset)

| LHS | RHS | Support | Confidence | Lift |
| --- | --- | --- | --- | --- |
| {Undoped_Perovskite=NaTaO} | {ProdRate=HIGH} | 0.10 | 0.48 | 1.45 |
| {Undoped_Perovskite=NaTaO} | {ProdRate=MEDIUM} | 0.07 | 0.35 | 1.08 |
| {Undoped_Perovskite=NaTaO} | {ProdRate=LOW} | 0.03 | 0.17 | 0.49 |
| LHS | RHS | Support | Confidence | Lift |
| {Undoped_Perovskite=SrTiO} | {ProdRate=HIGH} | 0.03 | 0.38 | 1.13 |
| {Undoped_Perovskite=SrTiO} | {ProdRate=MEDIUM} | 0.02 | 0.33 | 1.03 |
| {Undoped_Perovskite=SrTiO} | {ProdRate=LOW} | 0.02 | 0.29 | 0.85 |
| LHS | RHS | Support | Confidence | Lift |
| {Prep_Meth=SSR} | {ProdRate=HIGH} | 0.13 | 0.30 | 0.90 |
| {Prep_Meth=SSR} | {ProdRate=MEDIUM} | 0.11 | 0.26 | 0.79 |
| {Prep_Meth=SSR} | {ProdRate=LOW} | 0.19 | 0.44 | 1.29 |
| LHS | RHS | Support | Confidence | Lift |
| {Prep_Meth=HT} | {ProdRate=HIGH} | 0.07 | 0.31 | 0.92 |
| {Prep_Meth=HT} | {ProdRate=MEDIUM} | 0.08 | 0.35 | 1.07 |
| {Prep_Meth=HT} | {ProdRate=LOW} | 0.08 | 0.35 | 1.01 |
| LHS | RHS | Support | Confidence | Lift |
| {Prep_Meth=PC} | {ProdRate=HIGH} | 0.03 | 0.27 | 0.80 |
| {Prep_Meth=PC} | {ProdRate=MEDIUM} | 0.06 | 0.49 | 1.50 |
| {Prep_Meth=PC} | {ProdRate=LOW} | 0.03 | 0.24 | 0.71 |
| LHS | RHS | Support | Confidence | Lift |
| {Prep_Meth=SG} | {ProdRate=HIGH} | 0.05 | 0.57 | 1.71 |
| {Prep_Meth=SG} | {ProdRate=MEDIUM} | 0.03 | 0.32 | 0.99 |
| {Prep_Meth=SG} | {ProdRate=LOW} | 0.01 | 0.11 | 0.31 |

| Table S8.Continued |  |  |  |  |
| --- | --- | --- | --- | --- |
| LHS | RHS | Support | Confidence | Lift |
| {Promoter=Pt} | {ProdRate=HIGH} | 0.08 | 0.33 | 0.98 |
| {Promoter=Pt} | {ProdRate=MEDIUM} | 0.11 | 0.42 | 1.30 |
| {Promoter=Pt} | {ProdRate=LOW} | 0.06 | 0.25 | 0.74 |
| LHS | RHS | Support | Confidence | Lift |
| {Promoter=NAN} | {ProdRate=HIGH} | 0.15 | 0.35 | 1.06 |
| {Promoter=NAN} | {ProdRate=MEDIUM} | 0.13 | 0.29 | 0.90 |
| {Promoter=NAN} | {ProdRate=LOW} | 0.15 | 0.35 | 1.04 |
| LHS | RHS | Support | Confidence | Lift |
| {Crystal=cubic} | {ProdRate=HIGH} | 0.07 | 0.26 | 0.77 |
| {Crystal=cubic} | {ProdRate=MEDIUM} | 0.09 | 0.32 | 1.00 |
| {Crystal=cubic} | {ProdRate=LOW} | 0.12 | 0.42 | 1.22 |
| LHS | RHS | Support | Confidence | Lift |
| {Crystal=orthorombic} | {ProdRate=HIGH} | 0.08 | 0.33 | 0.98 |
| {Crystal=orthorombic} | {ProdRate=MEDIUM} | 0.05 | 0.21 | 0.66 |
| {Crystal=orthorombic} | {ProdRate=LOW} | 0.11 | 0.46 | 1.35 |
| LHS | RHS | Support | Confidence | Lift |
| {Alcohol%=NAN} | {ProdRate=HIGH} | 0.12 | 0.22 | 0.67 |
| {Alcohol%=NAN} | {ProdRate=MEDIUM} | 0.19 | 0.37 | 1.14 |
| {Alcohol%=NAN} | {ProdRate=LOW} | 0.21 | 0.41 | 1.20 |
| LHS | RHS | Support | Confidence | Lift |
| {Alcohol%=20} | {ProdRate=HIGH} | 0.14 | 0.61 | 1.83 |
| {Alcohol%=20} | {ProdRate=MEDIUM} | 0.04 | 0.17 | 0.52 |
| {Alcohol%=20} | {ProdRate=LOW} | 0.05 | 0.22 | 0.64 |
| LHS | RHS | Support | Confidence | Lift |
| {SacAgent1=Na2S} | {ProdRate=HIGH} | 0.00 | 0.00 | 0.00 |
| {SacAgent1=Na2S} | {ProdRate=MEDIUM} | 0.02 | 0.22 | 0.69 |
| {SacAgent1=Na2S} | {ProdRate=LOW} | 0.06 | 0.78 | 2.33 |

Fig. S6.  Optimal decision tree for UV light data.

Table S9. Confusion matrix for UV light data

| Actual Data |  | Predictions |  |  | Prediction |
| --- | --- | --- | --- | --- | --- |
| Class | # of data | LOW | MEDIUM | HIGH | Accuracy % |
| LOW | 109 | 89 | 13 | 7 | 81.65 |
| MEDIUM | 106 | 18 | 68 | 20 | 64.15 |
| HIGH | 109 | 9 | 7 | 93 | 85.32 |

Table S10. Confusion matrix for visible light data*

| Actual Data |  | Predictions |  |  | Prediction |
| --- | --- | --- | --- | --- | --- |
| Class | # of data | LOW | MEDIUM | HIGH | Accuracy % |
| LOW | 73 | 64 | 8 | 1 | 87.67 |
| MEDIUM | 71 | 6 | 58 | 7 | 81.69 |
| HIGH | 72 | 2 | 15 | 55 | 76.39 |

*First column on the right shows the actual number of data in each classes. The columns labeled as “prediction” indicate the classes in which the data placed. For example, there are 73 data points in high classes and tree accurately placed 64 of them while it placed 8 into medium and 1 into low classes. Consequently the prediction accuracy for high classes is (64/73)*100 = 87.67

Fig. S7 Predictions by random forest model for UV data

Table S11. Predictive variables for band bap

| Input Variable | Ranges for continuous or identities for discrete variables |
| --- | --- |
| Elements Used in A site of Perovskite (ABX3) | Ag, Ba, Bi, Ca, Ce, Co, Cr, Cu, Ga, H, In, K, La, Li, Mn, Na, Ni, Sb, Sm, Sn, Sr, Ta, Y, Yb, Zn |
| Elements Used in B site of Perovskite (ABX3) | Bi, Cd, Co, Cr, Cu, Fe, Ga, In, K, Nb, Ni, Rh, Sb, Sn, Ta, Ti, Zr |
| Elements Used in X site of Perovskite (ABX3) | N, O, S |
| Weight Percent of A site | 0.070 - 0.770 |
| Weight Percent of B site | 0.050 - 0.770 |
| Weight Percent of X site | 0.053 - 0.540 |
| Perovskite Preparation Methods | Co-precipitation (co-pre), electrospinning (ES), flux-type, hydrothermal (HT), ion-exchange (IE), novel, polymerized complex (PC), Pechini-type process (PTP), sol-gel, (SG), solid state reaction (SSR) |
| Calcination Temperature (K) | maximum 1773 |
| Calcination Time (hour) | maximum 72 |

Table S12. Confusion matrix for band gap data

| Actual Data |  | Predictions |  |  | Prediction |
| --- | --- | --- | --- | --- | --- |
| Class | # of data | VISIBLE | UV_A | UV_BC | Accuracy % |
| VISIBLE | 143 | 127 | 9 | 7 | 88.8% |
| UV_A | 120 | 30 | 69 | 21 | 57.5% |
| UV_BC | 109 | 4 | 23 | 82 | 75.2% |

REFERENCES

[S1]  M. Hahsler, C.Buchta, B.Gruen, K. Hornik, I. Johnson, C. Borgelt, ‘arules’ package of R, https://cran.r-project.org/web/packages/arules/arules.pdf, accessed: May, 2018.

[S2] M. Hahsler, G. Tyler, S. Chelluboina, ‘arulesViz’ package of R, https://cran.r-project.org/web/packages/arulesViz/vignettes/arulesViz.pdf, accessed: May, 2018.

[S3] T. Therneau, B. Atkinson, B. Ripley, ‘rpart’ package of R, https://cran.r-project.org/web/packages/rpart/rpart.pdf, accessed: May, 2018.

[S4] J. H. Epstein, S. Q. Wang, UVA & UVB,   https://www.skincancer.org/prevention/uva-and-uvb, accessed: May, 2018.

[S5] A. Liaw, ‘randomForest’ package of R, https://cran.r-project.org/web/packages/randomForest/randomForest.pdf, accessed: May, 2018.

[S6] B. Lawson, set.seed function of R, https://www.rdocumentation.org/packages/simEd/versions/1.0.3/topics/set.seed, accessed: May, 2018.

[S7] M. Zambrano-Bigiarini, ‘hydroGOF’ package of R, https://cran.r-project.org/web/packages/hydroGOF/hydroGOF.pdf, accessed: May, 2018.

[S8] B. Hamner, M. Frasco, E. LeDell, ‘metrics’ package of R, https://cran.r-project.org/web/packages/Metrics/Metrics.pdf, accessed: May, 2018.

[S9] T. Wei, V. Simko, M. Levy, Y. Xie, Y. Jin, J. Zemla, ‘corrplot’ package of R, https://cran.r-project.org/web/packages/corrplot/corrplot.pdf, accessed: May, 2018.

[S10] G. Williams, M. V. Culp, E. Cox, A. Nolan, D. White, D. Medri, A. Waljee, B. Ripley, J. Magana, S. Tipparaju, D. P. Chappidi, D. M. Venkata, M. Chakraborty, F. Zhou, ‘rattle’ package of R, https://cran.r-project.org/web/packages/rattle/rattle.pdf, accessed: May, 2018.

APPENDIX A. Database

A1. Hydrogen Production Rate Database Constructed from literature

Table A1. Data for hydrogen production rate under both visible and UV light

(If the 31th  column (light type) was Xe, halogen or visible it means that the article stated that they used visible light in their PWS experiments, so those instances were placed into the visible dataset. If the 31th columns were Hg or UV, then the corresponding instances were placed into the UV dataset.)

| Ref | A | A1 | A2 | B | B1 | B2 | X | X1 | A mole | A1 mole | A2 mole | B mole | B1 mole | B2 mole | X mole | X1 mole | Prep Meth | CalcT (K) | Calc time (h) | Prom Meth | Promoter | Prom %w | Crystal | BandGap (eV) | Surface Area (m2/g) | CatW (g/L) | Alcohol% | Sac. Agent1 | Sac. Agent2 | Light Type | Power (W) | Wave length (<nm) | ProdRate (μmol/g) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| [S1] | Sr |  |  | Ti |  |  | O |  | 0.478 |  |  | 0.261 |  |  | 0.262 |  | flux | 1373 | 10 | impreg | Rh | 0.1 | cubic | 3.2 | 0.9 | 1 | 0 |  |  | Xe | 300 | 300 | 540 |
| [S1] | Sr |  |  | Ti |  |  | O |  | 0.478 |  |  | 0.261 |  |  | 0.262 |  | flux | 1273 | 10 | impreg | Rh | 0.1 | cubic | 3.2 | 1.3 | 1 | 0 |  |  | Xe | 300 | 300 | 540 |
| [S1] | Sr |  |  | Ti |  |  | O |  | 0.478 |  |  | 0.261 |  |  | 0.262 |  | flux | 1173 | 10 | impreg | Rh | 0.1 | cubic | 3.2 | 1.9 | 1 | 0 |  |  | Xe | 300 | 300 | 32 |
| [S1] | Sr |  |  | Ti | Al |  | O |  | 0.477 |  |  | 0.261 | 1E-04 |  | 0.262 |  | flux | 1273 | 10 | impreg | Rh | 0.1 | cubic | 3.2 | 0.9 | 1 | 0 |  |  | Xe | 300 | 300 | 40 |
| [S1] | Sr |  |  | Ti | Al |  | O |  | 0.477 |  |  | 0.26 | 0.001 |  | 0.261 |  | flux | 1273 | 10 | impreg | Rh | 0.1 | cubic | 3.2 | 2.7 | 1 | 0 |  |  | Xe | 300 | 300 | 380 |
| [S1] | Sr |  |  | Ti | Al |  | O |  | 0.471 |  |  | 0.257 | 0.014 |  | 0.258 |  | flux | 1273 | 10 | impreg | Rh | 0.1 | cubic | 3.2 | 2.4 | 1 | 0 |  |  | Xe | 300 | 300 | 700 |
| [S2] | Mn |  |  | Co |  |  | O |  | 0.232 |  |  | 0.498 |  |  | 0.27 |  | novel | 743 | 12 |  |  |  | octahedral | 2.1 |  | 4 | 0 |  |  | visible | 64 | 420 | 91.07 |
| [S2] | Mn |  |  | Co |  |  | O |  | 0.232 |  |  | 0.498 |  |  | 0.27 |  | novel | 743 | 12 |  |  |  | octahedral | 2.1 |  | 4 | 5 |  |  | visible | 64 | 420 | 146.2 |
| [S3] | Sr | La |  | Ti | Cr |  | O |  | 0.475 | 0.004 |  | 0.26 | 0.001 |  | 0.26 |  | HT |  |  | PD | Pt | 0.5 | cubic | 2.95 |  | 0.5 | 20 |  |  | Xe | 300 | 420 | 66 |
| [S3] | Sr | La |  | Ti | Cr |  | O |  | 0.473 | 0.007 |  | 0.258 | 0.003 |  | 0.259 |  | HT |  |  | PD | Pt | 0.5 | cubic | 2.9 |  | 0.5 | 20 |  |  | Xe | 300 | 420 | 75 |
| [S3] | Sr | La |  | Ti | Cr |  | O |  | 0.468 | 0.015 |  | 0.256 | 0.006 |  | 0.256 |  | HT |  |  | PD | Pt | 0.5 | cubic | 2.92 |  | 0.5 | 20 |  |  | Xe | 300 | 420 | 76 |
| [S3] | Sr | La |  | Ti | Cr |  | O |  | 0.465 | 0.018 |  | 0.254 | 0.007 |  | 0.255 |  | HT |  |  | PD | Pt | 0.5 | cubic | 2.8 |  | 0.5 | 20 |  |  | Xe | 300 | 420 | 90 |
| [S3] | Sr | La |  | Ti | Cr |  | O |  | 0.463 | 0.022 |  | 0.253 | 0.008 |  | 0.254 |  | HT |  |  | PD | Pt | 0.5 | cubic | 2.85 |  | 0.5 | 20 |  |  | Xe | 300 | 420 | 71 |
| [S3] | Sr | La |  | Ti | Cr |  | O |  | 0.458 | 0.029 |  | 0.25 | 0.011 |  | 0.251 |  | HT |  |  | PD | Pt | 0.5 | cubic | 2.9 |  | 0.5 | 20 |  |  | Xe | 300 | 420 | 39 |
| [S4] | Sr |  |  | Ti | Rh | Sb | O |  | 0.473 |  |  | 0.258 | 0.003 | 0.007 | 0.259 |  | SSR | 1373 | 10 | impreg | IrO2 | 3 | cubic | 2.95 |  | 1.66 | 0 | H2SO4 |  | Xe | 300 | 440 | 22 |
| [S4] | Sr |  |  | Ti | Rh | Sb | O |  | 0.473 |  |  | 0.258 | 0.003 | 0.007 | 0.259 |  | SSR | 1373 | 10 | impreg | RuO2 | 1 | cubic | 2.95 |  | 1.66 | 0 | H2SO4 |  | Xe | 300 | 440 | 0.6 |
| [S4] | Sr |  |  | Ti | Rh | Sb | O |  | 0.473 |  |  | 0.258 | 0.003 | 0.007 | 0.259 |  | SSR | 1373 | 10 | PD | Ru | 0.5 | cubic | 2.95 |  | 1.66 | 0 | H2SO4 |  | Xe | 300 | 440 | 2.5 |
| [S4] | Sr |  |  | Ti | Rh | Sb | O |  | 0.473 |  |  | 0.258 | 0.003 | 0.007 | 0.259 |  | SSR | 1373 | 10 | impreg | IrO2 | 1 | cubic | 2.95 |  | 1.66 | 0 | H2SO4 |  | Xe | 300 | 440 | 18.5 |
| [S4] | Sr |  |  | Ti | Rh | Sb | O |  | 0.473 |  |  | 0.258 | 0.003 | 0.007 | 0.259 |  | SSR | 1373 | 10 | impreg | IrO2 | 3 | cubic | 2.95 |  | 1.66 | 0 | H2SO4 |  | Xe | 300 | 300 | 60 |
| [S4] | Sr |  |  | Ti | Rh | Sb | O |  | 0.473 |  |  | 0.258 | 0.003 | 0.007 | 0.259 |  | SSR | 1373 | 10 | impreg | IrO2 | 3 | cubic | 3.26 |  | 1.66 | 0 | H2SO4 |  | Xe | 300 | 440 | 3.15 |
| [S4] | Sr |  |  | Ti | Rh | Sb | O |  | 0.476 |  |  | 0.26 | 0.003 |  | 0.261 |  | SSR | 1373 | 10 | impreg | IrO2 | 3 | cubic | 3.26 |  | 1.66 | 0 | H2SO4 |  | Xe | 300 | 300 | 3.65 |
| [S5] | Sm |  |  | Ti |  |  | O | S | 0.556 |  |  | 0.177 |  |  | 0.148 | 0.119 | PC | 773 | 12 | PD | Rh | 1.5 | amorphous | 1.9 |  | 0.5 | 0 | Na2S | Na2SO3 | Hg | 450 | 400 | 312.5 |
| [S6] | Zn |  |  | In |  |  | S |  | 0.191 |  |  | 0.504 |  |  | 0.305 |  | HT |  |  | PD | Ru | 0.5 | hexagonal | 2.64 |  | 1 | 0 | Na2S | Na2SO3 | Xe | 300 | 420 | 1850 |
| [S6] | Zn | Ag |  | In |  |  | S |  | 0.191 | 0.002 |  | 0.503 |  |  | 0.305 |  | HT |  |  | PD | Ru | 0.5 | hexagonal | 2.57 |  | 1 | 0 | Na2S | Na2SO3 | Xe | 300 | 420 | 2810 |
| [S6] | Zn | Ag |  | In |  |  | S |  | 0.191 | 0.003 |  | 0.502 |  |  | 0.305 |  | HT |  |  | PD | Ru | 0.5 | hexagonal | 2.48 |  | 1 | 0 | Na2S | Na2SO3 | Xe | 300 | 420 | 2940 |
| [S6] | Zn | Ag |  | In |  |  | S |  | 0.191 | 0.005 |  | 0.501 |  |  | 0.305 |  | HT |  |  | PD | Ru | 0.5 | hexagonal | 2.47 |  | 1 | 0 | Na2S | Na2SO3 | Xe | 300 | 420 | 3200 |
| [S6] | Zn | Ag |  | In |  |  | S |  | 0.19 | 0.006 |  | 0.5 |  |  | 0.304 |  | HT |  |  | PD | Ru | 0.5 | hexagonal | 2.45 |  | 1 | 0 | Na2S | Na2SO3 | Xe | 300 | 420 | 2580 |
| [S6] | Zn | Ag |  | In |  |  | S |  | 0.189 | 0.009 |  | 0.498 |  |  | 0.304 |  | HT |  |  | PD | Ru | 0.5 | hexagonal | 2.41 |  | 1 | 0 | Na2S | Na2SO3 | Xe | 300 | 420 | 1940 |
| [S7] | K | Ca | Sr | Ta |  |  | O |  | 0.03 | 0.031 | 0.067 | 0.69 |  |  | 0.183 |  | SSR | 1173 | 10 |  |  | 0.5 | octahedral | 3.99 |  | 1.42 | 0 |  |  | Hg | 400 | 285 | 542 |
| [S7] | K | Ca | Sr | Ta |  |  | O |  | 0.03 | 0.031 | 0.067 | 0.69 |  |  | 0.183 |  | SSR | 1173 | 10 | impreg | NiO | 0.5 | octahedral | 3.99 |  | 1.42 | 0 |  |  | Hg | 400 | 285 | 1278 |
| [S7] | K | Ca | Sr | Ta |  |  | O |  | 0.03 | 0.031 | 0.067 | 0.69 |  |  | 0.183 |  | SSR | 1423 | 10 |  |  | 0.5 | octahedral | 4.13 |  | 1.42 | 0 |  |  | Hg | 400 | 285 | 204 |
| [S7] | K | Ca | Sr | Ta |  |  | O |  | 0.03 | 0.031 | 0.067 | 0.69 |  |  | 0.183 |  | SSR | 1423 | 10 | impreg | NiO | 0.5 | octahedral | 4.13 |  | 1.42 | 0 |  |  | Hg | 400 | 285 | 2678 |
| [S7] | K | Ca | Sr | Ta |  |  | O |  | 0.03 | 0.031 | 0.067 | 0.69 |  |  | 0.183 |  | SSR | 1423 | 10 | PD | Ni | 0.5 | octahedral | 4.13 |  | 1.42 | 0 |  |  | Hg | 400 | 285 | 50 |
| [S7] | K | Ca | Sr | Ta |  |  | O |  | 0.03 | 0.031 | 0.067 | 0.69 |  |  | 0.183 |  | SSR | 1423 | 10 | impreg | Ni | 0.5 | octahedral | 4.13 |  | 1.42 | 0 |  |  | Hg | 400 | 285 | 230 |
| [S7] | K | Ca | Sr | Ta |  |  | O |  | 0.03 | 0.031 | 0.067 | 0.69 |  |  | 0.183 |  | SSR | 1573 | 10 |  |  | 0.5 | octahedral | 4.27 |  | 1.42 | 0 |  |  | Hg | 400 | 285 | 212 |
| [S7] | K | Ca | Sr | Ta |  |  | O |  | 0.03 | 0.031 | 0.067 | 0.69 |  |  | 0.183 |  | SSR | 1573 | 10 | impreg | NiO | 0.5 | octahedral | 4.27 |  | 1.42 | 0 |  |  | Hg | 400 | 285 | 2540 |
| [S7] | K | Ca | Sr | Ta |  |  | O |  | 0.03 | 0.031 | 0.067 | 0.69 |  |  | 0.183 |  | SSR | 1773 | 10 |  |  | 0.5 | octahedral | 4.06 |  | 1.42 | 0 |  |  | Hg | 400 | 285 | 132 |
| [S7] | K | Ca | Sr | Ta |  |  | O |  | 0.03 | 0.031 | 0.067 | 0.69 |  |  | 0.183 |  | SSR | 1773 | 10 | impreg | NiO | 0.5 | octahedral | 4.06 |  | 1.42 | 0 |  |  | Hg | 400 | 285 | 424 |
| [S7] | K | Ca | Sr | Ta |  |  | O |  | 0.03 | 0.031 | 0.067 | 0.69 |  |  | 0.183 |  | SSR | 1423 | 10 | PD | Cu | 0.5 | octahedral | 4.13 |  | 1.42 | 0 |  |  | Hg | 400 | 285 | 432 |
| [S7] | K | Ca | Sr | Ta |  |  | O |  | 0.03 | 0.031 | 0.067 | 0.69 |  |  | 0.183 |  | SSR | 1423 | 10 | PD | Ru | 0.5 | octahedral | 4.13 |  | 1.42 | 0 |  |  | Hg | 400 | 285 | 56 |
| [S7] | K | Ca | Sr | Ta |  |  | O |  | 0.03 | 0.031 | 0.067 | 0.69 |  |  | 0.183 |  | SSR | 1423 | 10 | PD | Rh | 0.5 | octahedral | 4.13 |  | 1.42 | 0 |  |  | Hg | 400 | 285 | 86 |
| [S7] | K | Ca | Sr | Ta |  |  | O |  | 0.03 | 0.031 | 0.067 | 0.69 |  |  | 0.183 |  | SSR | 1423 | 10 | PD | Ag | 0.5 | octahedral | 4.13 |  | 1.42 | 0 |  |  | Hg | 400 | 285 | 106 |
| [S7] | K | Ca | Sr | Ta |  |  | O |  | 0.03 | 0.031 | 0.067 | 0.69 |  |  | 0.183 |  | SSR | 1423 | 10 | impreg | Ag | 0.5 | octahedral | 4.13 |  | 1.42 | 0 |  |  | Hg | 400 | 285 | 110 |
| [S7] | K | Ca | Sr | Ta |  |  | O |  | 0.03 | 0.031 | 0.067 | 0.69 |  |  | 0.183 |  | SSR | 1423 | 10 | impreg | Ag | 0.5 | octahedral | 4.13 |  | 1.42 | 0 |  |  | Hg | 400 | 285 | 192 |
| [S7] | K | Ca | Sr | Ta |  |  | O |  | 0.03 | 0.031 | 0.067 | 0.69 |  |  | 0.183 |  | SSR | 1423 | 10 | PD | Pt | 0.5 | octahedral | 4.13 |  | 1.42 | 0 |  |  | Hg | 400 | 285 | 124 |
| [S7] | K | Ca | Sr | Ta |  |  | O |  | 0.03 | 0.031 | 0.067 | 0.69 |  |  | 0.183 |  | SSR | 1423 | 10 | PD | Au | 0.5 | octahedral | 4.13 |  | 1.42 | 0 |  |  | Hg | 400 | 285 | 1168 |
| [S8] | Cu |  |  | In |  |  | S |  | 0.262 |  |  | 0.473 |  |  | 0.264 |  | novel |  |  |  |  |  | hexagonal | 1.55 |  | 0.2 | 0 | Na2S | Na2SO3 | Xe | 300 | 350 | 290 |
| [S8] | Cu |  |  | In | Ga |  | S |  | 0.267 |  |  | 0.434 | 0.029 |  | 0.269 |  | novel |  |  |  |  |  | hexagonal | 1.57 |  | 0.2 | 0 | Na2S | Na2SO3 | Xe | 300 | 350 | 368 |
| [S8] | Cu |  |  | In | Ga |  | S |  | 0.278 |  |  | 0.351 | 0.091 |  | 0.28 |  | novel |  |  |  |  |  | hexagonal | 1.6 |  | 0.2 | 0 | Na2S | Na2SO3 | Xe | 300 | 350 | 514 |
| [S8] | Cu |  |  | In | Ga |  | S |  | 0.289 |  |  | 0.261 | 0.158 |  | 0.292 |  | novel |  |  |  |  |  | hexagonal | 1.68 |  | 0.2 | 0 | Na2S | Na2SO3 | Xe | 300 | 350 | 660 |
| [S8] | Cu |  |  | In | Ga |  | S |  | 0.301 |  |  | 0.163 | 0.231 |  | 0.304 |  | novel |  |  |  |  |  | hexagonal | 1.75 |  | 0.2 | 0 | Na2S | Na2SO3 | Xe | 300 | 350 | 747 |
| [S8] | Cu |  |  | In | Ga |  | S |  | 0.315 |  |  | 0.057 | 0.311 |  | 0.318 |  | novel |  |  |  |  |  | hexagonal | 2 |  | 0.2 | 0 | Na2S | Na2SO3 | Xe | 300 | 350 | 582 |
| [S8] | Cu |  |  | In |  |  | S |  | 0.322 |  |  |  | 0.353 |  | 0.325 |  | novel |  |  |  |  |  | hexagonal | 2.35 |  | 0.2 | 0 | Na2S | Na2SO3 | Xe | 300 | 350 | 513 |
| [S9] | K |  |  | Ta |  |  | O |  | 0.146 |  |  | 0.675 |  |  | 0.179 |  | SG | 773 | 6 |  |  |  | cubic | 4.6 | 9.5 | 1 | 0 |  |  | Hg | 400 | 275 | 2800 |
| [S9] | K |  |  | Ta |  |  | O |  | 0.146 |  |  | 0.675 |  |  | 0.179 |  | HT | 773 | 6 |  |  |  | cubic | 4.5 | 4.5 | 1 | 0 |  |  | Hg | 400 | 275 | 650 |
| [S10] | K |  |  | Nb |  |  | O |  | 0.217 |  |  | 0.516 |  |  | 0.267 |  | HT |  |  |  |  |  | orthorombic | 3.15 | 1.42 | 1.25 | 25 |  |  | Xe | 300 | 380 | 33 |
| [S10] | K |  |  | Nb |  |  | O |  | 0.217 |  |  | 0.516 |  |  | 0.267 |  | HT |  |  |  |  |  | tetragonal | 3.08 | 0.68 | 1.25 | 25 |  |  | Xe | 300 | 380 | 118 |
| [S10] | K |  |  | Nb |  |  | O |  | 0.217 |  |  | 0.516 |  |  | 0.267 |  | HT |  |  |  |  |  | cubic | 3.24 | 3.9 | 1.25 | 25 |  |  | Xe | 300 | 380 | 1242 |
| [S10] | K |  |  | Nb |  |  | O |  | 0.217 |  |  | 0.516 |  |  | 0.267 |  | HT |  |  | PD | Pt | 0.5 | orthorombic | 3.15 | 1.42 | 1.25 | 25 |  |  | Xe | 300 | 380 | 170 |
| [S10] | K |  |  | Nb |  |  | O |  | 0.217 |  |  | 0.516 |  |  | 0.267 |  | HT |  |  | PD | Pt | 1 | orthorombic | 3.15 | 1.42 | 1.25 | 25 |  |  | Xe | 300 | 380 | 240 |
| [S10] | K |  |  | Nb |  |  | O |  | 0.217 |  |  | 0.516 |  |  | 0.267 |  | HT |  |  | PD | Pt | 1.5 | orthorombic | 3.15 | 1.42 | 1.25 | 25 |  |  | Xe | 300 | 380 | 300 |
| [S10] | K |  |  | Nb |  |  | O |  | 0.217 |  |  | 0.516 |  |  | 0.267 |  | HT |  |  | PD | Pt | 2 | orthorombic | 3.15 | 1.42 | 1.25 | 25 |  |  | Xe | 300 | 380 | 28 |
| [S11] | Zn |  |  | Cd |  |  | S |  | 0.541 |  |  | 0.151 |  |  | 0.308 |  | novel |  |  |  |  |  | cubic | 2.64 | 124.8 | 0.66 | 0 | Na2S | Na2SO3 | Xe | 300 | 420 | 520 |
| [S11] | Zn |  |  | Cd |  |  | S |  | 0.515 |  |  | 0.181 |  |  | 0.304 |  | novel |  |  |  |  |  | cubic | 2.61 | 131 | 0.66 | 0 | Na2S | Na2SO3 | Xe | 300 | 420 | 610 |
| [S11] | Zn |  |  | Cd |  |  | S |  | 0.49 |  |  | 0.21 |  |  | 0.3 |  | novel |  |  |  |  |  | cubic | 2.58 | 156 | 0.66 | 0 | Na2S | Na2SO3 | Xe | 300 | 420 | 970 |
| [S11] | Zn |  |  | Cd |  |  | S |  | 0.449 |  |  | 0.257 |  |  | 0.294 |  | novel |  |  |  |  |  | cubic | 2.55 | 65.6 | 0.66 | 0 | Na2S | Na2SO3 | Xe | 300 | 420 | 510 |
| [S11] | Zn |  |  | Cd |  |  | S |  | 0.388 |  |  | 0.328 |  |  | 0.284 |  | novel |  |  |  |  |  | cubic | 2.52 | 49.26 | 0.66 | 0 | Na2S | Na2SO3 | Xe | 300 | 420 | 360 |
| [S11] | Zn |  |  | Cd |  |  | S |  | 0.49 |  |  | 0.21 |  |  | 0.3 |  | novel |  |  | PD | Pt | 0.15 | cubic | 2.58 | 156 | 0.66 | 0 | Na2S | Na2SO3 | Xe | 300 | 420 | 1800 |
| [S11] | Zn |  |  | Cd |  |  | S |  | 0.49 |  |  | 0.21 |  |  | 0.3 |  | novel |  |  | PD | Pt | 0.25 | cubic | 2.58 | 156 | 0.66 | 0 | Na2S | Na2SO3 | Xe | 300 | 420 | 2275 |
| [S11] | Zn |  |  | Cd |  |  | S |  | 0.49 |  |  | 0.21 |  |  | 0.3 |  | novel |  |  | PD | Pt | 0.5 | cubic | 2.58 | 156 | 0.66 | 0 | Na2S | Na2SO3 | Xe | 300 | 420 | 1850 |
| [S11] | Zn |  |  | Cd |  |  | S |  | 0.49 |  |  | 0.21 |  |  | 0.3 |  | novel |  |  | PD | Pt | 1 | cubic | 2.58 | 156 | 0.66 | 0 | Na2S | Na2SO3 | Xe | 300 | 420 | 1725 |
| [S12] | Ba |  |  | Zr |  |  | O |  | 0.497 |  |  | 0.33 |  |  | 0.174 |  | PTP | 1273 | 6 |  |  |  | cubic | 4.8 | 8.5 | 0.476 | 0 |  |  | Hg | 400 | 365 | 112 |
| [S12] | Ba |  |  | Zr | Sn |  | O |  | 0.492 |  |  | 0.294 | 0.043 |  | 0.172 |  | PTP | 1273 | 6 |  |  |  | cubic | 4.4 | 5.7 | 0.476 | 0 |  |  | Hg | 400 | 365 | 100 |
| [S12] | Ba |  |  | Zr | Sn |  | O |  | 0.487 |  |  | 0.259 | 0.084 |  | 0.17 |  | PTP | 1273 | 6 |  |  |  | cubic | 4 | 3.8 | 0.476 | 0 |  |  | Hg | 400 | 365 | 125 |
| [S12] | Ba |  |  | Zr | Sn |  | O |  | 0.482 |  |  | 0.224 | 0.125 |  | 0.169 |  | PTP | 1273 | 6 |  |  |  | cubic | 3.6 | 4 | 0.476 | 0 |  |  | Hg | 400 | 365 | 138 |
| [S12] | Ba |  |  | Zr | Sn |  | O |  | 0.478 |  |  | 0.19 | 0.165 |  | 0.167 |  | PTP | 1273 | 6 |  |  |  | cubic | 3.3 | 2.1 | 0.476 | 0 |  |  | Hg | 400 | 365 | 70 |
| [S13] | Zn |  |  | Ti |  |  | S |  | 0.56 |  |  | 0.1 |  |  | 0.34 |  | HT |  |  |  |  |  | cubic | 3.08 |  | 1 | 50 |  |  | UV |  | 365 | 34.2 |
| [S13] | Zn |  |  | Ti |  |  | S |  | 0.58 |  |  | 0.08 |  |  | 0.34 |  | HT |  |  |  |  |  | cubic | 3.06 |  | 1 | 50 |  |  | UV |  | 365 | 113 |
| [S13] | Zn |  |  | Ti |  |  | S |  | 0.62 |  |  | 0.05 |  |  | 0.34 |  | HT |  |  |  |  |  | cubic | 3.05 |  | 1 | 50 |  |  | UV |  | 365 | 396 |
| [S13] | Zn |  |  | Ti |  |  | S |  | 0.61 |  |  | 0.07 |  |  | 0.32 |  | HT |  |  |  |  |  | cubic | 3.11 |  | 1 | 50 |  |  | UV |  | 365 | 275 |
| [S13] | Zn |  |  | Ti |  |  | S |  | 0.62 |  |  | 0.05 |  |  | 0.34 |  | HT |  |  |  |  |  | cubic | 3.05 |  | 1 | 50 | H2SO4 |  | UV |  | 365 | 13.9 |
| [S13] | Zn |  |  | Ti |  |  | S |  | 0.62 |  |  | 0.05 |  |  | 0.34 |  | HT |  |  |  |  |  | cubic | 3.05 |  | 1 | 50 | Na2SO4 |  | UV |  | 365 | 38.6 |
| [S13] | Zn |  |  | Ti |  |  | S |  | 0.62 |  |  | 0.05 |  |  | 0.34 |  | HT |  |  |  |  |  | cubic | 3.05 |  | 1 | 50 | CH3COOH |  | UV |  | 365 | 63.2 |
| [S13] | Zn |  |  | Ti |  |  | S |  | 0.62 |  |  | 0.05 |  |  | 0.34 |  | HT |  |  |  |  |  | cubic | 3.05 |  | 1 | 50 | NaOH |  | UV |  | 365 | 528 |
| [S13] | Zn |  |  | Ti |  |  | S |  | 0.62 |  |  | 0.05 |  |  | 0.34 |  | HT |  |  |  |  |  | cubic | 3.05 |  | 1 | 50 | KOH |  | UV |  | 365 | 794 |
| [S14] | Na | Ca |  | Nb |  |  | O |  | 0.07 | 0.11 |  | 0.53 |  |  | 0.3 |  | flux |  |  | impreg | Pt | 1 | orthorombic | 3.3 | 1.6 | 2 | 20 |  |  | Xe | 1000 | 350 | 74.17 |
| [S14] | Na | Ca |  | Nb |  |  | O |  | 0.07 | 0.11 |  | 0.53 |  |  | 1.3 |  | flux |  |  | impreg | Pt | 1 | orthorombic | 3.3 | 0.36 | 2 | 20 |  |  | Xe | 1000 | 350 | 150 |
| [S14] | Na | Ca |  | Nb |  |  | O |  | 0.07 | 0.11 |  | 0.53 |  |  | 2.3 |  | flux |  |  | impreg | Pt | 1 | orthorombic | 3.3 | 4.6 | 2 | 20 |  |  | Xe | 1000 | 350 | 445.5 |
| [S14] | Na | Ca |  | Nb |  |  | O |  | 0.07 | 0.11 |  | 0.53 |  |  | 3.3 |  | flux |  |  | impreg | Pt | 1 | orthorombic | 3.3 | 3.9 | 2 | 20 |  |  | Xe | 1000 | 350 | 275.5 |
| [S15] | Sb |  |  | Ti |  |  | S |  | 0.62 |  |  | 0.06 |  |  | 0.32 |  | HT |  |  |  |  |  | orthorombic | 1.81 |  | 0.5 | 50 |  |  | UV |  | 365 | 5.3 |
| [S15] | Sb |  |  | Ti |  |  | S |  | 0.54 |  |  | 0.11 |  |  | 0.36 |  | HT |  |  |  |  |  | orthorombic | 1.87 |  | 0.5 | 50 |  |  | UV |  | 365 | 10.2 |
| [S15] | Sb |  |  | Ti |  |  | S |  | 0.48 |  |  | 0.14 |  |  | 0.38 |  | HT |  |  |  |  |  | orthorombic | 2.04 |  | 0.5 | 50 |  |  | UV |  | 365 | 6.9 |
| [S15] | Sb |  |  | Ti |  |  | S |  | 0.54 |  |  | 0.11 |  |  | 0.36 |  | HT |  |  |  |  |  | orthorombic | 1.87 |  | 0.5 | 50 |  |  | UV |  | 365 | 2.9 |
| [S15] | Sb |  |  | Ti |  |  | S |  | 0.54 |  |  | 0.11 |  |  | 0.36 |  | HT |  |  |  |  |  | orthorombic | 1.87 |  | 0.5 | 50 |  |  | UV |  | 365 | 4.5 |
| [S15] | Sb |  |  | Ti |  |  | S |  | 0.54 |  |  | 0.11 |  |  | 0.36 |  | HT |  |  |  |  |  | orthorombic | 1.87 |  | 0.5 | 50 |  |  | UV |  | 365 | 12.1 |
| [S15] | Sb |  |  | Ti |  |  | S |  | 0.54 |  |  | 0.11 |  |  | 0.36 |  | HT |  |  |  |  |  | orthorombic | 1.87 |  | 0.5 | 50 |  |  | UV |  | 365 | 15.3 |
| [S16] | Ca |  |  | In |  |  | S |  | 0.1 |  |  | 0.58 |  |  | 0.32 |  | HT |  |  |  |  |  | cubic | 1.68 | 75.38 | 0.5 | 50 |  |  | Xe | 300 | 420 | 2.625 |
| [S16] | Ca |  |  | In |  |  | S |  | 0.1 |  |  | 0.58 |  |  | 0.32 |  | HT | 773 | 12 |  |  |  | cubic | 1.78 | 6.66 | 0.5 | 50 |  |  | Xe | 300 | 420 | 10.5 |
| [S16] | Ca |  |  | In |  |  | S |  | 0.1 |  |  | 0.58 |  |  | 0.32 |  | HT | 873 | 12 |  |  |  | cubic | 1.8 | 5.11 | 0.5 | 50 |  |  | Xe | 300 | 420 | 17.625 |
| [S16] | Ca |  |  | In |  |  | S |  | 0.1 |  |  | 0.58 |  |  | 0.32 |  | HT | 973 | 12 |  |  |  | cubic | 1.82 | 3.79 | 0.5 | 50 |  |  | Xe | 300 | 420 | 15 |
| [S16] | Ca |  |  | In |  |  | S |  | 0.1 |  |  | 0.58 |  |  | 0.32 |  | HT | 1073 | 12 |  |  |  | cubic | 1.83 | 3.26 | 0.5 | 50 |  |  | Xe | 300 | 420 | 13.75 |
| [S16] | Ca |  |  | In |  |  | S |  | 0.1 |  |  | 0.58 |  |  | 0.32 |  | HT | 1173 | 12 |  |  |  | cubic | 1.84 | 2.74 | 0.5 | 50 |  |  | Xe | 300 | 420 | 4.75 |
| [S16] | Ca |  |  | In |  |  | S |  | 0.1 |  |  | 0.58 |  |  | 0.32 |  | HT | 873 | 1 |  |  |  | cubic | 1.74 | 8.06 | 0.5 | 50 |  |  | Xe | 300 | 420 | 13.5 |
| [S16] | Ca |  |  | In |  |  | S |  | 0.1 |  |  | 0.58 |  |  | 0.32 |  | HT | 873 | 3 |  |  |  | cubic | 1.76 | 6.64 | 0.5 | 50 |  |  | Xe | 300 | 420 | 31.125 |
| [S16] | Ca |  |  | In |  |  | S |  | 0.1 |  |  | 0.58 |  |  | 0.32 |  | HT | 873 | 6 |  |  |  | cubic | 1.78 | 6.17 | 0.5 | 50 |  |  | Xe | 300 | 420 | 25.25 |
| [S16] | Ca |  |  | In |  |  | S |  | 0.1 |  |  | 0.58 |  |  | 0.32 |  | HT | 873 | 9 |  |  |  | cubic | 1.78 | 5.61 | 0.5 | 50 |  |  | Xe | 300 | 420 | 21.875 |
| [S17] | Sb |  |  | Nb |  |  | O |  | 0.44 |  |  | 0.33 |  |  | 0.23 |  | HT | 1173 | 2 |  |  |  | orthorombic | 3.12 | 1.7 | 0.833 | 0 |  |  | Hg | 450 | 365 | 4.5 |
| [S17] | Sb |  |  | Nb |  |  | O |  | 0.44 |  |  | 0.33 |  |  | 0.23 |  | SSR | 1173 | 2 |  |  |  | orthorombic | 3.12 | 1.7 | 0.833 | 0 |  |  | Hg | 450 | 365 | 5 |
| [S17] | Sb |  |  | Ta |  |  | O |  | 0.43 |  |  | 0.49 |  |  | 0.18 |  | SSR | 1173 | 2 |  |  |  | orthorombic | 3.72 | 1.5 | 0.833 | 0 |  |  | Hg | 450 | 365 | 10 |
| [S17] | Sb |  |  | Ta |  |  | O |  | 0.43 |  |  | 0.49 |  |  | 0.18 |  | SSR | 1173 | 2 |  |  |  | orthorombic | 3.72 | 1.5 | 0.833 | 0 |  |  | Hg | 450 | 365 | 9.5 |
| [S17] | Sb |  |  | Nb |  |  | O |  | 0.44 |  |  | 0.33 |  |  | 0.23 |  | SSR | 1173 | 2 | impreg | RuO2 | 1 | orthorombic | 3.12 | 1.7 | 0.833 | 0 |  |  | Hg | 450 | 365 | 61.5 |
| [S17] | Sb |  |  | Ta |  |  | O |  | 0.43 |  |  | 0.49 |  |  | 0.18 |  | SSR | 1173 | 2 | impreg | RuO2 | 1 | orthorombic | 3.72 | 1.5 | 0.833 | 0 |  |  | Hg | 450 | 365 | 146 |
| [S18] | K | La |  | Ta | Bi |  | O |  | 0.02 | 0.07 |  | 0.36 | 0.41 |  | 0.14 |  | SSR | 1173 | 6 |  |  |  | orthorombic | 3.44 | 1.3 | 3.07 | 0 |  |  | Hg | 300 | 365 | 2635 |
| [S19] | Bi | Na |  | Ti |  |  | O |  | 0.49 | 0.05 |  | 0.23 |  |  | 0.23 |  | SSR |  |  | PD | Pt | 0.5 | octahedral | 2.92 | 27.3 | 0.625 | 20 |  |  | Xe | 500 | 346 | 86.4 |
| [S19] | Bi | Na |  | Ti |  |  | O |  | 0.49 | 0.05 |  | 0.23 |  |  | 0.23 |  | SSR |  |  | PD | Pt | 1 | octahedral | 2.92 | 27.3 | 0.625 | 20 |  |  | Xe | 500 | 346 | 196.4 |
| [S19] | Bi | Na |  | Ti |  |  | O |  | 0.49 | 0.05 |  | 0.23 |  |  | 0.23 |  | PC |  |  | PD | Pt | 3 | octahedral | 2.92 | 27.3 | 0.625 | 20 |  |  | Xe | 500 | 346 | 356 |
| [S19] | Bi | Na |  | Ti |  |  | O |  | 0.49 | 0.05 |  | 0.23 |  |  | 0.23 |  | HT |  |  | PD | Pt | 5 | octahedral | 2.92 | 27.3 | 0.625 | 20 |  |  | Xe | 500 | 346 | 266 |
| [S19] | Bi | Na |  | Ti |  |  | O |  | 0.49 | 0.05 |  | 0.23 |  |  | 0.23 |  | HT |  |  | PD | Pt | 8 | octahedral | 2.92 | 27.3 | 0.625 | 20 |  |  | Xe | 500 | 346 | 226 |
| [S20] | Na |  |  | Ta |  |  | O |  | 0.09 |  |  | 0.72 |  |  | 0.19 |  | HT | 1173 | 10 |  |  |  | cubic | 2.64 | 1.22 | 0.5 | 20 |  |  | Xe | 800 | 390 | 0.08 |
| [S20] | Na |  |  | Ta |  |  | O |  | 0.09 |  |  | 0.72 |  |  | 0.19 |  | HT | 1173 | 10 | impreg | Pt | 0.03 | cubic | 2.64 | 1.22 | 0.5 | 20 |  |  | Xe | 800 | 390 | 0.58 |
| [S20] | Na |  |  | Ta |  |  | O |  | 0.09 |  |  | 0.72 |  |  | 0.19 |  | HT | 1173 | 10 | impreg | Pt | 0.06 | cubic | 2.64 | 1.22 | 0.5 | 20 |  |  | Xe | 800 | 390 | 1 |
| [S20] | Na |  |  | Ta |  |  | O |  | 0.09 |  |  | 0.72 |  |  | 0.19 |  | SSR | 1173 | 10 | impreg | Pt | 0.1 | cubic | 2.64 | 1.22 | 0.5 | 20 |  |  | Xe | 800 | 390 | 0.25 |
| [S20] | Na |  |  | Ta |  |  | O |  | 0.09 |  |  | 0.72 |  |  | 0.19 |  | SSR | 1173 | 10 | impreg | Pt | 0.13 | cubic | 2.64 | 1.22 | 0.5 | 20 |  |  | Xe | 800 | 390 | 0.16 |
| [S20] | Na |  |  | Ta |  |  | O |  | 0.09 |  |  | 0.72 |  |  | 0.19 |  | SSR | 1173 | 10 | impreg | Pt | 0.06 | cubic | 4.01 | 1.13 | 0.5 | 20 |  |  | Xe | 800 | 390 | 0.08 |
| [S21] | Sr |  |  | Sn |  |  | O |  | 0.35 |  |  | 0.47 |  |  | 0.19 |  | SSR | 1373 | 6 |  |  |  |  | 4.01 | 3.28 | 1 | 0 |  |  | Hg | 450 | 365 | 11 |
| [S21] | Sr |  |  | Sn |  |  | O |  | 0.35 |  |  | 0.47 |  |  | 0.19 |  | SSR | 1373 | 6 | impreg | NiO | 1 |  | 4.01 | 3.28 | 1 | 0 |  |  | Hg | 450 | 365 | 24.2 |
| [S21] | Sr |  |  | Sn |  |  | O |  | 0.35 |  |  | 0.47 |  |  | 0.19 |  | SSR | 973 | 6 |  |  |  | orthorombic | 4.04 | 27.08 | 1 | 0 |  |  | Hg | 450 | 365 | 59.8 |
| [S21] | Sr |  |  | Sn |  |  | O |  | 0.35 |  |  | 0.47 |  |  | 0.19 |  | SSR | 973 | 6 | impreg | NiO | 1 | orthorombic | 4.04 | 27.08 | 1 | 0 |  |  | Hg | 450 | 365 | 236 |
| [S22] | Li |  |  | Ta |  |  | O |  | 0.03 |  |  | 0.77 |  |  | 0.2 |  | SSR |  |  |  |  |  | rhombohedral | 3.93 | 1.34 | 0.25 | 0 | HCOOH |  | Hg | 150 | 366 | 354.5 |
| [S22] | Li |  |  | Ta |  |  | O |  | 0.03 |  |  | 0.77 |  |  | 0.2 |  | novel | 723 | 11 |  |  |  | rhombohedral | 3.3 | 4.08 | 0.25 | 0 | HCOOH |  | Hg | 150 | 366 | 308 |
| [S22] | Li |  |  | Ta |  |  | O |  | 0.03 |  |  | 0.77 |  |  | 0.2 |  | novel | 773 | 11 |  |  |  | rhombohedral | 3.77 | 3.66 | 0.25 | 0 | HCOOH |  | Hg | 150 | 366 | 525 |
| [S22] | Li |  |  | Ta |  |  | O |  | 0.03 |  |  | 0.77 |  |  | 0.2 |  | novel | 823 | 11 |  |  |  | rhombohedral | 3.69 | 3.08 | 0.25 | 0 | HCOOH |  | Hg | 150 | 366 | 765 |
| [S22] | Li |  |  | Ta |  |  | O |  | 0.03 |  |  | 0.77 |  |  | 0.2 |  | novel | 873 | 11 |  |  |  | rhombohedral | 3.74 | 3.01 | 0.25 | 0 | HCOOH |  | Hg | 150 | 366 | 545 |
| [S22] | Li |  |  | Ta |  |  | O |  | 0.03 |  |  | 0.77 |  |  | 0.2 |  | novel | 923 | 11 |  |  |  | rhombohedral | 4.9 | 2.86 | 0.25 | 0 | HCOOH |  | Hg | 150 | 366 | 450 |
| [S22] | Li |  |  | Ta |  |  | O |  | 0.03 |  |  | 0.77 |  |  | 0.2 |  | novel | 973 | 11 |  |  |  | rhombohedral | 4.93 | 2.49 | 0.25 | 0 | HCOOH |  | Hg | 150 | 366 | 429 |
| [S22] | Li |  |  | Ta |  |  | O |  | 0.03 |  |  | 0.77 |  |  | 0.2 |  | novel | 1023 | 11 |  |  |  | rhombohedral | 4.95 | 2.38 | 0.25 | 0 | HCOOH |  | Hg | 150 | 366 | 437 |
| [S22] | Li |  |  | Ta |  |  | O |  | 0.03 |  |  | 0.77 |  |  | 0.2 |  | novel | 1073 | 11 |  |  |  | rhombohedral | 4.98 | 1.96 | 0.25 | 0 | HCOOH |  | Hg | 150 | 366 | 336 |
| [S23] | Ca |  |  | Ta | Zr |  | O | N | 0.22 |  |  |  | 0.51 |  | 0.27 |  | novel | 923 | 6 | PD | Pt | 1 |  | 4 | 21.87 | 0.555 | 0 | HCOOH |  | Xe | 300 | 420 | 9.8 |
| [S23] | Ca |  |  | Ta | Zr |  | O | N | 0.2 |  |  | 0.18 | 0.37 |  | 0.23 | 0.01 | novel | 923 | 6 | PD | Pt | 1 |  | 3.22 | 15.74 | 0.555 | 0 | HCOOH |  | Xe | 300 | 420 | 10.4 |
| [S23] | Ca |  |  | Ta | Zr |  | O | N | 0.19 |  |  | 0.18 | 0.37 |  | 0.23 | 0.01 | novel | 923 | 6 | PD | Pt | 1 |  | 2.84 | 6.48 | 0.555 | 0 | HCOOH |  | Xe | 300 | 420 | 14.8 |
| [S23] | Ca |  |  | Ta | Zr |  | O | N | 0.17 |  |  | 0.47 | 0.16 |  | 0.17 | 0.04 | PC | 923 | 6 | PD | Pt | 1 |  | 2.69 | 7.65 | 0.555 | 0 | HCOOH |  | Xe | 300 | 420 | 16.8 |
| [S23] | Ca |  |  | Ta | Zr |  | O | N | 0.16 |  |  | 0.58 | 0.07 |  | 0.14 | 0.05 | PC | 923 | 6 | PD | Pt | 1 |  | 2.63 | 7.28 | 0.555 | 0 | HCOOH |  | Xe | 300 | 420 | 25.8 |
| [S23] | Ca |  |  | Ta | Zr |  | O | N | 0.15 |  |  | 0.68 |  |  | 0.12 | 0.05 | PC | 923 | 6 | PD | Pt | 1 |  | 2.57 | 6.96 | 0.555 | 0 | HCOOH |  | Xe | 300 | 420 | 18 |
| [S24] | Bi |  |  | Ti |  |  | O | N | 0.77 |  |  | 0.09 |  |  | 0.12 | 0.03 | PC | 973 | 2 | impreg | Pt | 1 | octahedral | 2.2 | 92.97 | 1 | 10 | NaNO2 |  | Hg | 125 | 400 | 1018 |
| [S25] | K |  |  | Nb |  |  | O |  | 0.16 |  |  | 0.57 |  |  | 0.28 |  | PC |  |  |  |  |  |  | 3.89 | 86.6 | 0.27 | 13.5 |  |  | Hg | 350 | 365 | 30266 |
| [S26] | Sr | H |  | Ta | Nb |  | O |  | 0.29 |  |  |  | 0.45 |  | 0.26 |  | PC |  |  |  |  |  | octahedral | 3.5 | 12.12 | 2 | 10 | NaNO2 |  | Hg | 100 | 400 | 1021 |
| [S26] | Sr | H |  | Ta | Nb |  | O |  | 0.25 |  |  | 0.26 | 0.26 |  | 0.23 |  | co-pre |  |  |  |  |  | octahedral | 3.77 | 10.54 | 2 | 10 | NaNO2 |  | Hg | 100 | 400 | 321.67 |
| [S26] | Sr | H |  | Ta | Nb |  | O |  | 0.24 |  |  | 0.36 | 0.19 |  | 0.21 |  | novel |  |  |  |  |  | octahedral | 3.8 | 11.82 | 2 | 10 | NaNO2 |  | Hg | 100 | 400 | 895 |
| [S26] | Sr | H |  | Ta | Nb |  | O |  | 0.22 |  |  | 0.46 | 0.12 |  | 0.2 |  | SSR |  |  |  |  |  | octahedral | 3.92 | 11.08 | 2 | 10 | NaNO2 |  | Hg | 100 | 400 | 888.33 |
| [S26] | Sr | H |  | Ta | Nb |  | O |  | 0.2 |  |  | 0.62 |  |  | 0.18 |  | SSR |  |  |  |  |  | octahedral | 4.25 | 12.1 | 2 | 10 | NaNO2 |  | Hg | 100 | 400 | 358.33 |
| [S26] | Sr | H |  | Ta | Nb |  | O |  | 0.29 |  |  |  | 0.45 |  | 0.26 |  | SSR |  |  |  |  |  | octahedral | 4.25 | 12.1 | 2 | 10 | NaNO2 |  | Hg | 100 | 400 | 6733.33 |
| [S26] | Sr | H |  | Ta | Nb |  | O |  | 0.25 |  |  | 0.26 | 0.26 |  | 0.23 |  | SSR |  |  |  |  |  | octahedral | 4.25 | 12.1 | 2 | 10 | NaNO2 |  | Hg | 100 | 400 | 8550 |
| [S26] | Sr | H |  | Ta | Nb |  | O |  | 0.24 |  |  | 0.36 | 0.19 |  | 0.21 |  | SSR |  |  |  |  |  | octahedral | 3.74 | 10.97 | 2 | 10 | NaNO2 |  | Hg | 100 | 400 | 2583.33 |
| [S26] | Sr | H |  | Ta | Nb |  | O |  | 0.22 |  |  | 0.46 | 0.12 |  | 0.2 |  | SSR |  |  |  |  |  | octahedral | 3.78 | 11.41 | 2 | 10 | NaNO2 |  | Hg | 100 | 400 | 1195 |
| [S26] | Sr | H |  | Ta | Nb |  | O |  | 0.2 |  |  | 0.62 |  |  | 0.18 |  | SSR |  |  |  |  |  | octahedral | 3.99 | 11.97 | 2 | 10 | NaNO2 |  | Hg | 100 | 400 | 250 |
| [S27] | K | Sn |  | Ti |  |  | O |  | 0.08 | 0.45 |  | 0.27 |  |  | 0.2 |  | SSR |  |  | PD | Pt | 0.5 | monoclinic | 2.8 |  | 0.37 | 18.5 |  |  | Xe | 300 | 420 | 257 |
| [S28] | Zn |  |  | In |  |  | S |  | 0.15 |  |  | 0.54 |  |  | 0.3 |  | SSR | 333 | 6 |  |  |  | cubic | 3.26 |  | 1.2 | 0 | Na2S | Na2SO3 | Xe | 350 | 250 | 319 |
| [S28] | Zn |  |  | In |  |  | S |  | 0.15 |  |  | 0.54 |  |  | 0.3 |  | SSR | 333 | 6 |  |  |  | cubic | 2.43 |  | 4.08 | 0 | Na2S | Na2SO3 | Xe | 350 | 250 | 284 |
| [S29] | La |  |  | Nb | Ta |  | O |  | 0.32 |  |  | 0.42 |  |  | 0.26 |  | HT |  |  | PD | Pt | 1.42 | tetragonal | 3.42 | 10.84 | 2 | 10 |  |  | Hg | 100 | 290 | 748 |
| [S29] | La |  |  | Nb | Ta |  | O |  | 0.28 |  |  | 0.25 | 0.24 |  | 0.23 |  | electrospinning |  |  | PD | Pt | 1.03 | tetragonal | 3.6 | 11.4 | 2 | 10 |  |  | Hg | 100 | 290 | 3066.6 |
| [S29] | La |  |  | Nb | Ta |  | O |  | 0.26 |  |  | 0.18 | 0.34 |  | 0.21 |  | electrospinning |  |  | PD | Pt | 1.12 | tetragonal | 3.72 | 11.13 | 2 | 10 |  |  | Hg | 100 | 290 | 1121.6 |
| [S29] | La |  |  | Nb | Ta |  | O |  | 0.25 |  |  | 0.11 | 0.43 |  | 0.2 |  | ionexchange |  |  | PD | Pt | 1.18 | tetragonal | 3.81 | 11.28 | 2 | 10 |  |  | Hg | 100 | 290 | 911.6 |
| [S29] | La |  |  | Nb | Ta |  | O |  | 0.23 |  |  |  | 0.59 |  | 0.18 |  | ionexchange |  |  | PD | Pt | 1.35 | tetragonal | 3.92 | 12.01 | 2 | 10 |  |  | Hg | 100 | 290 | 386.7 |
| [S30] | La |  |  | Ni | Cu |  | O |  | 0.56 |  |  | 0.12 | 0.13 |  | 0.19 |  | ionexchange | 1073 | 5 |  |  |  | rhombohedral | 2.47 |  | 0.5 | 0 | CH2O |  | Xe | 125 | 400 | 520 |
| [S31] | Bi | Sr |  | Nb |  |  | O |  | 0.5 | 0.11 |  | 0.22 |  |  | 0.17 |  | ionexchange | 1473 | 24 |  |  |  | orthorombic | 2.35 |  | 0.5 | 12.5 |  |  | Hg | 350 | 365 | 3636 |
| [S31] | Bi | Ba |  | Nb |  |  | O |  | 0.47 | 0.16 |  | 0.21 |  |  | 0.16 |  | ionexchange | 1473 | 72 |  |  |  | tetragonal | 1.27 |  | 0.5 | 12.5 |  |  | Hg | 350 | 365 | 1154 |
| [S31] | Bi | Ca |  | Nb |  |  | O |  | 0.53 | 0.05 |  | 0.24 |  |  | 0.18 |  | novel | 1473 | 24 |  |  |  | orthorombic | 2.65 |  | 0.5 | 12.5 |  |  | Hg | 350 | 365 | 531 |
| [S32] | Na |  |  | Ta |  |  | O |  | 0.09 |  |  | 0.72 |  |  | 0.19 |  | SSR | 873 | 6 |  |  |  |  | 3.96 | 14 |  | 0 |  |  | Hg | 400 | 200 | 113.67 |
| [S32] | Na | K |  | Ta |  |  | O |  | 0.06 | 0.36 |  | 0.46 |  |  | 0.12 |  | SSR | 873 | 6 |  |  |  |  | 4 | 14 |  | 0 |  |  | Hg | 400 | 200 | 172.33 |
| [S32] | Na | K |  | Ta |  |  | O |  | 0.06 | 0.36 |  | 0.46 |  |  | 0.12 |  | SSR | 873 | 6 | impreg | RuO2 | 0.6 |  | 4 | 14 |  | 0 |  |  | Hg | 400 | 200 | 3326 |
| [S32] | Na | K |  | Ta |  |  | O |  | 0.06 | 0.36 |  | 0.46 |  |  | 0.12 |  | SG | 873 | 6 | impreg | RuO2 | 1 |  | 4 | 13 |  | 0 |  |  | Hg | 400 | 200 | 3800 |
| [S32] | Na | K |  | Ta |  |  | O |  | 0.06 | 0.36 |  | 0.46 |  |  | 0.12 |  | SG | 873 | 6 | impreg | RuO2 | 0.2 |  | 4 | 14 |  | 0 |  |  | Hg | 400 | 200 | 706.67 |
| [S32] | Na | K |  | Ta |  |  | O |  | 0.06 | 0.36 |  | 0.46 |  |  | 0.12 |  | SG | 873 | 6 | impreg | RuO2 | 2 |  | 4 | 13 |  | 0 |  |  | Hg | 400 | 200 | 1953 |
| [S33] | K |  |  | Ti |  |  | O |  | 0.14 |  |  | 0.5 |  |  | 0.36 |  | SG | 1373 | 10 | PD | Rh | 0.005 | hexagonal | 3.52 | 2 | 0.4 | 0 |  |  | Xe | 300 | 254 | 16.2 |
| [S33] | K |  |  | Ti |  |  | O |  | 0.14 |  |  | 0.5 |  |  | 0.36 |  | SG | 1373 | 10 | PD | Rh | 0.005 | hexagonal | 3.53 | 1.2 | 0.4 | 0 |  |  | Xe | 300 | 254 | 17.6 |
| [S33] | K |  |  | Ti |  |  | O |  | 0.14 |  |  | 0.5 |  |  | 0.36 |  | SG | 1373 | 10 | PD | Rh | 0.005 | hexagonal | 3.54 | 2.1 | 0.4 | 0 |  |  | Xe | 300 | 254 | 14 |
| [S33] | K |  |  | Ti |  |  | O |  | 0.14 |  |  | 0.5 |  |  | 0.36 |  | flux | 1373 | 10 | PD | Rh | 0.003 | hexagonal | 3.6 | 2.9 | 0.4 | 0 |  |  | Xe | 300 | 254 | 8 |
| [S33] | K |  |  | Ti |  |  | O |  | 0.14 |  |  | 0.5 |  |  | 0.36 |  | flux | 1373 | 10 | PD | Rh | 0.003 | hexagonal | 3.6 | 2.2 | 0.4 | 0 |  |  | Xe | 300 | 254 | 7.6 |
| [S33] | K |  |  | Ti |  |  | O |  | 0.14 |  |  | 0.5 |  |  | 0.36 |  | flux | 1373 | 10 | PD | Rh | 0.003 | hexagonal | 3.6 | 2.6 | 0.4 | 0 |  |  | Xe | 300 | 254 | 2.6 |
| [S34] | In | Ni |  | Ta |  |  | O | N | 0.15 | 0.02 |  | 0.17 |  |  | 0.54 | 0.13 | flux | 1423 | 48 |  |  |  | monoclinic | 2.38 |  | 2 | 0 |  |  | Xe | 300 | 400 | 8.4 |
| [S35] | Na |  |  | Ta |  |  | O |  | 0.09 |  |  | 0.72 |  |  | 0.19 |  | flux | 623 | 1 | impreg | NiO | 0.1 | orthorombic | 4.08 | 1.13 | 0.625 | 0 |  |  | Hg | 8 | 254 | 86 |
| [S35] | Na |  |  | Ta |  |  | O |  | 0.09 |  |  | 0.72 |  |  | 0.19 |  | flux | 623 | 1 | impreg | NiO | 0.2 | orthorombic | 4.08 | 1.13 | 0.625 | 0 |  |  | Hg | 8 | 254 | 149 |
| [S35] | Na |  |  | Ta |  |  | O |  | 0.09 |  |  | 0.72 |  |  | 0.19 |  | SSR | 623 | 1 | impreg | NiO | 0.3 | orthorombic | 4.08 | 1.13 | 0.625 | 0 |  |  | Hg | 8 | 254 | 275 |
| [S35] | Na |  |  | Ta |  |  | O |  | 0.09 |  |  | 0.72 |  |  | 0.19 |  | HT | 623 | 1 | impreg | NiO | 0.4 | orthorombic | 4.08 | 1.13 | 0.625 | 0 |  |  | Hg | 8 | 254 | 168 |
| [S36] | Bi | K | La | Ta |  |  | O |  | 0.41 | 0.02 | 0.07 | 0.36 |  |  | 0.14 |  | HT | 1173 | 6 | PD | Pt | 0.006 | tetragonal | 4 | 3.84 | 1.54 | 0 |  |  | Hg | 250 | 365 | 221 |
| [S36] | Bi | K | La | Ta |  |  | O |  | 0.41 | 0.02 | 0.07 | 0.36 |  |  | 0.14 |  | HT | 1173 | 6 | PD | Pt | 0.124 | tetragonal | 4 | 3.84 | 1.54 | 0 |  |  | Hg | 250 | 365 | 266 |
| [S36] | Bi | K | La | Ta |  |  | O |  | 0.41 | 0.02 | 0.07 | 0.36 |  |  | 0.14 |  | HT | 1173 | 6 | PD | Pt | 0.251 | tetragonal | 4 | 3.84 | 1.54 | 0 |  |  | Hg | 250 | 365 | 288 |
| [S36] | Bi | K | La | Ta |  |  | O |  | 0.41 | 0.02 | 0.07 | 0.36 |  |  | 0.14 |  | PC | 1173 | 6 | PD | Pt | 0.373 | tetragonal | 4 | 3.84 | 1.54 | 0 |  |  | Hg | 250 | 365 | 404 |
| [S36] | Bi | K | La | Ta |  |  | O |  | 0.41 | 0.02 | 0.07 | 0.36 |  |  | 0.14 |  | PC | 1173 | 6 | PD | Pt | 0.501 | tetragonal | 4 | 3.84 | 1.54 | 0 |  |  | Hg | 250 | 365 | 386 |
| [S36] | Bi |  |  | Ta |  |  | O |  | 0.41 |  |  | 0.36 |  |  | 0.14 |  | PC | 1173 | 6 | PD | Pt | 0.008 | tetragonal | 3.9 | 6.88 | 1.54 | 0 |  |  | Hg | 250 | 365 | 159 |
| [S36] | Bi |  |  | Ta |  |  | O |  | 0.41 |  |  | 0.36 |  |  | 0.14 |  | PC | 1173 | 6 | PD | Pt | 0.123 | tetragonal | 3.9 | 6.88 | 1.54 | 0 |  |  | Hg | 250 | 365 | 405 |
| [S36] | Bi |  |  | Ta |  |  | O |  | 0.41 |  |  | 0.36 |  |  | 0.14 |  | PC | 1173 | 6 | PD | Pt | 0.251 | tetragonal | 3.9 | 6.88 | 1.54 | 0 |  |  | Hg | 250 | 365 | 491 |
| [S36] | Bi |  |  | Ta |  |  | O |  | 0.41 |  |  | 0.36 |  |  | 0.14 |  | PC | 1173 | 6 | PD | Pt | 0.376 | tetragonal | 3.9 | 6.88 | 1.54 | 0 |  |  | Hg | 250 | 365 | 448 |
| [S36] | Bi |  |  | Ta |  |  | O |  | 0.41 |  |  | 0.36 |  |  | 0.14 |  | PC | 1173 | 6 | PD | Pt | 0.501 | tetragonal | 3.9 | 6.88 | 1.54 | 0 |  |  | Hg | 250 | 365 | 354 |
| [S36] | Bi | Ca |  | Ta |  |  | O |  | 0.43 | 0.04 |  | 0.38 |  |  | 0.15 |  | PC | 1173 | 6 | PD | Pt | 0.0043 | tetragonal | 3.7 | 4.35 | 1.54 | 0 |  |  | Hg | 250 | 365 | 112 |
| [S36] | Bi | Ca |  | Ta |  |  | O |  | 0.43 | 0.04 |  | 0.38 |  |  | 0.15 |  | PC | 1173 | 6 | PD | Pt | 0.128 | tetragonal | 3.7 | 4.35 | 1.54 | 0 |  |  | Hg | 250 | 365 | 179 |
| [S36] | Bi | Ca |  | Ta |  |  | O |  | 0.43 | 0.04 |  | 0.38 |  |  | 0.15 |  | PC | 1173 | 6 | PD | Pt | 0.249 | tetragonal | 3.7 | 4.35 | 1.54 | 0 |  |  | Hg | 250 | 365 | 296 |
| [S36] | Bi | Ca |  | Ta |  |  | O |  | 0.43 | 0.04 |  | 0.38 |  |  | 0.15 |  | PC | 1173 | 6 | PD | Pt | 0.376 | tetragonal | 3.7 | 4.35 | 1.54 | 0 |  |  | Hg | 250 | 365 | 241 |
| [S36] | Bi | Ca |  | Ta |  |  | O |  | 0.43 | 0.04 |  | 0.38 |  |  | 0.15 |  | PC | 1173 | 6 | PD | Pt | 0.501 | tetragonal | 3.7 | 4.35 | 1.54 | 0 |  |  | Hg | 250 | 365 | 156 |
| [S36] | Bi | Ba |  | Ta |  |  | O |  | 0.39 | 0.13 |  | 0.34 |  |  | 0.14 |  | PC | 1173 | 6 | PD | Pt | 0.002 | tetragonal | 4.3 | 3.52 | 1.54 | 0 |  |  | Hg | 250 | 365 | 123 |
| [S36] | Bi | Ba |  | Ta |  |  | O |  | 0.39 | 0.13 |  | 0.34 |  |  | 0.14 |  | PC | 1173 | 6 | PD | Pt | 0.125 | tetragonal | 4.3 | 3.52 | 1.54 | 0 |  |  | Hg | 250 | 365 | 136 |
| [S36] | Bi | Ba |  | Ta |  |  | O |  | 0.39 | 0.13 |  | 0.34 |  |  | 0.14 |  | PC | 1173 | 6 | PD | Pt | 0.252 | tetragonal | 4.3 | 3.52 | 1.54 | 0 |  |  | Hg | 250 | 365 | 232 |
| [S36] | Bi | Ba |  | Ta |  |  | O |  | 0.39 | 0.13 |  | 0.34 |  |  | 0.14 |  | PC | 1173 | 6 | PD | Pt | 0.379 | tetragonal | 4.3 | 3.52 | 1.54 | 0 |  |  | Hg | 250 | 365 | 142 |
| [S36] | Bi | Ba |  | Ta |  |  | O |  | 0.39 | 0.13 |  | 0.34 |  |  | 0.14 |  | PC | 1173 | 6 | PD | Pt | 0.5 | tetragonal | 4.3 | 3.52 | 1.54 | 0 |  |  | Hg | 250 | 365 | 77 |
| [S37] | Na | Y |  | Ta |  |  | O |  | 0.07 | 0.26 |  | 0.53 |  |  | 0.14 |  | PC | 1173 | 12 |  |  |  | orthorombic | 4.08 | 4.4 | 0.2 | 10 |  |  | Hg | 150 | 365 | 238.3 |
| [S37] | Na | La |  | Ta |  |  | O |  | 0.06 | 0.36 |  | 0.46 |  |  | 0.12 |  | PC | 1173 | 12 |  |  |  | orthorombic | 4.07 | 2.4 | 0.2 | 10 |  |  | Hg | 150 | 365 | 161.5 |
| [S37] | Na | Yb |  | Ta |  |  | O |  | 0.05 | 0.46 |  | 0.43 |  |  | 0.11 |  | PC | 1173 | 12 |  |  |  | orthorombic | 4.09 | 2.4 | 0.2 | 10 |  |  | Hg | 150 | 365 | 166.5 |
| [S37] | Na |  |  | Ta |  |  | O |  | 0.09 |  |  | 0.72 |  |  | 0.19 |  | SSR | 1173 | 12 |  |  |  | orthorombic | 4.05 | 1.9 | 0.2 | 10 |  |  | Hg | 150 | 365 | 59.67 |
| [S37] | Na | Ce |  | Ta |  |  | O |  | 0.09 | 0.36 |  | 0.72 |  |  | 0.19 |  | SSR | 1173 | 12 |  |  |  | orthorombic | 4.04 | 4.7 | 0.2 | 10 |  |  | Hg | 150 | 365 | 25.83 |
| [S37] | Na | Y |  | Ta |  |  | O |  | 0.07 | 0.26 |  | 0.53 |  |  | 0.14 |  | SSR | 1173 | 12 | PD | Pt | 0.5 | orthorombic | 4.08 | 4.4 | 0.2 | 10 |  |  | Hg | 150 | 365 | 286.67 |
| [S37] | Na | La |  | Ta |  |  | O |  | 0.06 | 0.36 |  | 0.46 |  |  | 0.12 |  | SSR | 1173 | 12 | PD | Pt | 0.4 | orthorombic | 4.07 | 2.4 | 0.2 | 10 |  |  | Hg | 150 | 365 | 115.67 |
| [S37] | Na | Yb |  | Ta |  |  | O |  | 0.05 | 0.46 |  | 0.43 |  |  | 0.11 |  | SSR | 1173 | 12 | PD | Pt | 0.5 | orthorombic | 4.09 | 2.4 | 0.2 | 10 |  |  | Hg | 150 | 365 | 256.67 |
| [S37] | Na |  |  | Ta |  |  | O |  | 0.09 |  |  | 0.72 |  |  | 0.19 |  | SSR | 1173 | 12 | PD | Pt | 0.5 | orthorombic | 4.05 | 1.9 | 0.2 | 10 |  |  | Hg | 150 | 365 | 78.67 |
| [S37] | Na | Ce |  | Ta |  |  | O |  | 0.09 | 0.36 |  | 0.72 |  |  | 0.19 |  | SSR | 1173 | 12 | PD | Pt | 0.3 | orthorombic | 4.04 | 4.7 | 0.2 | 10 |  |  | Hg | 150 | 365 | 24.83 |
| [S38] | Na |  |  | Ta |  |  | O |  | 0.09 |  |  | 0.72 |  |  | 0.19 |  | SSR | 673 | 2 |  |  |  | monoclinic | 3.94 | 118 | 1 | 0 |  |  | Hg | 400 | 200 | 680.67 |
| [S38] | Na |  |  | Ta |  |  | O |  | 0.09 |  |  | 0.72 |  |  | 0.19 |  | SSR | 773 | 2 |  |  |  | monoclinic | 3.98 | 75 | 1 | 0 |  |  | Hg | 400 | 200 | 422 |
| [S38] | Na |  |  | Ta |  |  | O |  | 0.09 |  |  | 0.72 |  |  | 0.19 |  | SSR | 873 | 2 |  |  |  | orthorombic | 4.01 | 41 | 1 | 0 |  |  | Hg | 400 | 200 | 1056 |
| [S38] | Na |  |  | Ta |  |  | O |  | 0.09 |  |  | 0.72 |  |  | 0.19 |  | HT | 973 | 2 |  |  |  | orthorombic | 4 | 34 | 1 | 0 |  |  | Hg | 400 | 200 | 399.83 |
| [S38] | Na |  |  | Ta |  |  | O |  | 0.09 |  |  | 0.72 |  |  | 0.19 |  | HT | 873 | 2 | impreg | RuO2 | 0.5 | orthorombic | 4.01 | 41 | 1 | 0 |  |  | Hg | 400 | 200 | 2333.33 |
| [S38] | Na |  |  | Ta |  |  | O |  | 0.09 |  |  | 0.72 |  |  | 0.19 |  | HT | 873 | 2 | impreg | RuO2 | 1 | orthorombic | 4.01 | 41 | 1 | 0 |  |  | Hg | 400 | 200 | 25833.33 |
| [S38] | Na |  |  | Ta |  |  | O |  | 0.09 |  |  | 0.72 |  |  | 0.19 |  | HT | 873 | 2 | impreg | RuO2 | 1.5 | orthorombic | 4.01 | 41 | 1 | 0 |  |  | Hg | 400 | 200 | 12716.67 |
| [S39] | Na | La |  | Ta |  |  | O |  | 0.088 | 0.019 |  | 0.705 |  |  | 0.186 |  | HT | 1423 | 5 |  |  |  |  | 3.97 | 4.9 | 1 | 0 |  |  | Xe | 300 | 400 | 3433 |
| [S39] | Na | La |  | Ta |  |  | O |  | 0.088 | 0.019 |  | 0.705 |  |  | 0.186 |  | HT | 1423 | 5 |  |  |  |  | 3.97 | 4.9 | 1 | 20 |  |  | Xe | 300 | 400 | 9933 |
| [S40] | In |  |  | Ta |  |  | O |  | 0.32 |  |  | 0.5 |  |  | 0.18 |  | HT | 1373 | 12 | impreg | NiO | 3 |  | 2.62 | 1.43 | 1.42 | 0 |  |  | halogen | 500 | 420 | 2 |
| [S40] | In |  |  | Ta |  |  | O |  | 0.32 |  |  | 0.5 |  |  | 0.18 |  | SSR | 1373 | 12 | impreg | NiO | 3 |  | 2.73 | 0.7 | 1.42 | 0 |  |  | halogen | 500 | 420 | 1.2 |
| [S41] | Na | La |  | Ta |  |  | O |  | 0.089 | 0.011 |  | 0.712 |  |  | 0.189 |  | SSR | 1420 | 10 | impreg | NiO | 0.2 | orthorombic | 4.01 | 3.5 | 2.56 | 0 |  |  | Hg | 400 | 365 | 3565 |
| [S42] | La |  |  | Ta | Al |  | O |  | 0.47 |  |  | 0.3 | 0.05 |  | 0.19 |  | SG | 1473 | 24 | impreg | NiO | 0.2 | orthorombic | 4.6 | 2.14 | 0.238 | 5 |  |  | Hg | 350 | 365 | 109 |
| [S42] | La |  |  | Ta | Al |  | O |  | 0.47 |  |  | 0.3 | 0.05 |  | 0.19 |  | SSR | 1473 | 24 | impreg | NiO | 0.2 | orthorombic | 4.6 | 2.14 | 0.25 | 0 |  |  | Hg | 350 | 365 | 94.4 |
| [S42] | La |  |  | Ta | Al |  | O |  | 0.47 |  |  | 0.3 | 0.05 |  | 0.19 |  | SSR | 1473 | 24 |  |  |  | orthorombic | 4.6 | 2.14 | 0.25 | 0 |  |  | Hg | 350 | 365 | 39 |
| [S42] | La |  |  | Ta | Al |  | O |  | 0.47 |  |  | 0.3 | 0.05 |  | 0.19 |  | SSR | 1473 | 24 | impreg | NiO | 0.1 | orthorombic | 4.6 | 2.14 | 0.25 | 0 |  |  | Hg | 350 | 365 | 55 |
| [S42] | La |  |  | Ta | Al |  | O |  | 0.47 |  |  | 0.3 | 0.05 |  | 0.19 |  | SSR | 1473 | 24 | impreg | NiO | 0.3 | orthorombic | 4.6 | 2.14 | 0.25 | 0 |  |  | Hg | 350 | 365 | 87 |
| [S42] | La |  |  | Ta | Al |  | O |  | 0.47 |  |  | 0.3 | 0.05 |  | 0.19 |  | SSR | 1473 | 24 | impreg | NiO | 0.4 | orthorombic | 4.6 | 2.14 | 0.25 | 0 |  |  | Hg | 350 | 365 | 72 |
| [S42] | La |  |  | Ta | Al |  | O |  | 0.47 |  |  | 0.3 | 0.05 |  | 0.19 |  | SSR | 1473 | 24 | impreg | NiO | 0.5 | orthorombic | 4.6 | 2.14 | 0.25 | 0 |  |  | Hg | 350 | 365 | 61 |
| [S43] | Bi | La |  | Nb | Al |  | O |  | 0.592 | 0.044 |  | 0.146 | 0.042 |  | 0.176 |  | SSR | 1223 | 24 | impreg | NiO | 0.022 | cubic | 2.89 |  | 0.238 | 5 |  |  | Hg | 350 | 365 | 106 |
| [S43] | Bi | La |  | Nb | Al |  | O |  | 0.592 | 0.044 |  | 0.146 | 0.042 |  | 0.176 |  | SSR | 1223 | 24 | impreg | NiO | 0.987 | cubic | 2.89 |  | 0.238 | 5 |  |  | Hg | 350 | 365 | 124 |
| [S43] | Bi | La |  | Nb | Al |  | O |  | 0.592 | 0.044 |  | 0.146 | 0.042 |  | 0.176 |  | SSR | 1223 | 24 | impreg | NiO | 1.5 | cubic | 2.89 |  | 0.238 | 5 |  |  | Hg | 350 | 365 | 135 |
| [S43] | Bi | La |  | Nb | Al |  | O |  | 0.592 | 0.044 |  | 0.146 | 0.042 |  | 0.176 |  | SSR | 1223 | 24 | impreg | NiO | 2.03 | cubic | 2.89 |  | 0.238 | 5 |  |  | Hg | 350 | 365 | 141 |
| [S43] | Bi | La |  | Nb | Al |  | O |  | 0.592 | 0.044 |  | 0.146 | 0.042 |  | 0.176 |  | SSR | 1223 | 24 | impreg | NiO | 2.96 | cubic | 2.89 |  | 0.238 | 5 |  |  | Hg | 350 | 365 | 134 |
| [S43] | Bi | La |  | Nb | Al |  | O |  | 0.592 | 0.044 |  | 0.146 | 0.042 |  | 0.176 |  | SSR | 1223 | 24 | impreg | NiO | 5.02 | cubic | 2.89 |  | 0.238 | 5 |  |  | Hg | 350 | 365 | 125 |
| [S44] | Sr |  |  | Ta |  |  | O |  | 0.27 |  |  | 0.558 |  |  | 0.173 |  | SSR |  |  |  |  |  | amorphous | 4.6 |  | 1.25 | 0 |  |  | Hg | 350 | 365 | 1287.5 |
| [S44] | Sr |  |  | Ta |  |  | O |  | 0.27 |  |  | 0.558 |  |  | 0.173 |  | SSR | 643 | 1 | impreg | NiO | 0.15 | amorphous | 4.6 |  | 1.25 | 0 |  |  | Hg | 350 | 365 | 2345 |
| [S45] | Sr | H |  | Nb |  |  | O |  | 0.08 | 0.03 |  | 0.62 |  |  | 0.3 |  | SSR |  |  | PD | Pt | 1.12 | octahedral | 3.204 | 11.64 | 2 | 10 |  |  | Hg | 100 | 290 | 6633.33 |
| [S45] | Sr | H |  | Nb |  |  | O |  | 0.08 | 0.03 |  | 0.62 |  |  | 0.3 |  | HT |  |  |  |  |  | octahedral | 3.188 | 11.72 | 2 | 10 |  |  | Hg | 100 | 290 | 681.67 |
| [S45] | Sr | K |  | Nb |  |  | O |  | 0.07 | 0.1 |  | 0.55 |  |  | 0.27 |  | HT |  |  | PD | Pt | 1.12 | octahedral | 3.157 | 11.6 | 2 | 10 |  |  | Hg | 100 | 290 | 121 |
| [S46] | La | H |  | Nb |  |  | O |  | 0.317 | 0.002 |  | 0.424 |  |  | 0.256 |  | ionexchange | 1423 | 12 | PD | Pt | 1 | tetragonal | 3.36 | 4.18 | 2 | 10 | NaNO2 |  | Hg | 100 | 400 | 2600 |
| [S46] | La | H |  | Nb | In |  | O |  | 0.239 | 0.002 |  | 0.32 | 0.247 |  | 0.193 |  | ionexchange | 1423 | 12 | PD | Pt | 1 | tetragonal | 3.48 | 4.62 | 2 | 10 | NaNO2 |  | Hg | 100 | 400 | 2880 |
| [S46] | La | H |  | Nb | In |  | O |  | 0.192 | 0.001 |  | 0.256 | 0.396 |  | 0.155 |  | SSR | 1423 | 12 | PD | Pt | 1 | tetragonal | 3.47 | 5.17 | 2 | 10 | NaNO2 |  | Hg | 100 | 400 | 3003 |
| [S46] | La | H |  | Nb | In |  | O |  | 0.16 | 0.001 |  | 0.214 | 0.496 |  | 0.129 |  | ionexchange | 1423 | 12 | PD | Pt | 1 | tetragonal | 3.41 | 7.2 | 2 | 10 | NaNO2 |  | Hg | 100 | 400 | 4900 |
| [S46] | La | H |  | Nb | In |  | O |  | 0.137 | 0.001 |  | 0.184 | 0.567 |  | 0.111 |  | ionexchange | 1423 | 12 | PD | Pt | 1 | tetragonal | 3.42 | 7.7 | 2 | 10 | NaNO2 |  | Hg | 100 | 400 | 5233 |
| [S46] | La | H |  | Nb | In |  | O |  | 0.107 | 0.001 |  | 0.143 | 0.663 |  | 0.086 |  | ionexchange | 1423 | 12 | PD | Pt | 1 | tetragonal | 3.44 | 8.23 | 2 | 10 | NaNO2 |  | Hg | 100 | 400 | 940 |
| [S47] | Bi |  |  | Ta |  |  | O |  | 0.46 |  |  | 0.399 |  |  | 0.141 |  | ionexchange | 1373 | 48 |  |  |  | octahedral | 3.3 | 1.15 | 0.238 | 5 | NaNO2 |  | Hg | 350 | 400 | 528 |
| [S47] | Bi |  |  | Ta | Cu |  | O |  | 0.462 |  |  | 0.396 | 0.001 |  | 0.141 |  | ionexchange | 1373 | 48 |  |  |  | octahedral | 3.1 | 1.22 | 0.238 | 5 | NaNO2 |  | Hg | 350 | 400 | 746 |
| [S47] | Bi |  |  | Ta | Cu |  | O |  | 0.463 |  |  | 0.393 | 0.003 |  | 0.142 |  | ionexchange | 1373 | 48 |  |  |  | octahedral | 2.9 | 1.43 | 0.238 | 5 | NaNO2 |  | Hg | 350 | 400 | 884 |
| [S47] | Bi |  |  | Ta | Cu |  | O |  | 0.446 |  |  | 0.39 | 0.004 |  | 0.142 |  | SSR | 1373 | 48 |  |  |  | octahedral | 2.8 | 1.47 | 0.238 | 5 | NaNO2 |  | Hg | 350 | 400 | 649 |
| [S47] | Bi |  |  | Ta | Cu |  | O |  | 0.465 |  |  | 0.387 | 0.006 |  | 0.142 |  | SSR | 1373 | 48 |  |  |  | octahedral | 2.7 | 0.94 | 0.238 | 5 | NaNO2 |  | Hg | 350 | 400 | 387 |
| [S47] | Bi |  |  | Ta |  |  | O |  | 0.46 |  |  | 0.399 |  |  | 0.141 |  | SSR | 1373 | 48 | impreg | RuO2 | 0.1 | octahedral | 3.3 | 1.15 | 0.238 | 5 | NaNO2 |  | Hg | 350 | 400 | 490 |
| [S47] | Bi |  |  | Ta |  |  | O |  | 0.46 |  |  | 0.399 |  |  | 0.141 |  | SSR | 1373 | 48 | impreg | RuO2 | 0.2 | octahedral | 3.3 | 1.15 | 0.238 | 5 | NaNO2 |  | Hg | 350 | 400 | 560 |
| [S47] | Bi |  |  | Ta |  |  | O |  | 0.46 |  |  | 0.399 |  |  | 0.141 |  | SSR | 1373 | 48 | impreg | RuO2 | 0.3 | octahedral | 3.3 | 1.15 | 0.238 | 5 | NaNO2 |  | Hg | 350 | 400 | 929 |
| [S47] | Bi |  |  | Ta |  |  | O |  | 0.46 |  |  | 0.399 |  |  | 0.141 |  | SSR | 1373 | 48 | impreg | RuO2 | 0.4 | octahedral | 3.3 | 1.15 | 0.238 | 5 | NaNO2 |  | Hg | 350 | 400 | 785 |
| [S47] | Bi |  |  | Ta |  |  | O |  | 0.46 |  |  | 0.399 |  |  | 0.141 |  | SSR | 1373 | 48 | impreg | RuO2 | 0.5 | octahedral | 3.3 | 1.15 | 0.238 | 5 | NaNO2 |  | Hg | 350 | 400 | 663 |
| [S48] | Sr |  |  | Ti |  |  | O |  | 0.48 |  |  | 0.26 |  |  | 0.26 |  | SSR | 973 | 4 | impreg | Pt | 0.5 | cubic | 3.16 | 10 | 1 | 0 |  |  | Hg | 176 | 254 | 80 |
| [S48] | Sr |  |  | Ti |  |  | O |  | 0.48 |  |  | 0.26 |  |  | 0.26 |  | SSR | 973 | 4 | impreg | Pt | 0.5 | cubic | 3.16 | 10 | 1 | 20 |  |  | Hg | 176 | 254 | 212 |
| [S48] | Sr |  |  | Ti |  |  | O |  | 0.48 |  |  | 0.26 |  |  | 0.26 |  | SSR | 973 | 4 | impreg | Pt | 0.5 | cubic | 3.16 | 10 | 1 | 40 |  |  | Hg | 176 | 254 | 226 |
| [S48] | Sr |  |  | Ti |  |  | O |  | 0.48 |  |  | 0.26 |  |  | 0.26 |  | SG | 973 | 4 | impreg | Pt | 0.5 | cubic | 3.16 | 10 | 1 | 60 |  |  | Hg | 176 | 254 | 237 |
| [S48] | Sr |  |  | Ti |  |  | O |  | 0.48 |  |  | 0.26 |  |  | 0.26 |  | SG | 973 | 4 | impreg | Pt | 0.5 | cubic | 3.16 | 10 | 1 | 80 |  |  | Hg | 176 | 254 | 243 |
| [S48] | Sr |  |  | Ti |  |  | O |  | 0.48 |  |  | 0.26 |  |  | 0.26 |  | SG | 973 | 4 | impreg | Pt | 0.5 | cubic | 3.16 | 10 | 1 | 100 |  |  | Hg | 176 | 254 | 246 |
| [S48] | Sr |  |  | Ti |  |  | O |  | 0.48 |  |  | 0.26 |  |  | 0.26 |  | SG | 973 | 4 | impreg | Pt | 0.5 | cubic | 3.16 | 10 | 1 | 50 |  |  | Hg | 176 | 254 | 453.87 |
| [S49] | Na |  |  | Nb |  |  | O |  | 0.14 |  |  | 0.57 |  |  | 0.29 |  | SG | 1173 | 10 | PD | Pt | 0.5 | orthorombic | 3.4 | 1.7 | 0.27 | 13.5 |  |  | Hg | 400 | 365 | 9133.33 |
| [S49] | Na |  |  | Nb |  |  | O |  | 0.14 |  |  | 0.57 |  |  | 0.29 |  | SG |  |  | PD | Pt | 0.5 | orthorombic | 3.4 | 2 | 0.27 | 13.5 |  |  | Hg | 400 | 365 | 9150 |
| [S49] | Na |  |  | Nb |  |  | O |  | 0.14 |  |  | 0.57 |  |  | 0.29 |  | SG | 873 | 1 | PD | Pt | 0.5 | orthorombic | 3.3 | 37.8 | 0.27 | 13.5 |  |  | Hg | 400 | 365 | 10466 |
| [S49] | Na |  |  | Nb |  |  | O |  | 0.14 |  |  | 0.57 |  |  | 0.29 |  | SSR | 1173 | 5 | PD | Pt | 0.5 | orthorombic | 3.35 | 4.4 | 0.27 | 13.5 |  |  | Hg | 400 | 365 | 10116 |
| [S49] | Na |  |  | Nb |  |  | O |  | 0.14 |  |  | 0.57 |  |  | 0.29 |  | HT | 1173 | 10 | PD | RuO2 | 1.25 | orthorombic | 3.4 | 1.7 | 0.27 | 0 |  |  | Hg | 400 | 365 | 102 |
| [S49] | Na |  |  | Nb |  |  | O |  | 0.14 |  |  | 0.57 |  |  | 0.29 |  | PC |  |  | PD | RuO2 | 1.25 | orthorombic | 3.4 | 2 | 0.27 | 0 |  |  | Hg | 400 | 365 | 82.83 |
| [S49] | Na |  |  | Nb |  |  | O |  | 0.14 |  |  | 0.57 |  |  | 0.29 |  | PC | 873 | 1 | PD | RuO2 | 1.25 | orthorombic | 3.3 | 37.8 | 0.27 | 0 |  |  | Hg | 400 | 365 | 335 |
| [S49] | Na |  |  | Nb |  |  | O |  | 0.14 |  |  | 0.57 |  |  | 0.29 |  | SSR | 1173 | 5 | PD | RuO2 | 1.25 | orthorombic | 3.35 | 4.4 | 0.27 | 0 |  |  | Hg | 400 | 365 | 78 |
| [S50] | Bi | Sr |  | Ta |  |  | O |  | 0.413 | 0.087 |  | 0.358 |  |  | 0.142 |  | HT | 1473 | 24 |  |  |  | orthorombic | 3.64 | 2.36 | 0.5 | 12.5 |  |  | Hg | 350 | 365 | 22600 |
| [S50] | Bi | Ba |  | Ta |  |  | O |  | 0.394 | 0.129 |  | 0.341 |  |  | 0.136 |  | PC | 1473 | 24 |  |  |  | orthorombic | 3.52 | 2.18 | 0.5 | 12.5 |  |  | Hg | 350 | 365 | 513 |
| [S50] | Bi | Ca |  | Ta |  |  | O |  | 0.434 | 0.042 |  | 0.375 |  |  | 0.149 |  | PC | 1473 | 24 |  |  |  | orthorombic | 3.67 | 1.96 | 0.5 | 12.5 |  |  | Hg | 350 | 365 | 1400 |
| [S51] | Sr |  |  | Ti |  |  | O |  | 0.478 |  |  | 0.261 |  |  | 0.262 |  | SSR | 773 | 5 | PD | Pt | 0.32 | cubic | 3.1 |  | 1 | 41.67 |  |  | Hg | 500 | 365 | 1948 |
| [S51] | Sr |  |  | Ti |  |  | O |  | 0.478 |  |  | 0.261 |  |  | 0.262 |  | SSR | 873 | 5 | PD | Pt | 0.32 | cubic | 3.1 |  | 1 | 41.67 |  |  | Hg | 500 | 365 | 3020 |
| [S51] | Sr |  |  | Ti |  |  | O |  | 0.478 |  |  | 0.261 |  |  | 0.262 |  | SSR | 973 | 5 | PD | Pt | 0.32 | cubic | 3.1 |  | 1 | 41.67 |  |  | Hg | 500 | 365 | 2540 |
| [S51] | Sr |  |  | Ti |  |  | O |  | 0.478 |  |  | 0.261 |  |  | 0.262 |  | PC | 1073 | 5 | PD | Pt | 0.32 | cubic | 3.1 |  | 1 | 41.67 |  |  | Hg | 500 | 365 | 1686 |
| [S51] | Sr |  |  | Ti |  |  | O |  | 0.478 |  |  | 0.261 |  |  | 0.262 |  | PC | 1273 | 5 | PD | Pt | 0.32 | cubic | 3.1 |  | 1 | 41.67 |  |  | Hg | 500 | 365 | 580 |
| [S51] | Sr |  |  | Ti |  |  | O |  | 0.478 |  |  | 0.261 |  |  | 0.262 |  | PC | 1073 | 2 | PD | Pt | 0.32 | cubic | 2 |  | 1 | 41.67 |  |  | Hg | 500 | 365 | 16 |
| [S51] | Sr |  |  | Ti |  |  | O |  | 0.478 |  |  | 0.261 |  |  | 0.262 |  | PC | 1073 | 5 | PD | Pt | 0.32 | cubic | 3.1 |  | 1 | 41.67 |  |  | Hg | 500 | 365 | 988 |
| [S51] | Sr |  |  | Ti |  |  | O |  | 0.478 |  |  | 0.261 |  |  | 0.262 |  | PC | 1273 | 3 | PD | Pt | 0.32 | cubic | 3.1 |  | 1 | 41.67 |  |  | Hg | 500 | 365 | 1272 |
| [S51] | Sr |  |  | Ti |  |  | O |  | 0.478 |  |  | 0.261 |  |  | 0.262 |  | novel | 1273 | 3 | PD | Pt | 0.32 | cubic | 3.1 |  | 1 | 41.67 |  |  | Hg | 500 | 365 | 185 |
| [S52] | Na |  |  | Ta |  |  | O |  | 0.091 |  |  | 0.718 |  |  | 0.191 |  | SSR | 773 | 3 |  |  |  | orthorombic | 4.1 | 0.6 | 1.11 | 0 |  |  | Hg | 400 | 365 | 89.25 |
| [S52] | Na |  |  | Ta |  |  | O |  | 0.091 |  |  | 0.718 |  |  | 0.191 |  | SSR | 1473 | 1 |  |  |  | cubic | 3.9 | 23 | 1.11 | 0 |  |  | Hg | 400 | 365 | 2097.5 |
| [S53] | Ca |  |  | Ta |  |  | O |  | 0.145 |  |  | 0.653 |  |  | 0.202 |  | SSR | 873 | 1 | impreg | NiO | 0.2 | amorphous | 4.4 | 63 | 1.25 | 0 | NaOH |  | Hg | 450 | 200 | 295 |
| [S54] | Sr |  |  | Ti |  |  | O |  | 0.559 |  |  | 0.203 |  |  | 0.238 |  | SSR | 1373 | 30 | impreg | NiO | 1 | octahedral | 3.2 | 8.145 | 2.1 | 0 |  |  | Hg | 400 | 365 | 61.9 |
| [S54] | Sr |  |  | Ti |  |  | O |  | 0.559 |  |  | 0.203 |  |  | 0.238 |  | SG | 1073 | 2 | impreg | NiO | 1 | octahedral | 3.2 | 3.49 | 2.1 | 0 |  |  | Hg | 400 | 365 | 82.5 |
| [S55] | Sr |  |  | Ta |  |  | O |  | 0.161 |  |  | 0.663 |  |  | 0.176 |  | HT | 1273 | 12 | impreg | NiO | 0.15 | orthorombic | 4.49 | 3.94 | 1.28 | 0 |  |  | Hg | 400 | 365 | 310 |
| [S55] | Sr |  |  | Ta |  |  | O |  | 0.409 |  |  | 0.423 |  |  | 0.168 |  | SSR | 1273 | 12 | impreg | NiO | 0.15 | cubic | 4.81 | 2.61 | 1.28 | 0 |  |  | Hg | 400 | 365 | 25.16 |
| [S55] | Sr |  |  | Ta |  |  | O |  | 0.313 |  |  | 0.516 |  |  | 0.171 |  | PC | 1273 | 12 | impreg | NiO | 0.15 | hexagonal | 4.75 | 2.99 | 1.28 | 0 |  |  | Hg | 400 | 365 | 973.33 |
| [S56] | Zn |  |  | In |  |  | S |  | 0.16 |  |  | 0.449 |  |  | 0.392 |  | SSR |  |  | PD | Pt | 1 | hexagonal | 2.35 | 119.2 | 1 | 0 | Na2S | Na2SO3 | Xe | 350 | 420 | 157 |
| [S56] | Zn |  |  | In |  |  | S |  | 0.144 |  |  | 0.504 |  |  | 0.352 |  | SSR |  |  | PD | Pt | 1 | hexagonal | 2.32 | 123.3 | 1 | 0 | Na2S | Na2SO3 | Xe | 350 | 420 | 259.33 |
| [S56] | Zn |  |  | In |  |  | S |  | 0.134 |  |  | 0.539 |  |  | 0.327 |  | SSR |  |  | PD | Pt | 1 | hexagonal | 2.3 | 124.4 | 1 | 0 | Na2S | Na2SO3 | Xe | 350 | 420 | 360 |
| [S56] | Zn |  |  | In |  |  | S |  | 0.125 |  |  | 0.569 |  |  | 0.306 |  | HT |  |  | PD | Pt | 1 | hexagonal | 2.25 | 109 | 1 | 0 | Na2S | Na2SO3 | Xe | 350 | 420 | 323.67 |
| [S56] | Zn |  |  | In |  |  | S |  | 0.117 |  |  | 0.596 |  |  | 0.287 |  | HT |  |  | PD | Pt | 1 | hexagonal | 2.23 | 100.5 | 1 | 0 | Na2S | Na2SO3 | Xe | 350 | 420 | 307.67 |
| [S56] | Zn |  |  | In |  |  | S |  | 0.112 |  |  | 0.612 |  |  | 0.276 |  | HT |  |  | PD | Pt | 1 | hexagonal | 2.25 | 97.3 | 1 | 0 | Na2S | Na2SO3 | Xe | 350 | 420 | 282.33 |
| [S57] | Sr |  |  | Zr |  |  | O |  | 0.386 |  |  | 0.402 |  |  | 0.212 |  | HT | 1373 | 24 |  |  |  | orthorombic | 4.1 | 2 | 1 | 0 |  |  | UV |  | 254 | 8 |
| [S58] | Zn |  |  | Ga |  |  | O |  | 0.243 |  |  | 0.519 |  |  | 0.238 |  | HT | 1173 | 15 |  |  |  | cubic | 4.75 | 5.2 | 1 | 0 |  |  | Hg | 500 | 365 | 9 |
| [S58] | Zn |  |  | Ga |  |  | O |  | 0.243 |  |  | 0.519 |  |  | 0.238 |  | HT |  |  |  |  |  | cubic | 4.77 | 20 | 1 | 0 |  |  | Hg | 500 | 365 | 14.6 |
| [S58] | Zn |  |  | Ga |  |  | O |  | 0.243 |  |  | 0.519 |  |  | 0.238 |  | SSR | 873 | 2 |  |  |  | cubic | 4.37 | 29 | 1 | 0 |  |  | Hg | 500 | 365 | 29 |
| [S58] | Zn |  |  | Ga |  |  | O |  | 0.243 |  |  | 0.519 |  |  | 0.238 |  | SSR | 1173 | 15 |  |  |  | cubic | 4.75 | 5.2 | 1 | 20 |  |  | Hg | 500 | 365 | 27.2 |
| [S58] | Zn |  |  | Ga |  |  | O |  | 0.243 |  |  | 0.519 |  |  | 0.238 |  | HT |  |  |  |  |  | cubic | 4.77 | 20 | 1 | 20 |  |  | Hg | 500 | 365 | 97.8 |
| [S58] | Zn |  |  | Ga |  |  | O |  | 0.243 |  |  | 0.519 |  |  | 0.238 |  | SG | 873 | 2 |  |  |  | cubic | 4.37 | 29 | 1 | 20 |  |  | Hg | 500 | 365 | 134.8 |
| [S59] | Ni |  |  | Ga |  |  | O |  | 0.225 |  |  | 0.531 |  |  | 0.244 |  | SSR | 773 | 5 | impreg | RuO2 | 1 | octahedral | 3.85 | 17 | 2 | 33 |  |  | Hg | 300 | 320 | 3 |
| [S60] | Ba |  |  | Nb | Ta |  | O |  | 0.466 |  |  | 0.126 | 0.245 |  | 0.163 |  | HT | 1173 | 3 |  |  |  | amorphous | 4.2 | 5 | 0.5 | 8.3 |  |  | Hg | 500 | 250 | 356 |
| [S60] | Ba |  |  | Ta |  |  | O |  | 0.416 |  |  | 0.439 | 0.245 |  | 0.145 |  | SG | 1173 | 3 |  |  |  | amorphous | 4.5 | 5 | 0.5 | 8.3 |  |  | Hg | 500 | 250 | 485.5 |
| [S60] | Ba |  |  | Nb |  |  | O |  | 0.529 |  |  | 0.286 | 0.245 |  | 0.185 |  | ionexchange | 1173 | 3 |  |  |  | amorphous | 3.9 | 5 | 0.5 | 8.3 |  |  | Hg | 500 | 250 | 590 |
| [S61] | Ba |  |  | In | Ta |  | O |  | 0.41 |  |  | 0.17 | 0.27 |  | 0.14 |  | electrospinning | 1400 | 15 | impreg | Pt | 1 | octahedral | 4.17 | 1 | 0.5 | 0 |  |  | Hg | 500 | 250 | 15.2 |
| [S62] | La | K |  | Ta |  |  | O |  | 0.144 | 0.121 |  | 0.561 |  |  | 0.174 |  | electrospinning | 1498 | 15 |  |  |  | tetragonal | 4 | 3.7 | 2.5 | 0 |  |  | Hg | 400 | 365 | 146 |
| [S62] | La | H |  | Ta |  |  | O |  | 0.164 | 0.004 |  | 0.636 |  |  | 0.197 |  | electrospinning | 1498 | 15 |  |  |  | tetragonal | 4 | 7.8 | 2.5 | 0 |  |  | Hg | 400 | 365 | 158 |
| [S62] | La |  |  | Ta |  |  | O |  | 0.167 |  |  | 0.659 |  |  | 0.175 |  | SSR | 1498 | 15 |  |  |  | tetragonal | 4 | 3.3 | 2.5 | 0 |  |  | Hg | 400 | 365 | 35 |
| [S62] | Sr | H |  | Ta |  |  | O |  | 0.155 | 0.004 |  | 0.642 |  |  | 0.199 |  | SSR | 1498 | 15 |  |  |  | tetragonal | 3.9 | 4 | 2.5 | 0 |  |  | Hg | 400 | 365 | 385 |
| [S62] | K |  |  | Ta |  |  | O |  | 0.146 |  |  | 0.675 |  |  | 0.179 |  | SSR | 1498 | 15 |  |  |  | tetragonal | 3.6 | 1.5 | 2.5 | 0 |  |  | Hg | 400 | 365 | 25 |
| [S63] | Y |  |  | Ta |  |  | O |  | 0.477 |  |  | 0.323 |  |  | 0.2 |  | SSR | 1623 | 2 |  |  |  | cubic | 4.6 | 1.6 | 1.2 | 0 |  |  | Hg | 400 | 200 | 0.001 |
| [S63] | La |  |  | Ta |  |  | O |  | 0.587 |  |  | 0.255 |  |  | 0.158 |  | SSR | 1273 | 2 |  |  |  | cubic | 4.6 | 3 | 1.2 | 0 |  |  | Hg | 400 | 200 | 8 |
| [S63] | La |  |  | Ta |  |  | O |  | 0.587 |  |  | 0.255 |  |  | 0.158 |  | SSR | 1373 | 2 |  |  |  | orthorombic | 4.6 | 2.8 | 1.2 | 0 |  |  | Hg | 400 | 200 | 328 |
| [S63] | Y |  |  | Nb |  |  | O |  | 0.566 |  |  | 0.197 |  |  | 0.237 |  | PC | 1623 | 2 |  |  |  | cubic | 3.9 | 1.2 | 1.2 | 0 |  |  | Hg | 400 | 200 | 0.001 |
| [S63] | La |  |  | Nb |  |  | O |  | 0.67 |  |  | 0.149 |  |  | 0.18 |  | PC | 1173 | 2 |  |  |  | cubic | 3.9 | 2.8 | 1.2 | 0 |  |  | Hg | 400 | 200 | 2 |
| [S63] | La |  |  | Nb |  |  | O |  | 0.67 |  |  | 0.149 |  |  | 0.18 |  | PC | 1373 | 2 |  |  |  | cubic | 3.9 | 2.5 | 1.2 | 0 |  |  | Hg | 400 | 200 | 70 |
| [S63] | Y |  |  | Ti |  |  | O |  | 0.461 |  |  | 0.461 |  |  | 0.29 |  | PC | 1273 | 2 |  |  |  | cubic | 3.5 | 2 | 1.2 | 0 |  |  | Hg | 400 | 200 | 1700 |
| [S63] | La |  |  | Ti |  |  | O |  | 0.572 |  |  | 0.572 |  |  | 0.231 |  | PC | 1273 | 2 |  |  |  | monoclinic | 3.8 | 1.8 | 1.2 | 0 |  |  | Hg | 400 | 200 | 614 |
| [S64] | Sr |  |  | Sn |  |  | O |  | 0.345 |  |  | 0.467 |  |  | 0.189 |  | PC |  |  |  |  |  | orthorombic | 4.1 | 0.4 | 0.54 | 13.5 |  |  | Hg | 200 | 300 | 7200 |
| [S64] | Sr |  |  | Sn |  |  | O |  | 0.345 |  |  | 0.467 |  |  | 0.189 |  | PC |  |  |  |  |  | orthorombic |  | 0.5 | 0.54 | 13.5 |  |  | Hg | 200 | 300 | 7200 |
| [S64] | Sr |  |  | Sn |  |  | O |  | 0.345 |  |  | 0.467 |  |  | 0.189 |  | PC |  |  |  |  |  | orthorombic |  | 0.3 | 0.54 | 13.5 |  |  | Hg | 200 | 300 | 720 |
| [S65] | Y |  |  | In |  |  | O |  | 0.315 |  |  | 0.497 |  |  | 0.189 |  | HT | 1673 | 16 | impreg | RuO2 | 1 | cubic | 3.6 |  | 8.33 | 0 |  |  | Hg | 200 | 230 | 1 |
| [S65] | Y |  |  | In |  |  | O |  | 0.353 |  |  | 0.456 |  |  | 0.191 |  | HT | 1673 | 16 | impreg | RuO2 | 1 | cubic | 3.75 |  | 8.33 | 0 |  |  | Hg | 200 | 230 | 3.1 |
| [S65] | Y |  |  | In |  |  | O |  | 0.393 |  |  | 0.415 |  |  | 0.193 |  | HT | 1673 | 16 | impreg | RuO2 | 1 | cubic | 3.92 |  | 8.33 | 0 |  |  | Hg | 200 | 230 | 5 |
| [S65] | Y |  |  | In |  |  | O |  | 0.433 |  |  | 0.373 |  |  | 0.195 |  | SSR | 1673 | 16 | impreg | RuO2 | 1 | cubic | 4.1 |  | 8.33 | 0 |  |  | Hg | 200 | 230 | 6 |
| [S65] | Y |  |  | In |  |  | O |  | 0.474 |  |  | 0.329 |  |  | 0.197 |  | SSR | 1673 | 16 | impreg | RuO2 | 1 | cubic | 4.18 |  | 8.33 | 0 |  |  | Hg | 200 | 230 | 7.9 |
| [S65] | Y |  |  | In |  |  | O |  | 0.516 |  |  | 0.285 |  |  | 0.199 |  | SSR | 1673 | 16 | impreg | RuO2 | 1 | cubic | 4.39 |  | 8.33 | 0 |  |  | Hg | 200 | 230 | 7 |
| [S65] | Y |  |  | In |  |  | O |  | 0.559 |  |  | 0.24 |  |  | 0.201 |  | SSR | 1673 | 16 | impreg | RuO2 | 1 | cubic | 4.87 |  | 8.33 | 0 |  |  | Hg | 200 | 230 | 5.8 |
| [S66] | K |  |  | Nb |  |  | O |  | 0.217 |  |  | 0.516 |  |  | 0.267 |  | SSR |  |  | PD | Pt | 0.5 | orthorombic | 3.2 | 8.5 | 0.476 | 12 |  |  | Hg | 400 | 365 | 2060 |
| [S67] | Na |  |  | Nb |  |  | O |  | 0.14 |  |  | 0.567 |  |  | 0.293 |  | SSR | 773 | 12 | PD | Pt | 0.8 |  | 3.2 | 12.5 | 0.81 | 18.5 |  |  | Xe | 300 | 300 | 12.3 |
| [S67] | Na |  |  | Nb | In |  | O |  | 0.113 |  |  | 0.456 | 0.161 |  | 0.274 |  | SSR | 773 | 12 | PD | Pt | 0.8 |  | 3.1 | 17.4 | 0.81 | 18.5 |  |  | Xe | 300 | 300 | 16.9 |
| [S67] | Na |  |  | Nb | In |  | O |  | 0.09 |  |  | 0.362 | 0.298 |  | 0.25 |  | HT | 773 | 12 | PD | Pt | 0.8 |  | 3 | 22.9 | 0.81 | 18.5 |  |  | Xe | 300 | 300 | 42.9 |
| [S67] | Na |  |  | Nb | In |  | O |  | 0.07 |  |  | 0.281 | 0.417 |  | 0.232 |  | co-pre | 773 | 12 | PD | Pt | 0.8 |  | 2.9 | 29.3 | 0.81 | 18.5 |  |  | Xe | 300 | 300 | 44.6 |
| [S67] | Na |  |  | Nb | In |  | O |  | 0.052 |  |  | 0.21 | 0.52 |  | 0.217 |  | co-pre | 773 | 12 | PD | Pt | 0.8 |  | 2.8 | 32.7 | 0.81 | 18.5 |  |  | Xe | 300 | 300 | 15.6 |
| [S67] | Na |  |  | Nb | In |  | O |  | 0.023 |  |  | 0.093 | 0.691 |  | 0.193 |  | co-pre | 773 | 12 | PD | Pt | 0.8 |  | 2.7 | 44 | 0.81 | 18.5 |  |  | Xe | 300 | 300 | 4.1 |
| [S67] | Na |  |  | Nb |  |  | O |  | 0.14 |  |  | 0.567 |  |  | 0.293 |  | co-pre | 773 | 12 | PD | Pt | 0.8 |  | 3.2 | 12.5 | 0.81 | 18.5 |  |  | Xe | 300 | 420 | 0.3 |
| [S67] | Na |  |  | Nb | In |  | O |  | 0.113 |  |  | 0.456 | 0.161 |  | 0.274 |  | co-pre | 773 | 12 | PD | Pt | 0.8 |  | 3.1 | 17.4 | 0.81 | 18.5 |  |  | Xe | 300 | 420 | 6.6 |
| [S67] | Na |  |  | Nb | In |  | O |  | 0.09 |  |  | 0.362 | 0.298 |  | 0.25 |  | co-pre | 773 | 12 | PD | Pt | 0.8 |  | 3 | 22.9 | 0.81 | 18.5 |  |  | Xe | 300 | 420 | 16.4 |
| [S67] | Na |  |  | Nb | In |  | O |  | 0.07 |  |  | 0.281 | 0.417 |  | 0.232 |  | co-pre | 773 | 12 | PD | Pt | 0.8 |  | 2.9 | 29.3 | 0.81 | 18.5 |  |  | Xe | 300 | 420 | 13.2 |
| [S67] | Na |  |  | Nb | In |  | O |  | 0.052 |  |  | 0.21 | 0.52 |  | 0.217 |  | co-pre | 773 | 12 | PD | Pt | 0.8 |  | 2.8 | 32.7 | 0.81 | 18.5 |  |  | Xe | 300 | 420 | 4.8 |
| [S67] | Na |  |  | Nb | In |  | O |  | 0.023 |  |  | 0.093 | 0.691 |  | 0.193 |  | co-pre | 773 | 12 | PD | Pt | 0.8 |  | 2.7 | 44 | 0.81 | 18.5 |  |  | Xe | 300 | 420 | 1.3 |
| [S68] | Ba |  |  | Ta |  |  | O |  | 0.416 |  |  | 0.439 |  |  | 0.145 |  | co-pre | 1423 | 18 |  |  |  | octahedral | 4.06 |  | 1 | 20 |  |  | Xe | 300 | 400 | 300 |
| [S68] | Ba |  |  | Ta |  |  | O | N | 0.416 |  |  | 0.438 |  |  | 0.145 | 0.001 | co-pre | 1423 | 18 |  |  |  | octahedral | 1.78 |  | 1 | 20 |  |  | Xe | 300 | 400 | 500 |
| [S69] | Na |  |  | Ta |  |  | O |  | 0.091 |  |  | 0.718 |  |  | 0.191 |  | co-pre |  |  |  |  |  | orthorombic | 3.64 |  | 1 | 25 | AgNO3 |  | Xe | 300 | 420 | 1660 |
| [S69] | Na |  |  | Ta |  |  | O |  | 0.091 |  |  | 0.718 |  |  | 0.191 |  | SSR |  |  | PD | Ag | 0.05 | orthorombic | 3.64 |  | 1 | 25 | AgNO3 |  | Xe | 300 | 420 | 2740 |
| [S69] | Na |  |  | Ta |  |  | O |  | 0.091 |  |  | 0.718 |  |  | 0.191 |  | SSR |  |  | PD | Ag | 0.1 | orthorombic | 3.64 |  | 1 | 25 | AgNO3 |  | Xe | 300 | 420 | 3540 |
| [S69] | Na |  |  | Ta |  |  | O |  | 0.091 |  |  | 0.718 |  |  | 0.191 |  | HT |  |  | PD | Ag | 0.2 | orthorombic | 3.64 |  | 1 | 25 | AgNO3 |  | Xe | 300 | 420 | 3170 |
| [S70] | Na |  |  | Ta |  |  | O |  | 0.091 |  |  | 0.718 |  |  | 0.191 |  | HT | 1423 | 10 |  |  |  | cubic | 4 | 2 | 0.5 | 10 |  |  | Hg | 150 | 365 | 1600 |
| [S71] | Na |  |  | Ta |  |  | O |  | 0.091 |  |  | 0.718 |  |  | 0.191 |  | HT | 543 | 2 |  |  |  | cubic | 3.75 |  | 0.6 | 20 |  |  | Hg | 450 | 365 | 90 |
| [S71] | Na |  |  | Ta |  |  | O |  | 0.091 |  |  | 0.718 |  |  | 0.191 |  | HT | 543 | 2 | PD | NiO | 0.05 | cubic | 3.75 |  | 0.6 | 20 |  |  | Hg | 450 | 365 | 640 |
| [S71] | Na |  |  | Ta |  |  | O |  | 0.091 |  |  | 0.718 |  |  | 0.191 |  | SSR | 543 | 2 | PD | NiO | 0.1 | cubic | 3.75 |  | 0.6 | 20 |  |  | Hg | 450 | 365 | 740 |
| [S71] | Na |  |  | Ta |  |  | O |  | 0.091 |  |  | 0.718 |  |  | 0.191 |  | HT | 543 | 2 | PD | NiO | 0.2 | cubic | 3.75 |  | 0.6 | 20 |  |  | Hg | 450 | 365 | 1900 |
| [S71] | Na |  |  | Ta |  |  | O |  | 0.091 |  |  | 0.718 |  |  | 0.191 |  | HT | 543 | 2 | PD | NiO | 0.4 | cubic | 3.75 |  | 0.6 | 20 |  |  | Hg | 450 | 365 | 1600 |
| [S71] | Na |  |  | Ta |  |  | O |  | 0.091 |  |  | 0.718 |  |  | 0.191 |  | HT | 543 | 2 | PD | NiO | 0.8 | cubic | 3.75 |  | 0.6 | 20 |  |  | Hg | 450 | 365 | 1000 |
| [S71] | Na |  |  | Ta |  |  | O |  | 0.091 |  |  | 0.718 |  |  | 0.191 |  | HT | 543 | 2 | PD | NiO | 1.2 | cubic | 3.75 |  | 0.6 | 20 |  |  | Hg | 450 | 365 | 540 |
| [S71] | Na |  |  | Ta |  |  | O |  | 0.091 |  |  | 0.718 |  |  | 0.191 |  | HT | 543 | 2 | PD | NiO | 1.6 | cubic | 3.75 |  | 0.6 | 20 |  |  | Hg | 450 | 365 | 460 |
| [S71] | Na |  |  | Ta |  |  | O |  | 0.091 |  |  | 0.718 |  |  | 0.191 |  | HT | 543 | 2 | PD | NiO | 2 | cubic | 3.75 |  | 0.6 | 20 |  |  | Hg | 450 | 365 | 420 |
| [S71] | Na |  |  | Ta |  |  | O |  | 0.091 |  |  | 0.718 |  |  | 0.191 |  | HT | 543 | 2 | impreg | NiO | 0.05 | cubic | 3.75 |  | 0.6 | 20 |  |  | Hg | 450 | 365 | 160 |
| [S71] | Na |  |  | Ta |  |  | O |  | 0.091 |  |  | 0.718 |  |  | 0.191 |  | HT | 543 | 2 | impreg | NiO | 0.1 | cubic | 3.75 |  | 0.6 | 20 |  |  | Hg | 450 | 365 | 220 |
| [S71] | Na |  |  | Ta |  |  | O |  | 0.091 |  |  | 0.718 |  |  | 0.191 |  | HT | 543 | 2 | impreg | NiO | 0.2 | cubic | 3.75 |  | 0.6 | 20 |  |  | Hg | 450 | 365 | 340 |
| [S71] | Na |  |  | Ta |  |  | O |  | 0.091 |  |  | 0.718 |  |  | 0.191 |  | HT | 543 | 2 | impreg | NiO | 0.4 | cubic | 3.75 |  | 0.6 | 20 |  |  | Hg | 450 | 365 | 220 |
| [S71] | Na |  |  | Ta |  |  | O |  | 0.091 |  |  | 0.718 |  |  | 0.191 |  | HT | 543 | 2 | impreg | NiO | 0.8 | cubic | 3.75 |  | 0.6 | 20 |  |  | Hg | 450 | 365 | 310 |
| [S71] | Na |  |  | Ta |  |  | O |  | 0.091 |  |  | 0.718 |  |  | 0.191 |  | HT | 543 | 2 | impreg | NiO | 1.2 | cubic | 3.75 |  | 0.6 | 20 |  |  | Hg | 450 | 365 | 260 |
| [S71] | Na |  |  | Ta |  |  | O |  | 0.091 |  |  | 0.718 |  |  | 0.191 |  | HT | 543 | 2 | impreg | NiO | 1.6 | cubic | 3.75 |  | 0.6 | 20 |  |  | Hg | 450 | 365 | 460 |
| [S71] | Na |  |  | Ta |  |  | O |  | 0.091 |  |  | 0.718 |  |  | 0.191 |  | HT | 543 | 2 | impreg | NiO | 2 | cubic | 3.75 |  | 0.6 | 20 |  |  | Hg | 450 | 365 | 400 |
| [S72] | Ga |  |  | In |  |  | O |  | 0.351 |  |  | 0.437 |  |  | 0.212 |  | HT | 1470 | 10 | PD | Pt | 1 | octahedral | 3.8 | 1.3 | 1 | 5.4 | AgNO3 |  | Hg | 450 | 365 | 30 |
| [S73] | K |  |  | Ta | Zr |  | O |  | 0.169 |  |  | 0.624 | 0.027 |  | 0.18 |  | HT | 1173 |  | impreg | NiO | 1.5 |  | 3.8 |  | 3.33 | 0 |  |  | Xe | 500 | 420 | 1223 |
| [S74] | Na | La |  | Ta |  |  | O |  | 0.091 | 0.006 |  | 0.714 |  |  | 0.189 |  | HT | 1420 | 10 | impreg | NiO | 0.2 |  | 4.01 | 2.5 | 2.56 | 0 | NaOH |  | Hg | 400 | 365 | 15000 |
| [S75] | Na |  |  | Sb |  |  | O |  | 0.119 |  |  | 0.632 |  |  | 0.249 |  | SSR | 1173 | 16 | impreg | RuO2 | 1 | octahedral | 4.41 |  | 12.5 | 0 |  |  | Hg | 200 | 365 | 24 |
| [S76] | Na |  |  | Ta |  |  | O |  | 0.091 |  |  | 0.718 |  |  | 0.191 |  | SSR | 1420 | 10 | impreg | Pt | 0.05 | octahedral | 4 | 0.44 | 2.85 | 0 | NaOH |  | Hg | 400 | 365 | 3390 |
| [S76] | Li |  |  | Ta |  |  | O |  | 0.029 |  |  | 0.767 |  |  | 0.203 |  | SSR | 1420 | 10 | impreg | Pt | 0.05 | octahedral | 4 | 0.44 | 2.85 | 0 |  |  | Hg | 400 | 365 | 430 |
| [S76] | K |  |  | Ta |  |  | O |  | 0.146 |  |  | 0.675 |  |  | 0.179 |  | SSR | 1420 | 10 | impreg | Pt | 0.05 | octahedral | 4 | 0.44 | 2.85 | 0 |  |  | Hg | 400 | 365 | 29 |
| [S77] | Na |  |  | Ta |  |  | O |  | 0.091 |  |  | 0.718 |  |  | 0.191 |  | SSR | 770 | 2 | impreg | Ni | 1 |  | 4 |  | 2.5 | 0 | KNO3 |  | Hg | 450 | 365 | 300 |
| [S78] | Ag |  |  | Ta |  |  | O |  | 0.321 |  |  | 0.537 |  |  | 0.142 |  | SSR | 1350 | 5 | PD | NiO | 0.24 | orthorombic | 3.4 | 1 | 1 | 0 |  |  | Xe | 300 | 300 | 138 |
| [S78] | Ag |  |  | Nb |  |  | O |  | 0.434 |  |  | 0.373 |  |  | 0.193 |  | SSR | 1150 | 5 | PD | NiO | 0.24 | orthorombic | 3.4 | 1 | 1 | 0 | AgNO3 |  | Xe | 300 | 300 | 103.5 |
| [S79] | Sr | Cr |  | Ti | Sb |  | O |  | 0.467 | 0.006 |  | 0.255 | 0.016 |  | 0.256 |  | SSR | 1420 | 10 | PD | Pt | 0.3 | octahedral | 2.4 |  | 1.56 | 8 | AgNO3 |  | Xe | 300 | 420 | 156 |
| [S80] | Na | La |  | Ta |  |  | O |  | 0.09 | 0.011 |  | 0.71 |  |  | 0.188 |  | SSR | 1420 | 10 | impreg | NiO | 0.2 |  | 4.09 | 3.2 | 2.56 | 0 | NaOH |  | Hg | 400 | 365 | 19800 |
| [S81] | La |  |  | In |  |  | O |  | 0.46 |  |  | 0.381 |  |  | 0.159 |  | SSR | 1473 | 16 | impreg | RuO2 | 1 | octahedral | 4.425 |  | 1 | 0 |  |  | Hg | 200 | 365 | 5 |
| [S82] | In | Ba |  | Nb |  |  | O |  | 0.199 | 0.475 |  | 0.161 |  |  | 0.166 |  | SSR | 1123 | 8 | impreg | NiO | 1 | cubic | 3.51 | 1.71 | 1.85 | 18.5 |  |  | Hg | 400 | 365 | 54 |
| [S82] | In | Sr |  | Nb |  |  | O |  | 0.24 | 0.366 |  | 0.194 |  |  | 0.2 |  | SSR | 1123 | 8 | impreg | NiO | 1 | cubic | 3.51 | 1.71 | 1.85 | 18.5 |  |  | Hg | 400 | 365 | 27.6 |
| [S82] | In | Ca |  | Nb |  |  | O |  | 0.299 | 0.209 |  | 0.242 |  |  | 0.25 |  | SSR | 1123 | 8 | impreg | NiO | 1 | orthorombic | 3.51 | 1.71 | 1.85 | 18.5 |  |  | Hg | 400 | 365 | 29.6 |
| [S83] | Co | Ca |  | Nb |  |  | O |  | 0.116 | 0.236 |  | 0.365 |  |  | 0.283 |  | SSR | 1123 | 8 | impreg | NiO | 1 | monoclinic | 2.8 | 2.2 | 1.85 | 18.5 |  |  | Xe | 300 | 420 | 1.72 |
| [S83] | Co | Sr |  | Nb |  |  | O |  | 0.09 | 0.403 |  | 0.285 |  |  | 0.221 |  | SSR | 1123 | 8 | impreg | NiO | 1 | cubic | 2.8 | 2.2 | 1.85 | 18.5 |  |  | Xe | 300 | 420 | 1.72 |
| [S83] | Co | Ba |  | Nb |  |  | O |  | 0.074 | 0.515 |  | 0.232 |  |  | 0.18 |  | SSR | 1123 | 8 | impreg | NiO | 1 | cubic | 2.8 | 2.2 | 1.85 | 18.5 |  |  | Xe | 300 | 420 | 2.74 |
| [S84] | Ba | Zn |  | Nb |  |  | O |  | 0.51 | 0.081 |  | 0.23 |  |  | 0.178 |  | SSR | 1123 | 8 | PD | Pt | 0.5 | cubic | 3.82 | 0.61 | 1.35 | 13.5 |  |  | Hg | 400 | 365 | 1416.4 |
| [S84] | Ba |  |  | Ta |  |  | O |  | 0.419 |  |  | 0.368 |  |  | 0.146 |  | SSR | 1123 | 8 | PD | Pt | 0.5 | cubic | 3.82 | 0.61 | 1.35 | 13.5 |  |  | Hg | 400 | 365 | 389.6 |
| [S85] | Sr |  |  | Ti |  |  | O |  | 0.478 |  |  | 0.261 |  |  | 0.262 |  | SSR | 1373 | 15 | PD | Pt | 0.1 |  | 1.7 |  | 2 | 10 |  |  | Xe | 300 | 440 | 390 |
| [S84] | Ba | Ni |  | Nb |  |  | O |  | 0.514 | 0.074 |  | 0.232 |  |  | 0.18 |  | SSR | 1123 | 8 | PD | Pt | 0.5 | cubic | 3.82 | 0.61 | 1.35 | 13.5 |  |  | Hg | 400 | 365 | 136.44 |
| [S84] | Ba | Ni |  | Ta |  |  | O |  | 0.422 | 0.06 |  | 0.371 |  |  | 0.147 |  | SSR | 1123 | 8 | PD | Pt | 0.5 | cubic | 3.82 | 0.61 | 1.35 | 13.5 |  |  | Hg | 400 | 365 | 84.32 |
| [S86] | Ba | Zn |  | Nb |  |  | O |  | 0.51 | 0.081 |  | 0.23 |  |  | 0.178 |  | SSR | 1473 | 32 | impreg | NiO | 1 | cubic | 3.9 | 1.24 | 1.35 | 13.5 |  |  | Hg | 400 | 365 | 584.44 |
| [S87] | K | Ta |  | Zr |  |  | O |  | 0.143 | 0.643 |  | 0.028 |  |  | 0.185 |  | SSR | 1173 | 10 | impreg | Pt | 0.2 |  | 3.54 |  | 3.33 | 0 | KOH |  | Xe | 500 | 420 | 575 |
| [S88] | Sr |  |  | Ti | Fe |  | O |  | 0.097 |  |  | 0.053 | 0.743 |  | 0.107 |  | SSR |  |  |  |  |  |  | 3.7 |  | 1 | 8 |  |  | visible | 250 |  | 85 |
| [S88] | Sr | Bi |  | Ti | Fe |  | O |  | 0.048 | 0.689 |  | 0.026 | 0.184 |  | 0.053 |  | SSR |  |  |  |  |  |  | 3.26 |  | 1 | 8 |  |  | visible | 250 | 420 | 129 |
| [S89] | Na |  |  | Ta |  |  | O |  | 0.091 |  |  | 0.718 |  |  | 0.191 |  | SSR | 1473 | 10 |  |  |  | monoclinic | 3.99 | 23 | 1.11 | 0 |  |  | Hg | 400 | 365 | 1940 |
| [S90] | Ba |  |  | Nb | Co |  | O |  | 0.515 |  |  | 0.232 | 0.074 |  | 0.18 |  | HT | 1023 | 2 | impreg | Pt | 0.5 | cubic | 3 | 19.7 | 0.74 | 18.5 |  |  | Xe | 300 | 420 | 18.1 |
| [S91] | Sr | Cr |  | Ti |  |  | O |  | 0.458 | 0.014 |  | 0.263 |  |  | 0.264 |  | HT | 1373 | 24 | impreg | Pt | 0.4 | cubic | 1.9 | 1.92 | 0.92 | 18.5 |  |  | Hg | 300 | 420 | 84 |
| [S92] | Sr |  |  | Sn |  |  | O |  | 0.345 |  |  | 0.467 |  |  | 0.189 |  | SG |  |  |  | Pt | 0.5 | orthorombic | 4.1 | 0.4 | 0.54 | 13.5 | AgNO3 |  | Hg | 400 | 365 | 8.2 |
| [S93] | Na |  |  | Ta |  |  | O |  | 0.091 |  |  | 0.718 |  |  | 0.191 |  | SG | 1473 | 10 |  |  |  | monoclinic | 3.9 | 23 | 1.11 | 0 |  |  | Hg | 400 | 365 | 2050 |
| [S94] | Na |  |  | Nb |  |  | O |  | 0.14 |  |  | 0.567 |  |  | 0.293 |  | SSR |  |  |  |  |  | polyhedron | 3.08 | 2.08 | 2.38 | 5 |  |  | Hg | 350 | 365 | 950 |
| [S94] | K |  |  | Nb |  |  | O |  | 0.217 |  |  | 0.516 |  |  | 0.267 |  | HT |  |  |  |  |  |  | 3.08 | 2.08 | 2.38 | 5 |  |  | Hg | 350 | 365 | 100 |
| [S94] | Na |  |  | Ta |  |  | O |  | 0.091 |  |  | 0.718 |  |  | 0.191 |  | SG |  |  |  |  |  | cubic | 3.08 | 2.08 | 2.38 | 5 |  |  | Hg | 350 | 365 | 36750 |
| [S94] | K |  |  | Ta |  |  | O |  | 0.146 |  |  | 0.675 |  |  | 0.179 |  | HT |  |  |  |  |  |  | 3.08 | 2.08 | 2.38 | 5 |  |  | Hg | 350 | 365 | 1040 |
| [S95] | Sr | Ba |  | Sn |  |  | O |  | 0.075 | 0.353 |  | 0.407 |  |  | 0.165 |  | HT | 1273 | 3 | impreg | RuO2 | 1 | octahedral | 3.3 | 0.55 | 0.476 | 0 |  |  | Xe | 400 | 420 | 220 |
| [S96] | Na | La |  | Ta | Co |  | O |  | 0.082 | 0.055 |  | 0.648 | 0.023 |  | 0.191 |  | HT | 1423 | 10 | PD | Pt | 0.2 | octahedral | 2.95 |  | 1.85 | 18.5 |  |  | Hg | 300 | 420 | 8.68 |
| [S97] | Bi |  |  | Fe |  |  | O |  | 0.668 |  |  | 0.178 |  |  | 0.153 |  | HT |  |  |  |  |  | rhombohedral | 2.1 |  | 1 | 0 | FeCl3 |  | Hg | 500 | 400 | 7.5 |
| [S98] | Ba |  |  | Zr |  |  | O |  | 0.497 |  |  | 0.33 |  |  | 0.174 |  | PC | 1273 | 6 |  |  |  | cubic | 4.8 | 6.8 | 0.476 | 0 |  |  | Hg | 400 | 365 | 522.5 |
| [S99] | Sr |  |  | Ti |  |  | O |  | 0.333 |  |  | 0.364 |  |  | 0.304 |  | SSR | 1273 | 6 |  |  |  | tetragonal | 3.29 | 9.81 | 0.2 | 0 | HCOOH |  | Hg | 150 | 365 | 218.9 |
| [S99] | Ca |  |  | Ti |  |  | O |  | 0.186 |  |  | 0.444 |  |  | 0.371 |  | HT | 1273 | 6 |  |  |  | tetragonal | 3.29 | 9.81 | 0.2 | 0 | C3H8O |  | Hg | 150 | 365 | 65.1 |
| [S99] | Ba |  |  | Ti |  |  | O |  | 0.439 |  |  | 0.306 |  |  | 0.256 |  | SG | 1273 | 6 |  |  |  | tetragonal | 3.29 | 9.81 | 0.2 | 0 | C3H8O |  | Hg | 150 | 365 | 29.35 |
| [S100] | Sr |  |  | Ti |  |  | O |  | 0.478 |  |  | 0.261 |  |  | 0.262 |  | SSR | 1273 | 3 | PD | Pt | 0.32 | cubic | 3.1 |  | 0.4 | 10 |  |  | Hg | 500 | 365 | 3200 |
| [S101] | Sr |  |  | Ti |  |  | O |  | 0.478 |  |  | 0.261 |  |  | 0.262 |  | SSR | 1273 | 10 | impreg | Pt | 1 | cubic | 3.17 | 3.42 | 2 | 10 |  |  | Hg | 450 | 420 | 78 |
| [S102] | K |  |  | Nb |  |  | O |  | 0.217 |  |  | 0.516 |  |  | 0.267 |  | SSR |  |  | PD | Pt | 0.5 | orthorombic | 3.1 | 8.5 | 0.42 | 12 |  |  | Xe | 400 | 420 | 5170 |
| [S103] | Sr | La |  | Ti |  |  | O |  | 0.363 | 0.144 |  | 0.248 |  |  | 0.232 | 0.014 | SG | 1173 | 10 | impreg | Pt | 3 | cubic | 2.65 | 9.86 | 0.55 | 18.5 | AgNO3 |  | Xe | 300 | 420 | 66.67 |
| [S104] | Ag |  |  | Sb |  |  | O |  | 0.389 |  |  | 0.438 |  |  | 0.173 |  | HT | 1173 | 8 |  |  |  | cubic | 2.98 | 2.5 | 1.85 | 0 | AgNO3 |  | Hg | 300 | 400 | 296 |
| [S105] | Na | Sr |  | Ta |  |  | O |  | 0.089 | 0.017 |  | 0.706 |  |  | 0.187 |  | HT | 1423 | 10 | impreg | NiO | 0.1 | monoclinic | 4.09 | 2.6 | 1.42 | 0 |  |  | Hg | 400 | 365 | 27200 |
| [S105] | Na | Ba |  | Ta |  |  | O |  | 0.068 | 0.215 |  | 0.566 |  |  | 0.15 |  | novel | 1423 | 10 | impreg | NiO | 0.1 | monoclinic | 4.09 | 2.6 | 1.42 | 0 |  |  | Hg | 400 | 365 | 19560 |
| [S105] | Na | Ca |  | Ta |  |  | O |  | 0.089 | 0.016 |  | 0.708 |  |  | 0.188 |  | SSR | 1423 | 10 | impreg | NiO | 0.1 | monoclinic | 4.09 | 2.6 | 1.42 | 0 |  |  | Hg | 400 | 365 | 9860 |
| [S106] | Na |  |  | Ta |  |  | O |  | 0.091 |  |  | 0.718 |  |  | 0.191 |  | SSR | 1473 | 10 |  |  |  | monoclinic | 3.99 | 23 | 1.11 | 0 |  |  | Hg | 400 | 365 | 2600 |
| [S107] | Sr | Ag |  | Ti |  |  | O |  | 0.094 | 0.348 |  | 0.051 |  |  | 0.206 |  | SSR | 1073 | 2 |  |  |  | polyhedron | 3.75 | 2.6 | 0.37 | 0 | AgNO3 |  | Xe | 300 | 410 | 648 |
| [S108] | Sr | Na |  | Ti |  |  | O |  | 0.462 | 0.006 |  | 0.266 |  |  | 0.266 |  | SSR | 1373 | 20 | impreg | Rh | 0.5 |  | 3.5 | 2.6 | 0.75 | 0 |  |  | Hg | 450 | 365 | 22 |
| [S109] | Na | Sr |  | Ta |  |  | O |  | 0.091 | 0.002 |  | 0.717 |  |  | 0.19 |  | SG | 1423 | 10 |  |  |  |  | 4.05 |  | 0.5 | 0 |  |  | Hg | 400 | 365 | 2180 |
| [S110] | Y |  |  | In |  |  | O |  | 0.353 |  |  | 0.456 |  |  | 0.191 |  | SSR | 1373 | 12 |  | Pt | 0.5 | cubic | 3.75 |  | 2.91 | 0 | Na2S | Na2SO3 | Xe | 300 | 420 | 18.88 |
| [S111] | Na | Bi |  | Ta |  |  | O |  | 0.084 | 0.609 |  | 0.132 |  |  | 0.175 |  | SSR |  |  | impreg | NiO | 0.1 | octahedral | 4.27 | 9.44 | 0.476 | 5 |  |  | Hg | 350 | 400 | 59.48 |
| [S112] | Na | La |  | Ta | Cr |  | O |  | 0.056 | 0.225 |  | 0.44 | 0.084 |  | 0.195 |  | SSR | 1423 | 10 | PD | Pt | 0.2 | octahedral | 3.06 | 1 | 1.85 | 18.5 |  |  | Xe | 300 | 420 | 9 |
| [S113] | Na |  |  | Nb |  |  | O |  | 0.14 |  |  | 0.567 |  |  | 0.293 |  | novel | 773 | 5 | impreg | RuO2 | 0.5 | orthorombic | 3.4 | 38 | 0.85 | 0 |  |  | Hg | 400 | 365 | 70 |
| [S114] | Ba |  |  | Sn | Zr |  | O |  | 0.482 |  |  | 0.125 | 0.224 |  | 0.169 |  | HT | 1273 | 6 |  |  |  | cubic | 3.8 | 2.33 | 0.476 | 0 |  |  | Hg | 400 | 365 | 690 |
| [S115] | Ca |  |  | Ti |  |  | O |  | 0.295 |  |  | 0.352 |  |  | 0.353 |  | SSR | 1273 | 10 | PD | Pt | 0.04 |  | 3.5 | 1.7 | 2.5 | 10 | CH4 |  | Xe | 300 | 420 | 11.52 |
| [S116] | Na |  |  | Ta |  |  | O |  | 0.091 |  |  | 0.718 |  |  | 0.191 |  | novel | 1473 | 10 | impreg | NiO | 3 | monoclinic | 3.44 | 24 | 0.909 | 0 |  |  | Hg | 400 | 365 | 9000 |
| [S117] | Sr |  |  | Nb | Al |  | O |  | 0.343 |  |  | 0.364 | 0.106 |  | 0.188 |  | PC | 1673 | 10 | impreg | RuO2 | 1 | cubic | 4.1 | 3.2 | 1 | 10 |  |  | Hg | 100 | 365 | 53.4 |
| [S118] | La |  |  | Ni | Cu |  | O |  | 0.562 |  |  | 0.167 | 0.077 |  | 0.194 |  | SSR | 603 | 2 |  |  |  |  | 2.8 |  | 0.5 | 0 | CH2O |  | Xe | 125 | 400 | 583 |
| [S119] | Sr |  |  | Ti |  |  | O |  | 0.478 |  |  | 0.261 |  |  | 0.262 |  | SG | 973 | 4 | impreg | Au | 1 | cubic | 3.18 | 8.64 | 0.5 | 50 |  |  | Xe | 300 | 400 | 1000 |
| [S120] | Na |  |  | Nb | In |  | O |  | 0.09 |  |  | 0.362 | 0.298 |  | 0.25 |  | SSR | 773 | 12 | PD | Pt | 0.8 |  | 2.91 | 22.9 | 1.11 | 18.5 |  |  | Hg | 400 | 365 | 42.9 |
| [S121] | La |  |  | Fe |  |  | O |  | 0.572 |  |  | 0.23 |  |  | 0.198 |  | SG | 773 | 2 |  |  |  | orthorombic | 2.11 | 25.8 | 2.5 | 10 | AgNO3 |  | Hg | 125 | 420 | 1720 |
| [S122] | Ba |  |  | Ta | Zr |  | O |  | 0.382 |  |  | 0.478 | 0.013 |  | 0.091 |  | SG | 1223 | 20 | impreg | Pt | 0.3 |  | 2.03 | 2.55 | 0.4 | 0 | NaI |  | Xe | 300 | 420 | 1.8 |
| [S123] | Na | K |  | Ta |  |  | O |  | 0.086 | 0.008 |  | 0.716 |  |  | 0.19 |  | co-pre | 1023 | 2 |  |  |  | orthorombic | 3.9 | 20 | 0.285 | 14 |  |  | Hg | 400 | 365 | 1057 |
| [S124] | Na | La |  | Ti |  |  | O |  | 0.059 | 0.417 |  | 0.248 |  |  | 0.255 |  | SG |  |  | PD | Pt | 1 | cubic | 2.25 |  | 1.11 | 18.5 |  |  | Xe | 300 | 420 | 8.2 |
| [S125] | Sr | Cr |  | Ti |  |  | O |  | 0.458 | 0.014 |  | 0.263 |  |  | 0.264 |  | PC | 1373 | 24 | PD | Pt | 0.6 | cubic | 3.34 | 23.2 | 0.925 | 18.5 |  |  | Xe | 300 | 420 | 330.4 |
| [S126] | Na | La |  | Ta |  |  | O |  | 0.089 | 0.011 |  | 0.712 |  |  | 0.189 |  | SG | 1173 | 12 | impreg | NiO | 0.6 | orthorombic | 4 | 4.54 | 0.333 | 10 |  |  | Hg | 400 | 250 | 3450 |
| [S127] | Li |  |  | Nb |  |  | O |  | 0.047 |  |  | 0.628 |  |  | 0.325 |  | HT | 773 | 5 | impreg | RuO2 | 0.5 | amorphous | 4.13 | 12 | 0.833 | 10 |  |  | Hg | 400 | 365 | 103.33 |
| [S128] | Na | La |  | Ta |  |  | O |  | 0.09 | 0.011 |  | 0.71 |  |  | 0.188 |  | HT | 1173 | 12 |  |  |  | orthorombic | 4 | 4.54 | 0.333 | 10 |  |  | Hg | 400 | 365 | 1430 |
| [S129] | Sr | Cr |  | Ti | Ta |  | O |  | 0.476 | 0.001 |  | 0.26 | 0.001 |  | 0.261 |  | SG | 1423 | 20 | PD | Pt | 1 |  | 3.17 | 52.6 | 5 | 20 |  |  | Xe | 300 | 420 | 86.4 |
| [S130] | Ga |  |  | Fe |  |  | O |  | 0.402 |  |  | 0.322 |  |  | 0.277 |  | novel | 1623 | 8 |  |  |  | orthorombic | 2.1 | 56 | 3.33 | 0 |  |  | Xe | 300 | 420 | 722 |
| [S131] | Ag |  |  | Sb |  |  | O |  | 0.389 |  |  | 0.438 |  |  | 0.173 |  | SG | 1173 | 16 |  |  |  | tetragonal | 2.4 |  | 1.11 | 0 | AgNO3 |  | Xe | 300 | 420 | 276 |
| [S132] | Cr |  |  | Ti | Ta |  | O |  | 0.02 |  |  | 0.437 | 0.068 |  | 0.475 |  | novel |  |  | PD | Pt | 0.5 | cubic | 2.91 | 16.6 | 1.11 | 18.5 |  |  | Xe | 300 | 420 | 6.67 |
| [S133] | Ca |  |  | Ta | Zr |  | O |  | 0.161 |  |  | 0.58 | 0.073 |  | 0.141 |  | SG | 1273 | 12 | PD | Pt | 1 |  | 2.63 | 7.28 | 0.555 | 11 | HCOOH |  | Xe | 300 | 420 | 52.4 |
| [S134] | Sr | Ni |  | Ti | Ta |  | O |  | 0.475 | 0.001 |  | 0.26 | 0.004 |  | 0.26 |  | HT | 1173 |  | PD | Pt | 1 | cubic | 3.26 | 22.7 | 5 | 20 |  |  | Xe | 300 | 420 | 561.2 |
| [S135] | Na |  |  | Ta | Bi |  | O |  | 0.091 |  |  | 0.663 | 0.058 |  | 0.189 |  | HT | 1173 |  |  |  |  | orthorombic | 2.91 | 45.1 | 5 | 20 |  |  | Xe | 300 | 420 | 224 |
| [S135] | Na |  |  | Ta | Bi |  | O |  | 0.091 |  |  | 0.663 | 0.058 |  | 0.189 |  | PC | 1173 |  |  |  |  | orthorombic | 2.91 | 45.1 | 5 | 20 |  |  | Xe | 300 | 420 | 876 |
| [S135] | Na |  |  | Ta | Bi |  | O |  | 0.091 |  |  | 0.663 | 0.058 |  | 0.189 |  | novel | 1173 |  |  |  |  | orthorombic | 2.91 | 45.1 | 5 | 20 |  |  | Xe | 300 | 420 | 1108 |
| [S135] | Na |  |  | Ta | Bi |  | O |  | 0.091 |  |  | 0.663 | 0.058 |  | 0.189 |  | novel | 1173 |  |  |  |  | orthorombic | 2.91 | 45.1 | 5 | 20 |  |  | Xe | 300 | 420 | 1355 |
| [S135] | Na |  |  | Ta | Bi |  | O |  | 0.09 |  |  | 0.655 | 0.066 |  | 0.189 |  | novel | 1173 |  |  |  |  | orthorombic | 2.91 | 45.1 | 5 | 20 |  |  | Xe | 300 | 420 | 216 |
| [S136] | Bi | Na |  | Ti |  |  | O |  | 0.493 | 0.054 |  | 0.226 |  |  | 0.227 |  | novel |  |  | PD | Pt | 3 | octahedral | 3.02 | 17.4 | 0.75 | 20 |  |  | Xe | 500 | 420 | 369.8 |
| [S137] | Na |  |  | Ta | Bi |  | O |  | 0.086 |  |  | 0.676 | 0.059 |  | 0.179 |  | novel | 1173 | 10 | impreg | Pt | 0.06 | cubic | 2.95 | 1.35 | 0.5 | 20 |  |  | Xe | 800 | 390 | 17.2 |
| [S138] | Na |  |  | Nb |  |  | O |  | 0.14 |  |  | 0.567 |  |  | 0.293 |  | novel | 873 | 2 | PD | Pt | 0.5 | cubic | 3.29 | 28.6 | 1.11 | 18.5 |  |  | Xe | 300 | 300 | 520.33 |
| [S139] | Sr |  |  | Ti |  |  | O |  | 0.333 |  |  | 0.364 |  |  | 0.304 |  | HT | 823 | 1 |  |  |  | cubic | 3.17 | 98.26 | 0.5 | 18.5 |  |  | Hg | 400 | 365 | 1100 |
| [S140] | Na |  |  | Nb |  |  | O |  | 0.14 |  |  | 0.567 |  |  | 0.293 |  | SSR | 673 | 12 | impreg | Pt | 0.5 | orthorombic | 2.98 |  | 1 | 20 |  |  | Xe | 400 | 300 | 103.3 |
| [S140] | Na |  |  | Nb |  |  | O |  | 0.14 |  |  | 0.567 |  |  | 0.293 |  | PC | 773 | 12 | impreg | Pt | 1.5 | orthorombic | 2.99 |  | 1 | 20 |  |  | Xe | 400 | 300 | 330.3 |
| [S140] | Na |  |  | Nb |  |  | O |  | 0.14 |  |  | 0.567 |  |  | 0.293 |  | SG | 873 | 12 | impreg | Pt | 2.5 | orthorombic | 3.06 |  | 1 | 20 |  |  | Xe | 400 | 300 | 261.1 |
| [S140] | Na |  |  | Nb |  |  | O |  | 0.14 |  |  | 0.567 |  |  | 0.293 |  | HT |  |  | impreg | Pt | 3.5 | orthorombic | 3.09 |  | 1 | 20 |  |  | Xe | 400 | 300 | 7.5 |
| [S141] | K |  |  | Nb |  |  | O |  | 0.217 |  |  | 0.516 |  |  | 0.267 |  | HT | 973 |  |  | Pt | 1 | orthorombic | 3.21 | 1.5 | 2 | 10 |  |  | Xe | 450 |  | 29 |
| [S141] | K |  |  | Nb | Zr |  | O |  | 0.207 |  |  | 0.492 | 0.045 |  | 0.255 |  | HT | 973 |  |  | Pt | 1 | orthorombic | 3.2 | 1.83 | 2 | 10 |  |  | Xe | 450 |  | 175.41 |
| [S141] | K |  |  | Nb | Zr |  | O |  | 0.192 |  |  | 0.456 | 0.115 |  | 0.236 |  | HT | 973 |  |  | Pt | 1 | orthorombic | 3.16 | 2.96 | 2 | 10 |  |  | Xe | 450 |  | 886.87 |
| [S141] | K |  |  | Nb | Zr |  | O |  | 0.181 |  |  | 0.43 | 0.166 |  | 0.223 |  | HT | 973 |  |  | Pt | 1 | orthorombic | 3.08 | 8.55 | 2 | 10 |  |  | Xe | 450 |  | 517.95 |
| [S141] | K |  |  | Nb | Zr |  | O |  | 0.163 |  |  | 0.388 | 0.248 |  | 0.201 |  | HT | 973 |  |  | Pt | 1 | orthorombic | 3.01 | 14.55 | 2 | 10 |  |  | Xe | 450 |  | 520.8 |
| [S141] | K |  |  | Nb | Zr |  | O |  | 0.181 |  |  | 0.43 | 0.166 |  | 0.223 |  | HT | 973 |  |  | Pt | 0.5 | orthorombic | 3.08 | 8.55 | 2 | 10 |  |  | Xe | 450 |  | 895 |
| [S141] | K |  |  | Nb | Zr |  | O |  | 0.181 |  |  | 0.43 | 0.166 |  | 0.223 |  | HT | 973 |  |  | Pt | 2 | orthorombic | 3.08 | 8.55 | 2 | 10 |  |  | Xe | 450 |  | 458.33 |
| [S142] | Sr |  |  | Ti |  |  | O |  | 0.478 |  |  | 0.261 |  |  | 0.262 |  | HT | 1373 | 10 |  |  |  | cubic | 3.2 |  | 1 | 0 |  |  | visible | 420 | 420 | 0.6 |
| [S142] | Sr |  |  | Ti |  |  | O |  | 0.478 |  |  | 0.261 |  |  | 0.262 |  | HT | 1373 | 10 |  | NiO | 0.5 | cubic | 3.2 |  | 1 | 0 |  |  | visible | 420 | 420 | 3 |
| [S142] | Sr |  |  | Ti |  |  | O |  | 0.478 |  |  | 0.261 |  |  | 0.262 |  | HT | 1373 | 10 |  | NiO | 1 | cubic | 3.2 |  | 1 | 0 |  |  | visible | 420 | 420 | 12 |
| [S142] | Sr |  |  | Ti |  |  | O |  | 0.478 |  |  | 0.261 |  |  | 0.262 |  | SSR | 1373 | 10 |  | NiO | 3 | cubic | 3.2 |  | 1 | 0 |  |  | visible | 420 | 420 | 3 |
| [S143] | Na |  |  | Ta |  |  | O |  | 0.091 |  |  | 0.718 |  |  | 0.191 |  | SSR | 1023 | 2 |  |  |  | orthorombic | 3.97 |  | 1 | 10 |  |  | Xe | 300 | 400 | 633 |
| [S143] | Na |  |  | Ta | Nb |  | O |  | 0.095 |  |  | 0.67 | 0.038 |  | 0.197 |  | SSR | 1023 | 2 |  |  |  | orthorombic | 3.9 |  | 1 | 10 |  |  | Xe | 300 | 400 | 717 |
| [S143] | Na |  |  | Ta | Nb |  | O |  | 0.098 |  |  | 0.618 | 0.079 |  | 0.205 |  | SSR | 1023 | 2 |  |  |  | orthorombic | 3.83 |  | 1 | 10 |  |  | Xe | 300 | 400 | 1333 |
| [S143] | Na |  |  | Ta | Nb |  | O |  | 0.102 |  |  | 0.562 | 0.124 |  | 0.213 |  | novel | 1023 | 2 |  |  |  | orthorombic | 3.76 |  | 1 | 10 |  |  | Xe | 300 | 400 | 2000 |
| [S143] | Na |  |  | Ta | Nb |  | O |  | 0.111 |  |  | 0.435 | 0.223 |  | 0.231 |  | novel | 1023 | 2 |  |  |  | orthorombic | 3.69 |  | 1 | 10 |  |  | Xe | 300 | 400 | 2416 |
| [S143] | Na |  |  | Ta | Nb |  | O |  | 0.121 |  |  | 0.285 | 0.342 |  | 0.252 |  | novel | 1023 | 2 |  |  |  | cubic | 3.62 |  | 1 | 10 |  |  | Xe | 300 | 400 | 1583 |
| [S143] | Na |  |  | Ta | Nb |  | O |  | 0.127 |  |  | 0.199 | 0.409 |  | 0.264 |  | novel | 1023 | 2 |  |  |  | cubic | 3.55 |  | 1 | 10 |  |  | Xe | 300 | 400 | 1366 |
| [S143] | Na |  |  | Nb |  |  | O |  | 0.14 |  |  | 0.567 |  |  | 0.293 |  | novel | 1023 | 2 |  |  |  | cubic | 3.43 |  | 1 | 10 |  |  | Xe | 300 | 400 | 950 |
| [S144] | Ca |  |  | Ti |  |  | O |  | 0.295 |  |  | 0.352 |  |  | 0.353 |  | novel | 453 | 15 | impreg | Pt | 1 | orthorombic | 3.51 | 5.37 | 1 | 0 | Na2SO3 |  | Hg | 500 | 400 | 156 |
| [S144] | Ca | La |  | Ti | Cr |  | O |  | 0.27 | 0.049 |  | 0.322 | 0.018 |  | 0.34 |  | novel | 453 | 15 | impreg | Pt | 1 |  | 2.49 | 14.69 | 1 | 0 | Na2SO3 |  | Hg | 500 | 250 | 495 |
| [S144] | Ca | La |  | Ti | Cr |  | O |  | 0.27 | 0.049 |  | 0.322 | 0.018 |  | 0.34 |  | novel | 453 | 15 | impreg | Pt | 1 |  | 2.49 | 14.69 | 1 | 0 | Na2SO3 |  | Hg | 500 | 400 | 98.1 |
| [S144] | Ca | La |  | Ti | Cr |  | O |  | 0.247 | 0.095 |  | 0.295 | 0.036 |  | 0.328 |  | HT | 453 | 15 | impreg | Pt | 1 |  | 2.48 | 9.72 | 1 | 0 | Na2SO3 |  | Hg | 500 | 250 | 268 |
| [S144] | Ca | La |  | Ti | Cr |  | O |  | 0.247 | 0.095 |  | 0.295 | 0.036 |  | 0.328 |  | HT | 453 | 15 | impreg | Pt | 1 |  | 2.48 | 9.72 | 1 | 0 | Na2SO3 |  | Hg | 500 | 400 | 116 |
| [S144] | Ca | La |  | Ti | Cr |  | O |  | 0.205 | 0.177 |  | 0.245 | 0.066 |  | 0.307 |  | HT | 453 | 15 | impreg | Pt | 1 |  | 2.5 | 9.51 | 1 | 0 | Na2SO3 |  | Hg | 500 | 250 | 324 |
| [S144] | Ca | La |  | Ti | Cr |  | O |  | 0.205 | 0.177 |  | 0.245 | 0.066 |  | 0.307 |  | HT | 453 | 15 | impreg | Pt | 1 |  | 2.5 | 9.51 | 1 | 0 | Na2SO3 |  | Hg | 500 | 400 | 163 |
| [S145] | Zn |  |  | Cd |  |  | S |  | 0.27 |  |  | 0.465 |  |  | 0.265 |  | HT | 413 | 12 |  |  |  | cubic | 2.47 | 162 | 0.333 | 0 | Na2S | Na2SO3 | Xe | 300 | 420 | 7582 |
| [S145] | Zn | Cu |  | Cd |  |  | S |  | 0.265 | 0.05 |  | 0.465 |  |  | 0.265 |  | HT | 413 | 12 |  |  |  | cubic | 2.45 | 202.2 | 0.333 | 0 | Na2S | Na2SO3 | Xe | 300 | 420 | 12934 |
| [S145] | Zn | Cu |  | Cd |  |  | S |  | 0.26 | 0.011 |  | 0.465 |  |  | 0.265 |  | HT | 413 | 12 |  |  |  | cubic | 2.43 | 206.5 | 0.333 | 0 | Na2S | Na2SO3 | Xe | 300 | 420 | 21318.8 |
| [S145] | Zn | Cu |  | Cd |  |  | S |  | 0.254 | 0.016 |  | 0.465 |  |  | 0.265 |  | HT | 413 | 12 |  |  |  | cubic | 2.41 | 197.7 | 0.333 | 0 | Na2S | Na2SO3 | Xe | 300 | 420 | 13870.6 |
| [S145] | Zn | Cu |  | Cd |  |  | S |  | 0.249 | 0.021 |  | 0.465 |  |  | 0.265 |  | HT | 413 | 12 |  |  |  | cubic | 2.39 | 167.1 | 0.333 | 0 | Na2S | Na2SO3 | Xe | 300 | 420 | 13870.6 |
| [S145] | Zn | Cu |  | Cd |  |  | S |  | 0.243 | 0.026 |  | 0.465 |  |  | 0.265 |  | HT | 413 | 12 |  |  |  | cubic | 2.38 | 163 | 0.333 | 0 | Na2S | Na2SO3 | Xe | 300 | 420 | 10927 |
| [S146] | Sr | La |  | Ti | Cr |  | O |  | 0.417 | 0.073 |  | 0.228 | 0.028 |  | 0.254 |  | HT | 473 | 48 | impreg | Pt | 1 | cubic | 2.31 | 7.0301 | 1 | 10 | NaOH |  | Xe | 300 | 250 | 64 |
| [S146] | Sr | La |  | Ti | Cr |  | O |  | 0.417 | 0.073 |  | 0.228 | 0.028 |  | 0.254 |  | HT | 473 | 48 | impreg | Pt | 1 | cubic | 2.31 | 7.0301 | 1 | 10 | NaOH |  | Xe | 300 | 400 | 28.8 |
| [S146] | Ca | La |  | Ti | Cr |  | O |  | 0.247 | 0.095 |  | 0.295 | 0.036 |  | 0.328 |  | HT | 473 | 48 | impreg | Pt | 1 | orthorombic | 2.52 | 3.3447 | 1 | 10 | NaOH |  | Xe | 300 | 250 | 32 |
| [S146] | Ca | La |  | Ti | Cr |  | O |  | 0.247 | 0.095 |  | 0.295 | 0.036 |  | 0.328 |  | HT | 473 | 48 | impreg | Pt | 1 | orthorombic | 2.52 | 3.3447 | 1 | 10 | NaOH |  | Xe | 300 | 400 | 6 |
| [S146] | Ba | La |  | Ti | Cr |  | O |  | 0.529 | 0.059 |  | 0.184 | 0.022 |  | 0.205 |  | HT | 473 | 48 | impreg | Pt | 1 | tetragonal | 2.49 | 22.4631 | 1 | 10 | NaOH |  | Xe | 300 | 250 | 5.83 |
| [S146] | Ba | La |  | Ti | Cr |  | O |  | 0.529 | 0.059 |  | 0.184 | 0.022 |  | 0.205 |  | HT | 473 | 48 | impreg | Pt | 1 | tetragonal | 2.49 | 22.4631 | 1 | 10 | NaOH |  | Xe | 300 | 400 | 2 |
| [S147] | Sr | Bi |  | Ta |  |  | O |  | 0.087 | 0.413 |  | 0.358 |  |  | 0.142 |  | HT | 1273 | 2 |  |  |  | orthorombic | 4.21 |  | 0.5 | 12.5 | AgNO3 |  | Hg | 350 |  | 2640 |
| [S147] | Sr | Bi |  | Ta | Ce |  | O |  | 0.087 | 0.409 |  | 0.359 | 0.003 |  | 0.143 |  | HT | 1273 | 2 |  |  |  | orthorombic | 4.61 |  | 0.5 | 12.5 | AgNO3 |  | Hg | 350 |  | 2470 |
| [S147] | Sr | Bi |  | Ta | Ce |  | O |  | 0.087 | 0.405 |  | 0.36 | 0.005 |  | 0.143 |  | HT | 1273 | 2 |  |  |  | orthorombic | 4.78 |  | 0.5 | 12.5 | AgNO3 |  | Hg | 350 |  | 3000 |
| [S147] | Sr | Bi |  | Ta | Ce |  | O |  | 0.087 | 0.401 |  | 0.361 | 0.008 |  | 0.143 |  | SSR | 1273 | 2 |  |  |  | orthorombic | 5.06 |  | 0.5 | 12.5 | AgNO3 |  | Hg | 350 |  | 3460 |
| [S147] | Sr | Bi |  | Ta | Ce |  | O |  | 0.088 |  |  | 0.362 | 0.01 |  | 0.144 |  | SSR | 1273 | 2 |  |  |  | orthorombic | 5.85 |  | 0.5 | 12.5 | AgNO3 |  | Hg | 350 |  | 4640 |
| [S148] | Na |  |  | Ti |  |  | O |  | 0.085 |  |  | 0.531 |  |  | 0.384 |  | SSR | 453 | 4 |  |  |  | amorphous | 3.58 | 48 | 0.5 | 0 |  |  | UV | 300 | 254 | 85 |
| [S148] | Na |  |  | Ti |  |  | O |  | 0.085 |  |  | 0.531 |  |  | 0.384 |  | SSR | 673 | 4 |  |  |  | amorphous | 3.58 | 29 | 0.5 | 0 |  |  | UV | 300 | 254 | 128 |
| [S148] | Na |  |  | Ti |  |  | O |  | 0.085 |  |  | 0.531 |  |  | 0.384 |  | SSR | 873 | 4 |  |  |  | monoclinic | 3.58 | 22 | 0.5 | 0 |  |  | UV | 300 | 254 | 213 |
| [S148] | Na |  |  | Ti |  |  | O |  | 0.085 |  |  | 0.531 |  |  | 0.384 |  | novel | 1073 | 4 |  |  |  | monoclinic | 3.58 | 12 | 0.5 | 0 |  |  | UV | 300 | 254 | 179 |
| [S148] | Na |  |  | Ti |  |  | O |  | 0.085 |  |  | 0.531 |  |  | 0.384 |  | novel | 873 | 4 | impreg | NiO | 2 | monoclinic | 3.59 | 22 | 0.5 | 0 |  |  | UV | 300 | 254 | 389 |
| [S148] | Na |  |  | Ti | Zr |  | O |  | 0.079 |  |  | 0.409 | 0.156 |  | 0.356 |  | novel | 673 | 2 |  |  |  | monoclinic | 3.62 | 21 | 0.5 | 0 |  |  | UV | 300 | 254 | 1896 |
| [S148] | Na |  |  | Ti | Zr |  | O |  | 0.079 |  |  | 0.409 | 0.156 |  | 0.356 |  | novel | 673 | 2 | impreg | NiO | 2 | monoclinic | 3.61 | 21 | 0.5 | 0 |  |  | UV | 300 | 254 | 2482 |
| [S149] | La |  |  | Fe |  |  | O |  | 0.572 |  |  | 0.23 |  |  | 0.198 |  | novel | 1273 | 10 | PD | Pt | 0.5 | orthorombic | 2.2 |  | 1 | 10 |  |  | Xe | 300 | 420 | 133 |
| [S149] | La |  |  | Fe | Ti |  | O |  | 0.575 |  |  | 0.196 | 0.03 |  | 0.199 |  | novel | 1273 | 10 | PD | Pt | 0.5 | orthorombic | 2.1 |  | 1 | 10 |  |  | Xe | 300 | 420 | 300 |
| [S149] | La | Sr |  | Fe |  |  | O |  | 0.502 | 0.056 |  | 0.237 |  |  | 0.204 |  | novel | 1273 | 10 | PD | Pt | 0.5 | orthorombic | 1.5 |  | 1 | 10 |  |  | Xe | 300 | 420 | 33.33 |
| [S149] | La | Sr |  | Fe | Ti |  | O |  | 0.521 | 0.042 |  | 0.227 | 0.008 |  | 0.203 |  | flux | 1273 | 10 | PD | Pt | 0.5 | orthorombic | 1.5 |  | 1 | 10 |  |  | Xe | 300 | 420 | 53.33 |
| [S149] | La | Sr |  | Fe | Ti |  | O |  | 0.557 | 0.014 |  | 0.206 | 0.022 |  | 0.2 |  | flux | 1273 | 10 | PD | Pt | 0.5 | orthorombic | 1.5 |  | 1 | 10 |  |  | Xe | 300 | 420 | 426.67 |
| [S149] | La | Sr |  | Fe | Ti |  | O |  | 0.539 | 0.028 |  | 0.217 | 0.015 |  | 0.201 |  | flux | 1273 | 10 | PD | Pt | 0.5 | orthorombic | 2 |  | 1 | 10 |  |  | Xe | 300 | 420 | 560 |
| [S150] | Sr |  |  | Ti | Al |  | O |  | 0.471 |  |  | 0.257 | 0.014 |  | 0.258 |  | flux | 1273 | 10 |  | Au | 0.1 | cubic | 3.3 |  | 2.5 | 20 |  |  | Xe | 150 |  | 200 |
| [S150] | Sr |  |  | Ti | Al |  | O |  | 0.471 |  |  | 0.257 | 0.014 |  | 0.258 |  | flux | 1273 | 10 |  | Au | 0.1 | cubic | 3.3 |  | 2.5 | 0 | C3H8O |  | Xe | 150 |  | 200 |
| [S150] | Sr |  |  | Ti | Al |  | O |  | 0.471 |  |  | 0.257 | 0.014 |  | 0.258 |  | flux | 1273 | 10 |  | Au | 0.25 | cubic | 3.3 |  | 2.5 | 20 |  |  | Xe | 150 |  | 270 |
| [S150] | Sr |  |  | Ti | Al |  | O |  | 0.471 |  |  | 0.257 | 0.014 |  | 0.258 |  | SSR | 1273 | 10 |  | Au | 0.25 | cubic | 3.3 |  | 2.5 | 0 | C3H8O |  | Xe | 150 |  | 230 |
| [S150] | Sr |  |  | Ti | Al |  | O |  | 0.471 |  |  | 0.257 | 0.014 |  | 0.258 |  | SSR | 1273 | 10 |  | Au | 0.5 | cubic | 3.3 |  | 2.5 | 20 |  |  | Xe | 150 |  | 255 |
| [S150] | Sr |  |  | Ti | Al |  | O |  | 0.471 |  |  | 0.257 | 0.014 |  | 0.258 |  | SSR | 1273 | 10 |  | Au | 0.5 | cubic | 3.3 |  | 2.5 | 0 | C3H8O |  | Xe | 150 |  | 250 |
| [S150] | Sr |  |  | Ti |  |  | O |  | 0.478 |  |  | 0.261 |  |  | 0.262 |  | SSR | 1273 | 10 |  | Au | 0.25 | cubic | 3.4 |  | 2.5 | 20 |  |  | Xe | 150 |  | 10 |
| [S150] | Sr |  |  | Ti |  |  | O |  | 0.478 |  |  | 0.261 |  |  | 0.262 |  | SSR | 1273 | 10 |  | Au | 0.25 | cubic | 3.4 |  | 2.5 | 0 | C3H8O |  | Xe | 150 |  | 150 |
| [S150] | Sr |  |  | Ti | Al |  | O |  | 0.474 |  |  | 0.259 | 0.007 |  | 0.26 |  | SSR | 1273 | 10 |  | Au | 0.25 | cubic | 3.45 |  | 2.5 | 20 |  |  | Xe | 150 |  | 40 |
| [S150] | Sr |  |  | Ti | Al |  | O |  | 0.474 |  |  | 0.259 | 0.007 |  | 0.26 |  | SSR | 1273 | 10 |  | Au | 0.25 | cubic | 3.45 |  | 2.5 | 0 | C3H8O |  | Xe | 150 |  | 210 |
| [S150] | Sr |  |  | Ti | Al |  | O |  | 0.467 |  |  | 0.255 | 0.022 |  | 0.256 |  | SSR | 1273 | 10 |  | Au | 0.25 | cubic | 3.45 |  | 2.5 | 20 |  |  | Xe | 150 |  | 275 |
| [S150] | Sr |  |  | Ti | Al |  | O |  | 0.467 |  |  | 0.255 | 0.022 |  | 0.256 |  | SSR | 1273 | 10 |  | Au | 0.25 | cubic | 3.45 |  | 2.5 | 0 | C3H8O |  | Xe | 150 |  | 345 |
| [S151] | La |  |  | Co |  |  | O |  | 0.565 |  |  | 0.24 |  |  | 0.195 |  | SSR | 1073 | 2 |  |  |  | rhombohedral | 1.42 |  | 1 | 0 | CH2O |  | Xe | 500 |  | 14.37 |
| [S151] | La |  |  | Co |  |  | O |  | 0.565 |  |  | 0.24 |  |  | 0.195 |  | SSR | 773 | 2 |  | Au | 0.1 | rhombohedral | 1.42 |  | 1 | 0 | CH2O |  | Xe | 500 |  | 22.75 |
| [S151] | La |  |  | Co |  |  | O |  | 0.565 |  |  | 0.24 |  |  | 0.195 |  | SSR | 773 | 2 |  | Au | 0.5 | rhombohedral | 1.42 |  | 1 | 0 | CH2O |  | Xe | 500 |  | 33.53 |
| [S151] | La |  |  | Co |  |  | O |  | 0.565 |  |  | 0.24 |  |  | 0.195 |  | SG | 773 | 2 |  | Au | 1 | rhombohedral | 1.42 |  | 1 | 0 | CH2O |  | Xe | 500 |  | 28.74 |
| [S151] | La |  |  | Co |  |  | O |  | 0.565 |  |  | 0.24 |  |  | 0.195 |  | SG | 773 | 2 |  | Au | 2 | rhombohedral | 1.42 |  | 1 | 0 | CH2O |  | Xe | 500 |  | 26.94 |

Table A2. Database for stability analysis of individual perovskites

| Ref | Full Name of Perovskite | A site | A2 site | B site | B2 site | Duration of cycles (h) | PRODUCTION RATE (μmol gcat-1 h-1) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  | cycle1 | cycle2 | cycle3 | cycle4 | cycle5 | cycle6 | cycle7 | cycle8 | cycle9 | cycle10 |
| [A152] | KTiNbO5 | K |  | Ti | Nb | 3.0 | 350.0 | 350.3 | 350.0 | - | - | - | - | - | - | - |
| [A152] | HTiNbO5 | H |  | Ti | Nb | 3.0 | 400.0 | 393.3 | 386.7 | - | - | - | - | - | - | - |
| [A152] | KTiTaO5 | K |  | Ti | Ta | 3.0 | 195.0 | 187.0 | 180.7 | - | - | - | - | - | - | - |
| [A152] | HTiTaO5 | H |  | Ti | Ta | 3.0 | 257.7 | 248.0 | 243.3 | - | - | - | - | - | - | - |
| [A153] | Cd0.5Zn0.5S | Zn |  | Cd |  | 5.0 | 2100.0 | 2160.0 | 2280.0 | - | - | - | - | - | - | - |
| [A154] | HTiNbO5 | H |  | Ti | Nb | 1.0 | 263.3 | 397.0 | 245.3 | - | - | - | - | - | - | - |
| [A74] | La:NaTaO3 | Na | La | Ta |  | 3.0 | 5866.7 | 5333.3 | 5266.7 | - | - | - | - | - | - | - |
| [A74] | NaTaO3 | Na |  | Ta |  | 2.0 | 2130.0 | 1795.0 | 1690.0 | - | - | - | - | - | - | - |
| [A75] | Ca2Sb2O7 | Ca |  | Sb |  | 5.0 | 14.8 | 8.7 | 7.4 | 8.2 | - | - | - | - | - | - |
| [A75] | Sr2Sb2O7 | Sr |  | Sb |  | 5.0 | 21.6 | 23.0 | 26.0 | 23.0 | - | - | - | - | - | - |
| [A76] | NaTaO3 | Na |  | Ta |  | 1.0 | - | - | - | - | - | - | - | - | - | - |
| [A78] | AgTaO3 | Ag |  | Ta |  | 22.0 | 80.5 | 50.0 | 46.8 | - | - | - | - | - | - | - |
| [A81] | CaIn2O4 | Ca |  | In |  | 3.9 | 53.5 | 46.0 | 46.0 | - | - | - | - | - | - | - |
| [A82] | BaIn0.5Nb0.5O3 | Ba |  | In | Nb | 10.0 | 0.4 | 0.3 | - | - | - | - | - | - | - | - |
| [A82] | CaIn0.5Nb0.5O3 | Ca |  | In | Nb | 12.0 | 0.2 | 0.2 | - | - | - | - | - | - | - | - |
| [A82] | SrIn0.5Nb0.5O3 | Sr |  | In | Nb | 13.0 | 0.0 | 0.0 | - | - | - | - | - | - | - | - |
| [A85] | Rh:SrTiO3 | Sr |  | Ti | Rh | 6.0 | 238.3 | 230.0 | - | - | - | - | - | - | - | - |
| [A86] | BaZn0.33Nb0.67O3 | Ba |  | Zn | Nb | 14.9 | 319.2 | 182.7 | - | - | - | - | - | - | - | - |
| [A91] | Cr:SrTiO3 | Sr | Cr | Ti |  | 43.7 | 44.9 | 44.4 | 47.6 | 47.6 | 48.7 | 49.4 | 54.7 | 54.2 | 59.0 | 57.0 |
| [A98] | BaZrO3 | Ba |  | Zr |  | 11.2 | 500.0 | 455.6 | - | - | - | - | - | - | - | - |
| [A104] | Sr:NaTaO3 | Na | Sr | Ta |  | 2.5 | 22240.0 | 12800.0 | - | - | - | - | - | - | - | - |
| [A111] | Na0.6La0.4Ta0.6Cr0.4O3 | Na | La | Ta | Cr | 88.2 | 7.3 | 9.2 | 10.9 | - | - | - | - | - | - | - |
| [A112] | NaNbO3 | Na |  | Nb |  | 13.0 | 73.1 | 84.6 | - | - | - | - | - | - | - | - |
| [A118] | LaNi0.7Cu0.3O3 | La |  | Ni | Cu | 1.1 | 515.0 | 512.4 | 501.8 | 485.8 | - | - | - | - | - | - |
| [A124] | Cr:SrTiO3 | Sr | Cr | Ti |  | 12.1 | 332.2 | 306.6 | 283.5 | - | - | - | - | - | - | - |
| [A125] | La:NaTaO3 | Na | La | Ta |  | 9.9 | 26.9 | 27.1 | 27.1 | 26.8 | - | - | - | - | - | - |
| [A127] | La:NaTaO3 | Na | La | Ta |  | 7.0 | 2800.0 | 2785.7 | 2785.7 | - | - | - | - | - | - | - |
| [A135] | Bi0.5Na0.5TiO3 | Bi | Na | Ti |  | 5.0 | 352.0 | 346.0 | 342.0 | 356.0 | - | - | - | - | - | - |
| [A155] | K2Ti6O13 | K |  | Ti |  | 2.5 | 8720.0 | 8760.0 | 8640.0 | 8120.0 | 8240.0 | 8240.0 | 7920.0 | 7800.0 | - | - |
| [A11] | Zn0.8Cd0.2S | Zn |  | Cd |  | 4.9 | 970.0 | 1140.0 | 1114.0 | 914.0 | - | - | - | - | - | - |
| [A156] | AgTa0.7Nb0.3O3 | Ag |  | Ta | Nb | 42.3 | 0.1 | 0.2 | 0.2 | 0.2 | - | - | - | - | - | - |
| [A4] | Rh-Sb:SrTiO3 | Sr |  | Ti | Rh+Sb | 6.9 | 18.3 | 17.4 | 14.6 | - | - | - | - | - | - | - |
| [A5] | Sm2Ti2S2O5 | Sm |  | Ti |  | 5.1 | 46.0 | 29.6 | 14.8 | - | - | - | - | - | - | - |
| [A6] | Ag:ZnIn1.5S3.3 | Ag | Zn | In |  | 4.8 | 3240.0 | 3120.0 | 3220.0 | - | - | - | - | - | - | - |
| [A8] | CuIn0.3Ag0.7S2 | Cu |  | In | Ag | 23.5 | 587.2 | 574.5 | 527.7 | 497.9 | - | - | - | - | - | - |
| [A62] | H2La0.67Ta2O7 | H | La | Ta |  | 11.9 | 1500.0 | 1475.0 | 1491.7 | - | - | - | - | - | - | - |
| [A157] | InNbOx | In |  | Nb |  | 1.5 | 156.7 | 167.3 | 157.3 | - | - | - | - | - | - | - |
| [A65] | Y1.3In0.7O3 | Y |  | In |  | 2.9 | 34.7 | 30.2 | 31.6 | - | - | - | - | - | - | - |
| [A143] | La-Cr:CaTiO3 | Ca | La | Ti | Cr | 2.5 | 536.0 | 648.0 | 764.0 | - | - | - | - | - | - | - |
| [A140] | Zr:KNbO3 | K |  | Nb | Zr | 6.0 | 888.3 | 800.0 | 776.7 | 773.3 | 776.7 | - | - | - | - | - |
| [A139] | NaNbO3 | Na |  | Nb |  | 4.9 | 336.0 | 364.0 | 350.0 | - | - | - | - | - | - | - |
| [A40] | InTaO4 | In |  | Ta |  | 7.0 | 2.0 | 1.5 | 1.0 | - | - | - | - | - | - | - |
| [A53] | Ca2Ta2O7 | Ca |  | Ta |  | 6.0 | 298.3 | 280.0 | 311.7 | - | - | - | - | - | - | - |
| [A158] | Rh:SrTiO3 | Sr |  | Ti | Rh | 9.9 | 937.0 | 933.0 | 931.0 | - | - | - | - | - | - | - |
| [A59] | NiGa2O4 | Ni |  | Ga |  | 9.6 | 102.0 | 100.0 | 95.9 | 91.1 | - | - | - | - | - | - |
| [A159] | Zn0.2Cd0.8S | Zn |  | Cd |  | 4.9 | 1674.0 | 1586.0 | 1424.0 | - | - | - | - | - | - | - |
| [A76] | Ba2InTaO6 | Ba |  | In | Ta | 5.0 | 310.0 | 304.0 | 298.0 | 294.0 | 230.0 | - | - | - | - | - |
| [A160] | HTiNbO5 | H |  | Ti | Nb | 10.0 | 4810.0 | 4750.0 | 4750.0 | - | - | - | - | - | - | - |
| [A16] | CaIn2S4 | Ca |  | In |  | 7.9 | 30.9 | 30.4 | 30.8 | 30.4 | - | - | - | - | - | - |
| [A44] | Sr2Ta2O7 | Sr |  | Ta |  | 4.0 | 4725.0 | 4625.0 | - | - | - | - | - | - | - | - |
| [A28] | ZNIn2S4 | Zn |  | In |  | 20.1 | 286.0 | 284.0 | 227.0 | - | - | - | - | - | - | - |
| [A19] | Bi0.5Na0.5TiO3 | Bi | Na |  | Ti | 5.0 | 356.0 | 350.0 | 346.0 | 362.0 | - | - | - | - | - | - |
| [A17] | SbNbO4 | Sb |  | Nb |  | 2.3 | 8.8 | 8.4 | 8.6 | - | - | - | - | - | - | - |
| [A17] | SbTaO4 | Sb |  | Ta |  | 1.0 | - | - | - | - | - | - | - | - | - | - |
| [A161] | Zn0.5Cd0.5S | Zn |  | Cd |  | 6.0 | 1003.3 | 1015.0 | 991.7 | - | - | - | - | - | - | - |
| [A162] | KTiNbO5 | K |  | Ti | Nb | 1.5 | 3900.0 | 3233.3 | 3066.7 | - | - | - | - | - | - | - |
| [A163] | Zn0.8Cd0.2S | Zn |  | Cd |  | 4.0 | 3450.0 | 3150.0 | 2750.0 | - | - | - | - | - | - | - |
| [A25] | K4NB6O17 | K |  | Nb |  | 3.0 | 30433.3 | 30566.7 | 30400.0 | - | - | - | - | - | - | - |
| [A48] | SrTiO3 | Sr |  | Ti |  | 4.9 | 268.0 | 232.0 | - | - | - | - | - | - | - | - |
| [A42] | La2AlTaO7 | La |  | Ta | Al | 10.0 | 1090.0 | 977.0 | 950.0 | - | - | - | - | - | - | - |
| [A56] | ZNIn2S4 | Zn |  | In |  | 3.0 | 383.3 | 413.3 | 386.7 | 420.0 | 383.3 | - | - | - | - | - |
| [A164] | BaZrO3 | Ba |  | Zr |  | 9.2 | 509.8 | 493.5 | - | - | - | - | - | - | - | - |

References for Database

[A1] Y. Ham, T. Hisatomi, Y. Goto, Y. Moriya, Y. Sakata, A. Yamakata, J. Kubota, K. Domen, J. Mater. Chem. A, 2016, 4, 3027.

[A2] S. M. A. Shibli, P. S. Arun, A. V. Raj, RSC Adv.,2015, 5, 19393.

[A3] F. Cai, Y. Meng, B. Hu, Y. Tang, W. Shi , RSC Adv., 2015, 5, 57354.

[A4] R. Asai, H. Nemoto, Q. Jia, K. Saito, A. Iwase, A. Kudo, Chem. Commun., 2014, 50, 2543.

[A5] W. Zhao, K. Maeda, F. Zhang, T. Hisatomi, K. Domen, Phys. Chem. Chem. Phys., 2014, 16, 12051.

[A6] F. Li, J. Luo, G. Chen, Y. Fan, Q. Huang, Y. Luo, D. Li, Q. Meng, Catal. Sci. Technol., 2014, 4, 1144.

[A7] T. Takayama, K. Tanabe, K. Saito, A. Iwase, A. Kudo, Phys. Chem. Chem. Phys., 2014, 16, 24417.

[A8] X. Yu, A. An, A. Shavel, M. Ibanez, A. Cabot, J. Mater. Chem. A, 2014, 2, 12317.

[A9] C. C. Hu, T. F. Yeh, H. Teng, Catal. Sci. Technol., 2013, 3, 1798.

[A10] T. Zhang, K. Zhao, J. Yu, J. Jin, Y. Qi, H. Li, X. Hou, G. Liu, Nanoscale, 2013, 5, 8375.

[A11] D. H. Wang, L. Wang, A. W. Xu, Nanoscale, 2012,  4, 2046.

[A12] Y. Yuan, Z. Zhao, J. Zheng, M. Yang, L. Qiu, Z. Li, Z. Zou, J. Mater. Chem.,2010, 20, 6772.

[A13] H. Lee, Y. Park, M. Kang, J. Indust. Eng. Chem., 2013, 19, 1162.

[A14] D. Arney, L. Fuoco, J. Boltersdorf, P. A. Maggard, J. Am. Ceram. Soc.,2012, 96, 1158.

[A15] J. Kim, Y. Sohn, M. Kang, Int. J. Hydrogen Energy, 2013, 38, 2136.

[A16] J. Ding, S. Sun, W. Yan, J. Bao, C. Gao, Int. J. Hydrogen Energy, 2013, 38, 13153.

[A17] S. H. Kim, S. Park, S. W. Lee, B. S. Han, S. W. Seo, J. S. Kim, I. S. Cho, K. S. Hong, Int. J. Hydrogen Energy, 2012, 37, 16895.

[A18] W. Chen, C. Li, H. Gao, J. Yuan, W. Shangguan, J. Su, Y. Sun, Int. J. of Hydrogen Energy, 2012, 37, 12846.

[A19] D. H. Wang, L. Wang, A. W. Xu, Nanoscale, 2012,  4, 2041.

[A20] P. Kanhere, J. Zheng, Z. Chen, Int. J. Hydrogen Energy, 2012, 37, 4889.

[A21] C. W. Lee, D. W. Kim, I. S. Cho, S. Park, S. S. Shin, S. W. Seo, K. S. Hong, Int. J. Hydrogen Energy, 2012, 37, 10557.

[A22] B. Zielinska, E. Mijowska, R. J. Kalenczuk, Mater. Charact., 2012, 68, 71.

[A23] P. Wu, J. Shi, Z. Zhou, W. Tang, L. Guo, Int. J. Hydrogen Energy,  2012, 37, 13704.

[A24] B. Naik, S. Martha, K. M. Parida, Int. J. Hydrogen Energy, 2011, 36, 2794.

[A25] C. Zhou, G. Chen, Q. Wang, J. Mol. Catal. A Chem, 2011, 339, 37.

[A26] Y. Huang, Y. Li, Y. Wei, M. Huang, J. Wu, Sol. Energ. Mat. Sol. C., 2011, 95, 1019.

[A27] Q. Li, T. Kako, J. Ye, Int. J. Hydrogen Energy, 2011, 36, 4716.

[A28] W. J. Fan, Z. F. Zhou, W. B. Xu, Z. F. Shi, F. M. Ren, H. H. Ma, S. W. Huang, Int. J. Hydrogen Energy, 2010, 35, 6525.

[A29] Y. Li, Y. Huang, J. Wu, M. Huang, J. Lin, J. Hazard. Mater., 2010, 177, 458.

[A30] J. Li, J. Zeng, L. Jia, W. Fang, Int. J. Hydrogen Energy, 2010, 35, 12733.

[A31] Y. Li, G. Chen, H. Zhang, Z. Lv, Int. J. Hydrogen Energy, 2010, 35, 2652.

[A32] L. M. Torres-Martinez, R. Gomez, O. Vazquez-Cuchillo, I. Juarez-Ramirez, A. Cruz-Lopez, F. J. Alejandre-Sandoval, Catal. Commun., 2010, 12, 268.

[A33] H. Yoshida, M. Takeuchi, M. Sato, L. Zhang, T. Teshima, M. G. Chaskar, Catal. Today, 2014, 232, 158.

[A34] Y. Li, S. Jing, J. Xiao, Y. Li, Int. J. Hydrogen Energy, 2014, 39, 731.

[A35] Y. Li, H. Gou, J. Lu, C. Wang, Int. J. Hydrogen Energy, 2014, 39, 13481.

[A36] W. Chen, X. Chen, Y. Yang, J. Yuan, W. Shangguan, Int. J. Hydrogen Energy, 2014, 39, 1.

[A37] P. Jana, C. M. Montero, P. Pizarro, J. M. Coronado, D. P. Serrano, V. A. P. O’Shea, Int. J. Hydrogen Energy, 201, 39, 5283.

[A38] C. Gomez-Solis, M. A. Ruiz-Gomez, L. M. Torres-Martinez, I. Juarez-Ramirez, D. Sanchez-Martinez, Fuel, 2014, 130, 221.

[A39] Z. Wu, G. Li, F. Zhang, W. Zhang, Appl. Surf. Sci., 2014, 319, 372.

[A40] Y. C. Chiou, U. Kumar, J. C. S. Wu, Appl. Catal. A, 2009, 357, 73.

[A41] S. C. Yan, Z. Q. Wang, Z. S. Li, Z. G. Lou, Solid State Ionics, 2009, 180, 1539.

[A42] Y. Li, G. Chen, H. Zhang, Z. Li, J. Phys. Chem. Solids, 2009, 70, 536.

[A43] Y. Li, G. Chen, H. Zhang, Z. Li, Mater. Res. Bull., 2009, 44, 741.

[A44] C. Zhou, G. Chen, Y. Li, H. Zhang, J. Pei, Int. J. Hydrogen Energy, 2009, 34, 2113.

[A45] Y. Li, J. Wu, Y. Huang, M. Huang, J. Lin, Int. J. Hydrogen Energy, 2009, 34, 7927.

[A46] Y. Wei, J. Li, Y. Huang, M. Huang, J. Lin, J. Wu, T, Sol. Energy Mater. Sol. Cells, 2009, 93, 1176.

[A47] H. Zhang, G. Chen, X. Li, Q. Wang, Q., Int. J. Hydrogen Energy, 2009, 34, 3631.

[A48] T. Puangpetch, T. Sreethawong, S. Yoshikawa, S. Chavadej, J. Mol. Catal. A, 2009, 312, 97.

[A49] G. Li, T. Kako, D. Wang, Z. Zou, J. Ye, J. Phys. Chem. Solids, 2008, 69, 2487.

[A50] Y. Li, G. Chen, H. Zhang, Z. Li, J. Sun, J. Solid State Chem., 2008, 181, 2653.

[A51] Y. Liu,  L. Xie, Y. Li, R. Yang, J. Qu, Y. Li, X. Li, , J. Power Sources,  2008, 183, 701.

[A52] C.C. Hu, H. Teng, Appl. Catal. A, 2007, 331, 44.

[A53] S. Ikeda, M. Fubuki, Y. K. Takahara, M. Matsumura, Appl. Catal. A,  2006,  300, 186.

[A54] H. Jeong, T. Kim, D. Kim, K. Kim, Int. J. Hydrogen Energy, 2006, 31, 1142.

[A55] K. Yoshioka, V. Petrykin, M. Kakihana, H. Kato, A. Kudo, J. Catal., 2005, 232, 102.

[A56] K. Song, R. Zhu, F. Tian, G. Cao, F. Ouyang, J. Solid State Chem., 2015, 232, 138.

[A57] A. M. Huerta-Flores, L. M. Torres-Martinez, D. Sanchez-Martinez, M. E. Zarazua-Morin., Fuel, 2015, 158, 66.

[A58] C. Zeng, T. Hu, N. Hou, S. Liu, W. Gao, R. Cong, T. Yang, Mater. Res. Bull., 2015,  61, 481.

[A59] S. Zhou, X. Lv, C. Zhang, X. Huang, L. Kang, Z. Lin, Y. Chen, W. Fu, Chempluschem, 2015, 80, 223.

[A60] N. C. Hildebrandt, J. Soldat, R Marschall, Small, 2015, 11, 2051.

[A61] K. Song, J. Yang, P. Jiang, W. Gao, R. Cong, T. Yang, Eur. J. Inorg. Chem, 2015, 5786.

[A62] K. Shimizu, S. Itoh, T. Hatamachi, T. Kodama, M. Sato, K. Toda, Chem. Mater., 2005, 17, 5161.

[A63] R. Abe, M. Higashi, K. Sayama, Y. Abe, H. Sugihara, J. Phys. Chem. B, 2006, 110, 2219.

[A64] D. Chen, J. Ye, Chem. Mater., 2007, 19, 4585.

[A65] N. Arai, N. Saito, H. Nishiyama, Y. Shimodaria, H. Kobayashi, Y. Inoue, K. Sato, J. Phys. Chem., 2008, 112, 5000.

[A66] Q. Ding, Y. Yuan, X. Xiong, R. Li, H. Huang, Z. Li, T. Yu, Z. Zou, S. Yang, J. Phys. Chem,  2008, 112, 18846.

[A67] J. Lv, T. Kako, Z. Li, Z. Zou, J. Ye, J. Phys. Chem. C, 2010, 114, 6157.

[A68] A. Mukherji, C. Sun, S. C. Smith, G. Q. Lu, L. Wang, J. Phys. Chem C, 2011, 115, 15674.

[A69] D. Xu, S. Yang, Y. Jin, M. Chen, W. Fan, B. Luo, W. Shi, Langmuir, 2015, 31, 9694.

[A70] T. Grewe, H. Tüysüz, T. Grewe, H. Tüysüz, ACS Appl. Mater. Interfaces,  2015, 7, 23153.

[A71] Q. Zhang, Z. L, S. Wang, R. Li, X. Zhang, Z. Liang, H. Han, S. Lia, C. Li, Catal., 2016, 6, 2182.

[A72] A. Kudo, I. Mikami, J. Chem. Soc., Faraday. Trans., 1998, 94, 2929.

[A73] T. Ishihara, H. Nishiguchi, K. Fukamachi, Y. Takita, J. Phys. Chem. B, 1999, 103, 1.

[A74] A. Kudo, H. Kato, Chem. Phys. Lett., 2000, 331, 373.

[A75] J. Sato, N. Saito, H. Nishiyama, Y. Inoue, J. Photochem. Photobiol. A,  2002, 148, 85.

[A76] H. Kato, A. Kudo, J. Phys. Chem., 2001, 105, 4285.

[A77] H. Kato, A. Kudo, Phys. Chem. Chem. Phys, 2002, 4, 2833.

[A78] H. Kato, H. Kobayashi, A. Kudo, J. Phys. Chem. B, 2002, 106, 12441.

[A79] H. Kato, A. Kudo, J. Phys. Chem. B,  2002, 106, 5029.

[A80] H. Kato, K. Asakura, A. Kudo, J. Am. Chem. Soc., 2003, 125, 3082.

[A81] J. Sato, N. Saito, H. Nishiyama, Y. Inoue, J. Phys. Chem. B, 2003, 107, 7965.

[A82] J. Yin, Z. Zou, J. Ye, J. Phys. Chem. B, 2003, 107, 61.

[A83] J. Yin, Z. Zou, J. Ye, J. Phys. Chem., 2003, 107, 4936.

[A84] J. Yin, Z. Zou, J. Ye, J. Phys. Chem. B,2004, 108, 8888.

[A85] R. Konta, T. Ishii, H. Kato, A. Kudo, J. Phys. Chem. B, 2004, 108, 8992.

[A86] J. Yin, Z. Zou, J. Ye, J. Phys. Chem. B, 2004, 108, 12790.

[A87] H. Hagiwara, T. Inoue, K. Kaneko, T. Ishihara, Chem. Eur. J, 2009, 15, 12862.

[A88] J. Luo, and P. A. Maggard, Adv. Mater.,2006, 18, 514.

[A89] W. Lin, C. Cheng, C. Hu, H. Tong, Appl. Phys. Lett., 2006, 89, 211904.

[A90] J. Yin, Z. Zou, J. Ye, J. Mater. Sci., 2006, 41, 1131.

[A91] D. Wang, J. Ye, T. Kako, T. Kimura, J. Phys. Chem. B, 2006, 110, 15824.

[A92] D. Chen, J. Ye, Chem. Mater., 2007, 19, 4585.

[A93] C.C. Hu, H. Teng, Appl. Catal. A, 2007, 331, 44.

[A94] J. W. Liu., G. Chen, Z. H. Li, Z. G. Zhang, Int. J. of Hydrogen Energy, 2007, 32, 2269.

[A95] Y. Yuan, J. Lv, X. Jiang, Z. Li, T. Yu, Z. Zou, J. Ye, Appl. Phys. Lett., 2007, 91, 094107.

[A96] Z. G. Li, J. H. Ye, Appl. Phys. Lett., 2007, 91, 254108.

[A97] U. A. Joshi, J. S. Jang, P. H. Borse, J. S. Lee, Appl. Phys. Lett., 2008, 92, 242106.

[A98] Y. Yuan, X. Zhang, L. Liu, X. Hiang, J. Lv, Z. Li, Z. Zou, Int. J. Hydrogen Energy, 2008, 33, 5941.

[A99] B. Zielinska, E. Borowiak-Palen, R. J. Kalenczuk, Int. J. Hydrogen Energy, 2008, 33, 1797.

[A100] Y. Liu,  L. Xie, Y. Li, R. Yang, J. Qu, Y. Li, X. Li, , J. Power Sources,  2008, 183, 701.

[A101] S. W. Bae, P. H. Borse, J. S. Lee, Appl. Phys. Lett., 2008, 92, 104107.

[A102] Q. Ding, Y. Yuan, X. Xiong, R. Li, H. Huang, Z. Li, Z. Zou, S. Yang, J. Phys. Chem., 2008, 112, 18846.

[A103] W. Luo, Z. Li, X. Jiang, T. Yu, L. Liu, X. Chen, J. Ye, Z. Zou, Phys. Chem. Chem. Phys., 2008, 10, 6717.

[A104] T. Kako, N. Kikugawa, J. Ye, Catal. Today, 2008,  131, 197.

[A105] A. Iwase, H. Kato, A. Kudo, ChemSusChem, 2009, 2, 873.

[A106] C. Hu, C. Tsai, H. Teng, J. Am. Ceram. Soc., 2009, 92, 460.

[A107] T.Ishii, H.Kato, A.Kudo, J. Photochem. Photobiol. A, 2004, 163, 181.

[A108] T. Takata, K. Domen, J. Phys. Chem. Lett., 2009, 113, 19386.

[A109] M. Maruyama, A. Iwase, H. Kato, A. Kudo, H. Onishi, J. Phys. Chem. C., 2009, 113, 13918.

[A110] J. Ding, J. Bao, S. Sun, Z. Luo, C. Gao, J. Comb.Chem.,2009, 11, 523.

[A111] Z. Li, Y. Wang, J. Li, G. Chen, Y. Li, Z. Zhou, Int. J. Hydrogen Energy,  2009, 34, 147.

[A112] Z. G. Li, J. H. Ye, J. Appl. Phys., 2009, 106, 074910.

[A113] K. Saito, A. Kudo, Inorg. Chem., 2010, 49, 2017.

[A114] Y. Yuan, Z. Zhao, J. Zheng, M. Yang, L. Qiu, Z. Li, Z. Zou, J. Mater. Chem.,2010, 20, 6772.

[A115]	K. SHimura, H. Yoshida, Energy Environ. Sci., 2010, 3, 615.

[A116] C. C. Hu, H. Teng, J. Catal., 2010, 272, 1.

[A117] H. Iwakura, H. Einaga, Y. Teraoka, Inorg. Chem., 2010, 49, 11362.

[A118] J. Li, L. Jia, W. Fang, J. Zeng, Int. J. Hydrogen Energy, 2010, 35, 5270.

[A119] T. Puangpetch, T. Sreethawong, S. Chavadej, Int. J. Hydrogen Energy,  2010, 35, 6531.

[A120] J. Lv, T. Kako, Z. Li, Z. Zou, J. Ye, J. Phys. Chem. C, 2010, 114, 6157.

[A121] K. M. Parida, K. H. Reddy, S. Martha, D. P. Nas, N. Biswal, Int. J. Hydrogen Energy, 2010, 35, 12161.

[A122] T. Matoba, K. Maeda, K. Domen, Chem. Eur. J., 2011,  17. 14731.

[A123] J. Sun, G. Chen, Y. Li, R. Jin, Q. Wang, J. Pei, Energy Environ. Sci., 2011, 4, 4052.

[A124] J. Shi, J. Ye, Z. Zhou, M. Li, L. Guo, Chem. Eur. J., 2011, 17, 7858.

[A125] H. Yu, S. Ouyang, S. Yan, Z. Li, T. Yu, Z. Zou, J. Mater. Chem., 2011, 21, 11347.

[A126] H. Husin, W. N. Su, H. M. Chen, C. J. Pan, S. H. Chang, J. Rick, W. T. Chuang, H. S. Sheu, B. J. Hwang, Green Chem., 2011, 13, 1745.

[A127] K. Saito, K. Koga, A. Kudo, Dalton Trans., 2011, 40, 3909.

[A128] H. Husin, W. N. Su, H. M. Chen, C. J. Pan, S. H. Chang, W. T. Chuang, H. S. Sheu, B. J. Hwang, Appl Catal B, 2011, 102, 343.

[A129] H. W. Kang, S. B. Park, Int. J. Hydrogen Energy, 2011, 36, 9496.

[A130] P. Dhanasekaran, N. M. Gupta, Int. J. Hydrogen Energy, 2012, 37, 4897.

[A131] J. SHi, J. Ye, Q. Li, Z. Zhou, H. Tong, G. Xi, L. Guo, Chem. Eur. J., 2012, 18, 3157.

[A132] S. Ouyang, H. Tong, N. Umezawa, J. Cao, P. Li, Y. Bi, Y. Zhnag, J. Ye, J. Am. Chem. Soc., 2012, 134, 1974.

[A133] P. Wu, J. Shi, Z. Zhou, W. Tang, L. Guo, Int. J. Hydrogen Energy,  2012, 37, 13704.

[A134] H. W. Kang, S. N. Lim, S. B. Park, Int. J. Hydrogen Energy, 2012, 37, 5540.

[A135] H. W. Kang, S. N. Lim, S. B. Park, Int. J. Hydrogen Energy, 2012, 37, 4026.

[A136] L. Wang, W. Wang, Int. J. Hydrogen Energy, 2012, 37, 3041.

[A137] P. Kanhere, J. Zheng, Z. Chen, Int. J. Hydrogen Energy, 2012, 37, 4889.

[A138] P. Li, S. Ouyang, G. Xi, T. Kako, J. Ye, J. Phys., Chem. C, 2012, 116, 7621.

[A139] H. Bai, J. Juay, Z. Liu, X. Song, S. S. Lee, D. D. Sun, Appl. Catal. B, 2012, 125, 367.

[A140] Q. Liu, L. ZHang, Y. Chai, W. Dai, J. Phys. Chem.,  2017,  121, 25898.

[A141] I. Mondal, M. Srikanth, K. Srinivasu, Y. Soujanya, U. Pal, J. Phys. Chem. C, 2017, 121, 2597.

[A142] K. Han, Y. Lin, C. Yang, R. Jong, G. Mul, B. Mel, ChemSusChem, 2017, 10, 4510.

[A143] M. Wang, M. Fang, X. Min, Z. Huang, C. Tang, Y. Liu, X. Wu, Chem. Phys. Lett., 2017, 686, 18.

[A144] R. Wang, S. Ni, G. Liu, X. Xu, Appl. Catal. B, 2018, 225, 139.

[A145] Z. Mei, B. ZHang, J. Zheng, S. Yuan, Z. Zhuo, X. Meng, Z. Chen, K. Amine, W. Yang, L. Wang, W. Wang, S. Wang, Q. Gong, J. Li, F. Liu, F. Pan, Nano Energy,  2016, 26, 405.

[A146] L. Lu, S. Ni, G. Liu, X. Xu, Int. J. Hydrogen Energy, 2017, 42, 23539.

[A147] V. Senthil, T. Badapanda, A. Chithambararaj, A. Chandra Bose, S. Panigrahi, Int. J. Hydrogen Energy, 2016, 41, 22856.

[A148] A. M. Huerta-Flores, L. M. Torres-Martinez, E. Moctezuma, Int. J. Hydrogen Energy, 2017, 42, 14547.

[A149] M. Hojambedriev, K. Kawashima, M. Kumar, A. Yamakata, K. Yabuta, A. Gurlo, M. Hasegawa, K. Domen, K. Teshima, Int. J. Hydorgen Energy, 2017, 42, 27024.

[A150] D. Saadetnejad, R. Yıldırım, Int. J. Hydrogen Energy, 2018, 43, 1116.

[A151] B. Zhang, J. Liu, S. Yue, Y. Teng, Z. Wang, X. Li, S. Qu, Z. Wang, Appl. Catal. B,  2017, 432.

[A152] J. S. Jang, H. G. Kim, V. R. Reddy, S. W. Bae, S. M. Ji, J. S. Lee, J. Catal., 2005, 231, 213.

[A153] B. Gong, Y. Lu, P. Wu, Z. Huang, Y. Zhu, Z. Fang, N. Zhu, G. Lu, J. Huang, Appl. Sur. Sci., 2016, 365, 280.

[A154] H. Lin, Y. Chang, Int. J. Hydrogen Energy, 2014, 39, 3118.

[A155] J. Cai, Y. Zhu, D. Liu, M. Meng, Z. Hu, Z. Jiang, ACS Catal., 2015,  5, 1708.

[A156] L. Ni, M. Tanabe, H. Irie, Chem. Commun, 2013, 49, 10094.

[A157] H. Lin, H. Huang, W. Wang, Microporous Mesoporous Mater., 2008, 115, 568.

[A158] P. Shen, J. C. Lofaro Jr., W. R. Woerner, M. G. White, D. Su, A. Orlov, Chem. Eng. J., 2013, 223, 200.

[A159] X. Wang, G. Liu, Z. Chen, F. Li, G. Q. Lu, H. Cheng, Electrochem. Commun., 2009, 11, 1174.

[A160] X. Fan, B. Lin, H. Liu, L. He, Y. Chen, B. Gao, Int. J. Hydorgen Energy,  2013, 38, 832.

[A161] C. Chan, C. Chang, C. Hsu, Y. Weng, K. Chen, H. Lin, W. Huang, S. Cheng, Int. J. Hydrogen Energy, 2014, 39, 1630.

[A162] H. Lin, Y. Chang, Int. J. Hydrogen Energy,  2010, 35, 8463.

[A163] Y. ZHou, Y. Wang, T. Wen, S. Zhang, B. Zhang, Y. Guo, B. Yang, J. Colloid Interface Sci, 2016, 467, 97.

[A164]Y. Yuan, X. Zhang, L. Liu, X. Jiang, J. Lv, Z. Li, Z. Zou, Int. J. Hydrogen Energy, 2008, 33, 5941.